## Slide 1: MIT 3.022 Microstructural Evolution in Materials 12: Nucleation
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Thermodynamics of phase transition
G
Liquid
Crystal
Tm
Tm
Supercooled liquid
Crystal
Liquid
H
T
T
Notes: Crystal melting usually does not require superheating due to surface nucleation. For example, the surface energies of ice/water follows the Antonov’s rule, and therefore there is no surface energy barrier for liquid water formation on solid ice surface.

## Slide 3: Homogeneous nucleation from a fluid phase
r
Crystal nucleus
Liquid
Volumetric
Surface

## Slide 4: Thermodynamics of homogeneous nucleation
Volumetric Gibbs free energy change
Surface energy change
G
Liquid
Crystal
Tm
T

## Slide 5: Gibbs free energy change in solidification
Gibbs free energy change of nucleation
Critical nucleus size
Energy barrier towards nucleation
Nucleus size r
Gibbs free energy change

## Slide 6: Vapor-liquid nucleation of water

## Slide 7: “Seeing” nucleation using atomic tomography
https://www.nature.com/articles/s41586-019-1317-x

## Slide 8: Density of critical nuclei
Number of clusters with size greater than r
Example: number of ice clusters in 1 g of water at 0 °C
  r > 0.4 nm (~ 9 molecules): 1.3 × 1015
  r > 0.7 nm (~ 48 molecules): 0.7
where
g = 0.033 J/m2, DHm = 333.6 J/g, Tm = 273.15 K
A supercooling threshold exists for onset of nucleation events
Notes: The pre-exponential factor n0 is usually linked to atomic numbers in the classical nucleation theory. This is, however, heuristic. See for example, Ford, I. J. "Statistical mechanics of nucleation: a review“ for more detailed discussions.

## Slide 9: Homogeneous nucleation rate
Nucleation rate I
  Number of nuclei with size just under r* × Rate of atoms hopping to the nuclei
I
DT
Nucleation onset
0
Driving force limited
Diffusion limited

## Slide 10: Experimental measurement of nucleation rate
T
t
Tm
Liquid
Nucleation
Growth
Nucleation zone
Nucleation rate in lithium silicate glass
Nucleation zone
Adapted from Phys. Chem. Glasses 15, 95 (1974)
Notes: For vapor-liquid transition latest technology leverages Mie scattering measurement to quantify nucleation rate

## Slide 11: Heterogeneous nucleation
Gibbs free energy change of cluster formation
  Volumetric term
  Surface term
Substrate
Cluster
Y-L equation:
Liquid

## Slide 12: Heterogeneous nucleation
Gibbs free energy change of cluster formation
  Volumetric term
  Surface term

## Slide 13: Heterogeneous nucleation
Critical nucleus size
Energy barrier towards nucleation
Nucleus size r
Gibbs free energy change
Wetting on a substrate reduces energy barrier towards nucleation

## Slide 14: Nucleation kinetics and grain size
Acta Mater. 54, 5591 (2006)
Fast cooling and addition of secondary phase contribute to grain refinement
Magnesium alloy w/o SiC particles
Magnesium alloy with SiC particles
Notes: http://innomag.gkss.de/english/projekte/15/index.html

## Slide 15: Vapor-Liquid-Solid (VLS) nanowire growth
Substrate
Melted gold nanoparticles saturated with SiH4
SiCl4 vapor + H2
Heterogeneous nucleation of Si at the interface
Substrate
Growth direction
Interface where growth continues
Temperature for Si deposition on a planar substrate (homogeneous nucleation): ~ 800 ˚C
Diameter of nanowire is determined by the gold droplet size

## Slide 16: Nanowires formed by VLS growth
Gold nano-particle
Growth direction
S. Kodambaka, J. Tersoff, M. C. Reuter, and F. M. Ross, Science 316, 729 (2007).

## Slide 17: Why gold?
“The influence of the surface migration of gold on the growth of silicon nanowires,” Nature 440, 69-71 (2006).
Reason #1:
Low eutectic temperature
Question: what would happen if we were to grow nanowires at high temperature?

## Slide 18: Why gold?
Reason #2:
Small gold solubility in Si (Eutectoid transformation)
Question: why is such small solubility important?
Albert P. Levitt, Whisker Technology (1975)
99.8%
Solubility: 0.2%

## Slide 19: Summary
Driving force for nucleation
  Supercooling (undercooling)
  Volumetric Gibbs free energy reduction
Energy barrier against nucleation
  Surface energy
Kinetics of nucleation
  Number of sub-critical nuclei
  Diffusion
Heterogeneous nucleation
  Lowering the surface energy barrier of nucleation

## Slide 20: List of symbols
T – temperature
k – Boltzmann constant (1.38 × 10-23 m2 kg s-2 K-1)
GL / HL / SL – Gibbs free energy / enthalpy / entropy of liquid
GC / HC / SC – Gibbs free energy / enthalpy / entropy of crystalline solid
Tm – melting point
DG – Gibbs free energy change associated with phase transition
DGV / DGS – volumetric / surface contributions to Gibbs free energy change of phase transition
r – radius of nucleus

## Slide 21: List of symbols
DHm – enthalpy of fusion per unit volume
V – volume of nucleus
DT – supercooling, defined as:
g – surface/interface energy
S – surface area of nucleus
r* – critical nucleus size
DG* – energy barrier towards nucleation
nr – number of clusters with size greater than r
n0 – number of atoms/molecules in the system (see discussions at the notes section of slide 7)
I – nucleation rate

## Slide 22: List of symbols
nh – frequency of successful atomic hops from liquid phase to the nucleus
n – vibrational frequency of atoms in the liquid phase
D – diffusion coefficient (from liquid phase to the nucleus)
a – atomic hopping distance
VC – volume of cluster (which serves as a nucleus in heterogenous nucleation process)
gSL / gSC / gLC – interface energy between S: substrate, C: cluster, and L: liquid phase
q – contact angle
– defined as:

## Slide 23: List of symbols
DGhet / DGhomo – Gibbs free energy change associated with heterogeneous / homogeneous nucleation
– critical nucleus size in heterogeneous / homogeneous nucleation
– energy barrier towards heterogeneous nucleation