## Slide 1: MIT 3.022 Microstructural Evolution in Materials 13: Precipitate Growth
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Spherulite nucleation and growth
Video credit: Ian Chesser

## Slide 3: Classifications of precipitate growth
Growth from a single-component solution
  Faceted precipitates: 2-D nucleation controlled
  Precipitates with atomically rough surfaces: interface kinetics controlled
Growth from a binary system with miscibility gap
  Diffusion controlled
Faceted surface

## Slide 4: Classifications of precipitate growth
Temperature
100% A
100% B
DT
a
b
Non-faceted surface
Growth from a single-component solution
  Faceted precipitates: 2-D nucleation controlled
  Precipitates with atomically rough surfaces: interface kinetics controlled
Growth from a binary system with miscibility gap
  Diffusion controlled

## Slide 5: Continuous growth
Continuous growth on atomically rough surface: plenty of surface sites for atom attachment
Growth rate determined by atom attaching rate n h
Non-faceted surface
Liquid
Solid
Ea
Gibbs free energy
Atomic location

## Slide 6: Continuous growth
Volumetric Gibbs free energy change
Growth rate (interface velocity)
Non-faceted surface
Liquid
Solid
Ea
Gibbs free energy
Atomic location

## Slide 7: Growth rate dependence on supercooling
Growth rate
Supercooling DT
Driving force limited regime
Diffusion limited regime
There is no supercooling threshold for continuous growth

## Slide 8: Impact of supercooling on nucleation and growth
Metastable zone of supercooling
Tm
Driving force: supercooling
Both processes are thermally activated
Supercooling
Phase transition
Notes: Here a continuous growth mode is assumed (i.e. no 2-D nucleation is required for growth)

## Slide 9: Time-temperature-transformation (TTT) diagram
R. Busch, JOM 52, 39-42 (2000)
Driving force (supercooling) limited
Diffusion limited

## Slide 10: 2-D nucleation on faceted surfaces
Faceted surface
2-D nucleus
Large surface area
2-D nucleus
“The origin of traveling waves in an emperor penguin huddle,” New J. Phys. 15, 125022 (2013)
R. Gerum et al. 2013 New J. Phys. 15, 125022, CC-BY 3.0

## Slide 11: Free energy barrier for 2-D nucleation
Gibbs free energy change of cluster formation
  “Volumetric” term
  “Surface” term
r
h
2-D nucleus
Crystal precipitate

## Slide 12: Free energy barrier for 2-D nucleation
Gibbs free energy change of cluster formation
  “Volumetric” term
  “Surface” term
DG2D
Nucleus radius r

## Slide 13: Growth rate on faceted planes
In-plane growth rate is much higher than nucleation rate
Growth rate scales with 2-D nucleation rate
Nucleation rate I2D
  Number of 2-D nuclei with size just under r*2D × Rate of atoms hopping to the nuclei
Driving force term
Diffusion term
2-D nucleus

## Slide 14: Growth rate dependence on supercooling
Growth rate
Supercooling DT
Continuous growth
Diffusion limited regime
Supercooling threshold
2-D nucleation

## Slide 15: Screw dislocation assisted growth on facets
Growth via atom attachment to the ledge around a screw dislocation without requiring 2-D nucleation
Growth rate
http://home.gwu.edu/~hteng/resareaone.html
2-D nucleation
Spiral growth
Image Credit: H. Henry Teng
Notes: With increasing supercooling, 2-D nucleation starts to become important (the images are calcite crystal surfaces)

## Slide 16: Precipitate growth from a binary solution
Precipitates generally have compositions different from the solution
Mass transport via diffusion is the rate limiting step
Temperature
100% A
100% B
DT
a
b
b
Continuous phase a
b
b
B
Concentration of B
b
a
a – b interface

## Slide 17: Precipitate growth kinetics
Local equilibrium assumption
The phases a and b are in chemical equilibrium with each other locally on the a – b interface
Concentration of B
b
xa–b
A
B
DT
a
b
C0
Ca
Cb
a
C0
Ca
Cb

## Slide 18: Precipitate growth kinetics
Linear concentration assumption
Flux of B atoms:
Growth rate (interface velocity):
Concentration of B
a
b
L
xa–b
C0
Ca
Cb

## Slide 19: Precipitate growth kinetics
Mass conservation
Excess B in the b phase all comes from the a phase
Concentration of B
a
C0
Ca
b
L
Cb
xa–b
where

## Slide 20: Precipitate growth kinetics
Concentration relationships
A
B
DT
C0
Ca
Cb
a
b

## Slide 21: Growth rate dependence on supercooling
Growth rate
Supercooling DT
Driving force limited regime
Diffusion limited regime
There is no supercooling threshold for diffusion-limited growth

## Slide 22: Summary
Type of precipitate | Single-component system |  | Binary system
 | Faceted (defect-free) | Non-faceted | 
Rate limiting factor | 2-D nucleation | Interface kinetics | Diffusion
Growth rate |  |  | 
Supercooling threshold | Yes | No | No
Comments | 1) Presence of screw dislocations can lead to spiral growth; 2) Transition to continuous growth can occur at large supercooling |  | The formalism above does not apply to the Spinodal region

## Slide 23: List of symbols
DT – supercooling, defined as the difference between the equilibrium and the actual phase transition temperatures
T – temperature
k – Boltzmann constant (1.38 × 10-23 m2 kg s-2 K-1)
n – vibrational frequency of an atom
nh – frequency of successful hops of an atom, i.e. atom attaching rate to an atomically rough surface
nL→S / nS→L – frequency of successful hops of an atom from the liquid / solid phase to the solid / liquid phase
Ea – activation energy of atomic hopping from the liquid phase to the solid phase
g – surface/interface energy

## Slide 24: List of symbols
– volumetric Gibbs free energy difference of an atom in solid and liquid phases
DHm – enthalpy of fusion per unit volume
Tm – melting point
R – precipitate growth rate measured by the velocity of the solid-liquid interface
– volume occupied by one atom
rS – surface density of atoms, i.e. number of atoms per unit surface area
DGV / DGS – volumetric / surface contributions to Gibbs free energy change of phase transition

## Slide 25: List of symbols
r – radius of a 2-D nucleus
h – height of a 2-D nucleus
DG2D – Gibbs free energy change associated with formation of a 2-D nucleus
– critical 2-D nucleus size
– energy barrier towards 2-D nucleation
I2D – 2-D nucleation rate
Ea,2D – activation energy of atomic diffusion to 2-D nuclei
C0 / Ca / Cb – concentration of component B in the sample / in the precipitate phase b / in the continuous phase a that equilibrates with the precipitate phase b

## Slide 26: List of symbols
FB – diffusion flux of component B
DB – diffusion coefficient of component B in the a phase
t – time
L – length of the region near the surface of b phase precipitates where the a phase composition deviates from the bulk continuous phase composition
xa-b – size of the precipitate, defined by the position of the interface between the precipitate and continuous phases
Ea,B – activation energy of diffusion for component B