## Slide 1: MIT 3.022 Microstructural Evolution in Materials 14: Interface Stability
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Dendritic growth
© Aqueous Technologies

## Slide 3: Condition for dendritic growth: interface instability
Liquid
Solid
A
B
x
Stable interface: planar growth
Liquid
Solid
A
B
x
Unstable interface: dendritic growth
Notes: Interface stability deals with macroscopic interface morphology, whereas the Jackson model evaluates atomic scale interface roughness

## Slide 4: Example 1: Bridgman-Stockbarger crystal growth
melt

## Slide 5: Example 1: Bridgman-Stockbarger crystal growth
Liquid
Solid
T
x
Tm
Heat flux
Single-component system

## Slide 6: Example 1: Bridgman-Stockbarger crystal growth
Heat flux continuity at solid-liquid interface
Supercooling in liquid
Liquid
Solid
T
x
Tm
Heat flux
Single-component system
Planar interface: heat removal via the solid side

## Slide 7: Example 2: Solidification in a supercooled liquid
Solid
T
x
Tm
Heat flux
Single-component system
Supercooled liquid
Heat flux continuity at solid-liquid interface
Supercooling in liquid
Heat extraction is more efficient at dendrites

## Slide 8: Dendrite branching and crystallography
Directionally solidified Co-Sm-Cu alloy
<100>
Image credit: University of Cambridge CC BY-NC-SA 2.0 UK
Image credit: Alexey Kljatov CC BY-SA 4.0

## Slide 9
“At sub-zero temperature, moisture from the surrounding atmosphere condenses almost immediately. The dendritic form of the crystallization is a natural fractal pattern.”
– Francis Chee / Science Photo Library

## Slide 10: Example 3: constitutional supercooling
B
b
L
A
C0
a
Solid a
Liquid L
x
CB
Ca
CL
C0
x = 0
Ca
CL
T0

## Slide 11: Example 3: constitutional supercooling
Solid a
Liquid L
x
CB
Ca
CL
C0
Steady state solution
RDt
Growth rate is determined by diffusion of solute away from the interface
x = 0

## Slide 12: Example 3: constitutional supercooling
B
T0
b
L
A
C0
Ca
CL
a
Liquidus temperature
Supercooling in liquid
Interface stability condition

## Slide 13: Example 3: constitutional supercooling
Solid a
Liquid L
x
CB
Ca
CL
C0
Solid a
Liquid L
x
TL
TL (C0)
TL (CL)
Critical T (x)
Supercooling zone DT (x) > 0
x = 0
x = 0

## Slide 14: Summary
Interface stability criterion: supercooling decreases away from the solid-liquid interface
  Single-component system:
  Binary or multi-component system:
In single component systems, latent heat removal from the solid phase side usually indicates stable interface
Phase transition occurring at condition far away from equilibrium (large supercooling) is often accompanied by dendritic growth
Impurities can lead to constitutional supercooling and dendrite growth (even in nominally ‘single-component’ alloys)

## Slide 15: List of symbols
DT – supercooling, defined as the difference between the liquidus temperature and the phase transition temperature
Tm – melting point or liquidus temperature
T – temperature
x – coordinate along the x-axis
kS / kL – thermal conductivity of solid / liquid phase
R – precipitate growth rate measured by the velocity of the solid-liquid interface
DHm – enthalpy of fusion per unit volume
CB – concentration of component B
C0 – concentration of B in the starting liquid phase

## Slide 16: List of symbols
T0 – temperature at which the solidification takes place
Ca / CL – equilibrium concentration of component B in the a / liquid phase at T0
D – diffusion coefficient of B in the liquid phase
TL – liquidus temperature of the A-B binary alloy, which is a function of the alloy composition CB