## Slide 1: MIT 3.022 Microstructural Evolution in Materials 15: Glass Transition
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: 3.071 Amorphous Materials
3-d printing with glass
Sapphire vs. tempered glass: which is better?
Glass
What is Liquidmetal®?
Glass: where arts and science meet

## Slide 3: “The Nature of Glass Remains Anything but Clear”
“What don’t we know?” Science 309, 83 (2005)

## Slide 4: Glass transition
Tm
Supercooled liquid
Crystal
Liquid
H, V
Glass
Glass transition
Suppression of crystallization: glass formation
The glassy state is different from the supercooled liquid state
Fictive temperature
Tf

## Slide 5: Glass structures are dependent on history
H, V
T
Tm
Supercooled liquid
Liquid
Increasing
cooling rate
3
2
1
Glasses obtained at different cooling rates have different structures
Faster cooling results in higher Fictive temperature
Notes: Questions to be addressed:
What is glass?
How fast is “fast enough” during cooling?
Why some materials easily form glass while others do not?
Why glass properties are dependent on thermal history?

## Slide 6: What is glass?
A metastable solid which exhibits glass transition and has no long-range atomic order
G
Structure
Metastable glassy state
Thermodynamically stable crystalline state
Glasses are metastable with respect to their stable crystalline phase
Atoms can rearrange to form a more stable state given enough time and thermal energy

## Slide 7: What is glass?
A metastable solid which exhibits glass transition and has no long-range atomic order
A2O3 crystal
A2O3 glass
Short-range order is preserved (AO3 triangles)
Long-range order is disrupted by changing bond angle (mainly) and bond length
Structure lacks symmetry and is usually isotropic
Zachariasen's Random Network Theory (1932)
A fictitious A2O3 2-D compound:
Notes: Amorphous does not mean random

## Slide 8: Potential energy landscape (PEL)
PE
Atomic coordinates r1, r2, … r3N
Crystal
Ideal glass
Laboratory glass states

## Slide 9: Laboratory glass transition: ergodicity breakdown
Liquid: ergodic
Glass: nonergodic, confined to a few local minima
Inter-valley transition time t :
Liquid
Glass
E : barrier height
n : attempt frequency

## Slide 10: Crystal nucleation and growth
Metastable zone of supercooling
Tm
Driving force: supercooling
Both processes are thermally activated

## Slide 11: Time-temperature-transformation (TTT) diagram
Critical cooling rate Rc
R. Busch, JOM 52, 39-42 (2000)
Driving force (supercooling) limited
Diffusion limited

## Slide 12: Critical cooling rate and glass formation
Technique | Typical cooling rate (°C/s)
Air quench | 1-10
Liquid quench | 103
Droplet spray | 102-104
Melt spinning | 105-108
Selective laser melting | 106-108
Vapor deposition | Up to 1014
Material | Critical cooling rate (°C/s)
Silica | 9 × 10-6
GeO2 | 3 × 10-3
Na2O·2SiO2 | 6 × 10-3
Salol | 10
Water | 107
Vitreloy-1 | 1
Typical metal | 109
Silver | 1010
Maximum glass sample thickness:
a : thermal diffusivity

## Slide 13: Summary
What is glass?
  Metastable solids exhibiting glass transition and lacking long-range order
Why are glass properties history-dependent?
  Glass structure can be trapped in different metastable basins and is path-dependent
How to determine the cooling rate necessary for glass formation?
  Time-temperature-transformation (TTT) diagram

## Slide 14
THE FOLLOWING PREVIEW HAS BEEN APPROVED FOR
ALL 3.022 PARTICIPANTS
R | RESTRICTED
 | VIEWERS WHO HAVEN’T TAKEN KINETICS REQUIRE ACCOMPANYING MIT DMSE STUDENTS
STRONG MATERIALS SCIENCE COMPONENTS | 
www.classratings.com
dmse.mit.edu
®

## Slide 15
We proudly present
“Microstructural Evolution in Foods”
Image Credit: profkarim CC BY-SA 2.0

## Slide 16: List of symbols
H – enthalpy
V – volume
Tm – melting point
T – temperature
Tf – Fictive temperature
G – Gibbs free energy
tobs – observation time, duration of experimental observation
t – intervalley transition time, time it takes for a system to transition from a local metastable energy basin to another
n – attempt frequency or atomic vibrational frequency
k – Boltzmann constant (1.38 × 10-23 m2 kg s-2 K-1)

## Slide 17: List of symbols
E – average energy barrier height between metastable states
Tg – glass transition temperature
Rc – critical cooling rate to prevent crystallization
DT – supercooling corresponding to the nose temperature
a – thermal diffusivity
dmax – maximum thickness of sample that can maintain a homogeneous glassy state