## Slide 1: MIT 3.022 Microstructural Evolution in Materials 2: Solid Solutions
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Solid solution consisting of indistinguishable atoms
In classical mechanics, all particles are distinguishable
In quantum mechanics, two microscopic particles become indistinguishable if:
  The particles are identical
  The wave functions of the particles spatially overlap
Distinguishability does not affect energy but changes entropy
1
2
1+2

## Slide 3
Selena & Eos Hu
Number of states from permutation:

## Slide 4: Gibbs theorem
Solid 1 consisting of n1 atoms on n1 lattice sites
Solid 2 consisting of n2 atoms on n2 lattice sites
Solid solution with the same lattice structure and completely random distribution of atoms
  Inter-atomic force are the same for all three types of atomic pairs: 1-1, 2-2, and 1-2
1
2
1+2
Notes: Assumptions: 1) no crystalline defects; 2) solids 1, 2 and their solution have the same crystal structure and the number of lattice sites is conserved; 3) all atoms distribute randomly on lattice (equal bonding energy for homopolar and heteropolar bonds)

## Slide 5: Gibbs theorem
Ideal (random) solid solution
Entropy of mixing
1
2
1+2

## Slide 6: Ideal solid solutions
Inter-atomic force is the same for all types of bonds
Random mixing is always preferred!

## Slide 7: Gibbs theorem for ideal gas
Entropy of mixing ideal gases (at the same T and P):
Derivation: # of spatial “sites” m >> # of molecules n for ideal gas (classical limit of quantum statistics)
T, P, n1
T, P, n2
Same T and P :

## Slide 8: Regular binary solution theory
Assumptions:
  Random distribution of atoms
  Bond energy between 1-2 is different from those of 1-1 and 2-2
negative enthalpy of mixing: 1-2 type of hetero-polar bond energetically favorable
positive enthalpy of mixing: 1-1 and 2-2 types of homopolar bonds preferred
Site i
Site j
1
2

## Slide 9: Negative enthalpy of mixing

## Slide 10: Positive enthalpy of mixing (high T)

## Slide 11: Positive enthalpy of mixing (intermediate T)

## Slide 12: Positive enthalpy of mixing (low T)

## Slide 13: Phase composition determination
The composition of phases are determined by the common tangent lines on the Gibbs free energy curve
  Minimization of G
The curve is generally asymmetric for real solutions
x1,a
x1,b
DGmix at T = T0
m1
m2
a
b

## Slide 14
Gibbs free energy
Phase diagram
Miscibility gap
Miscible region
Convex G curve: miscible solution
Concave G curve: phase separation

## Slide 15: Summary
Distinguishability of microscopic particles
Gibbs theorem
Ideal solid solution
Regular binary solution
  Negative enthalpy of mixing: single phase solution
  Positive enthalpy of mixing
    High temperature: single phase solution
    Low temperature: miscibility gap
when

## Slide 16: List of symbols
S – entropy
k – Boltzmann constant (1.38 × 10-23 m2 kg s-2 K-1)
W – Number of microscopic states
n – number of atoms in solid solution
N – mole number of component in solid solution
R – Ideal gas constant (8.314 J mol-1 K-1)
V – Volume
x – Molar fraction of component
DSmix / DHmix / DGmix – Entropy / enthalpy / Gibbs free energy of mixing

## Slide 17: List of symbols
T – Temperature
Pi – Probability of atom site i being occupied by atom 1
w – A constant proportional to enthalpy of mixing: w < 0 corresponds to negative enthalpy of mixing, and w > 0 indicates positive enthalpy of mixing
m1,a – Chemical potential of component 1 in a phase