## Slide 1: MIT 3.022 Microstructural Evolution in Materials 6: Substitutional Diffusion
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Vacancy mechanism (substitutional diffusion)
Ultra High Vacuum Scanning Tunneling Microscopy movie showing the thermal migration of a single vacancy on a Ge(111)-c(2×8) surface. The vacancy was deliberately created with the STM tip by a slight tip-sample contact.
Used with permission from the American Physical Society
Brihuega et al., Phys. Rev. B 70, 165410 (2004)

## Slide 3: Frequency of successful hops in substitutional diffusion
Frequency of successful hops
  Frequency of atomic vibration
  Probability of having sufficient energy
  Probability of finding an adjacent vacancy
  = vacancy concentration xv × coordination number Z

## Slide 4: Equilibrium vacancy concentration
Entropy contribution
Enthalpy contribution
Gibbs free energy
Equilibrium vacancy concentration
Notes: Sv is due to vibrational entropy change

## Slide 5: Entropy is the cause of imperfection
DG
Vacancy fraction xv
Equilibrium concentration

## Slide 6: Substitutional self-diffusion
Atom vibration frequency:
Successful hop frequency:
Self diffusion coefficient:
Energy
harmonic potential

## Slide 7: Data for substitutional self-diffusion
Class | Material | Tm (K) | D0 (mm2/s) | ESD (kJ/mol)
BCC alkali metals | Rb | 312 | 23 | 39.4
 | K | 337 | 31 | 40.8
 | Na | 371 | 24.2 | 43.8
 | Li | 454 | 23 | 55.3
FCC | Pb | 601 | 137 | 109.1
 | Al | 933 | 170 | 142.0
 | Ag | 1234 | 40 | 184.6
 | Au | 1336 | 10.7 | 176.9
 | Cu | 1356 | 31 | 200.3
 | Ni | 1726 | 190 | 279.7
Data from Acta. Metall. Mater. 28, 1085 (1980)

## Slide 8: Example: substitutional self-diffusion in gold
A thin layer of radioactive gold is placed on the end of a gold rod. This surface is bonded to another gold crystal and the two are heat treated for 100 h at 920 °C. Estimate the diffusivity of gold.
Point source diffusion:
Diffusion length:
Using data from last slide:

## Slide 9: Vacancy diffusion
An atom hopping into a vacancy is equivalent to the vacancy hopping into that atom’s initial position
Frequency of successful vacancy hops
  Frequency of atomic vibration
  Coordination number
  Probability of having sufficient energy
Diffusion of atoms is always accompanied by an opposing vacancy flux (in the lattice reference frame)

## Slide 10: Interdiffusion in binary alloys
A
B
What happens when ?
B atom
A atom
Vacancy
x

## Slide 11: Re-examine the Fick’s 1st law
Number of atoms hopped from plane 1 to 2 per unit time and per unit area:
1
2
Similarly, the flux from 2 to 1 is:
The net diffusion flux is:
Fick’s 1st law
The flux is defined with respect to lattice planes

## Slide 12: Vacancy diffusion in a binary system
Diffusion flux of atoms with respect to the lattice
Concentration of lattice sites
Net vacancy diffusion flux (with respect to the lattice)

## Slide 13: Sources and sinks of vacancy
Surfaces, voids, grain boundaries, dislocations
Vacancy
Heat treated at 1000 °C in Argon for 1 min
Heat treated at 1000 °C in Argon for 15 min
“An analysis of diffusion-induced porosity in Cu-Ni laminate composites,” A124, I. Choi, D. Matlock, L15-L18, Copyright 1990, with permission from Elsevier.

## Slide 14: Dislocation motion and crystal plane growth/removal
Climb of edge dislocations leads to crystal plane growth/removal
Image Credit: Nick Bagnall; CC0 1.0 Universal License

## Slide 15: The Kirkendall effect
Motion of the boundary between a diffusion pair with different diffusion coefficients
Solder
“Kirkendall voiding is a phenomenon related to the intermetallic formation of a Cu/Sn alloy matrix. When the solder joints solidifies, the intermetallic becomes the bond mechanism between the bulk solder and the Cu pad on the circuit board. Over time, and particularly at elevated temperature, the Cu/Sn intermetallic will increase in thickness. This intermetallic growth is caused by the solid state diffusion of the Cu and the Sn into one another. The Cu diffuses into Sn much faster than Sn diffuses in Cu, which results in vacancies forming throughout the intermetallic bond area.”
http://www.indium.com/blog/intermetallics-in-soldering.php
© unknown
Notes: The voids are in fact formed in Cu3Sn IMC layer rather than in Cu (see for example: http://www.materialenkennis.nl/dico/UserFiles/File/Zacht-solderen-18-jan-2007.pdf)

## Slide 16: Kirkendall effect in nanomaterial synthesis
Nanoshell:
Nanotube:
Nanoscale 6, 12195 (2014); Chem. Commun. 12, 1565 (2009).

## Slide 17: Convective flow: motion of crystal planes
Concentration of lattice sites
Flux of lattice sites (opposing to the vacancy flux)
Velocity of crystal plane motion
where

## Slide 18: Diffusion in the laboratory reference frame
In the laboratory reference frame, both diffusion and convective flow contribute to atomic flux
Interdiffusion coefficient for a binary alloy
The diffusion coefficient of A approaches that of pure A (the solute) when A is dilute in B
Darken equation

## Slide 19: Interdiffusion in ionic solids
Ion exchange in salt bath
Interdiffusion process
  Kinetics limited by slow-moving ion species
Charge neutrality at steady state
Nernst-Planck equation for diffusion in ionic crystals
© BCE
Notes: There is no Kirkendall effect in ionic diffusion pairs because there is no net vacancy flux

## Slide 20: Summary
Substitutional self-diffusion coefficient
Vacancy diffusion
Interdiffusion coefficient in binary metal alloys
Interdiffusion coefficient in binary ionic solids
Darken equation
Nernst-Planck equation
in lattice reference frame

## Slide 21: In a diffusion pair where DA < DB
A
B
B atom
A atom
Vacancy
Lattice frame
Lab frame
Lattice plane

## Slide 22: List of symbols
T – temperature
k – Boltzmann constant (1.38 × 10-23 m2 kg s-2 K-1)
m – mass of an atom
K – effective spring constant of the potential well where an atom is located
xv – fraction of lattice sites occupied by vacancies
xA / xB – fraction of lattice sites occupied by atom A / B
n – number of vacancies in a solid
N – number of atoms in a solid
DSv – vibrational entropy change due to formation of a vacancy

## Slide 23: List of symbols
DHv – enthalpy change due to formation of a vacancy
DGv – defined as : the Gibbs free energy change due to formation of a vacancy minus the configurational entropy contribution
DG – total Gibbs free energy change due to formation of vacancies compared to a defect-free crystal
Z – coordination number
n – vibrational frequency of an atom
nh – frequency of successful hops of an atom
ESD – defined as : activation energy of substitutional diffusion

## Slide 24: List of symbols
Ea – activation energy of atomic hopping
D – diffusivity, diffusion coefficient (of atoms)
a – hopping distance (distance between neighboring lattice sites for substitutional diffusion)
nh,v – frequency of successful hops of a vacancy
x – coordinate along the x-axis
J – diffusion flux of atoms measured in the lattice frame
J’ – diffusion flux of atoms measured in the laboratory frame
Jv – diffusion flux of vacancies

## Slide 25: List of symbols
Js – flux of lattice sites due to vacancy diffusion
C – number concentration of atoms (subscripts A, B, 0, v denote the concentrations of atom A, atom B, all lattice sites, and vacancies, respectively)
v – velocity of crystal plane motion due to the Kirkendall effect (note the difference with the Greek letter n, which represents the atomic vibrational frequency)
– interdiffusion coefficient
Dv – diffusion coefficient of vacancies