## Slide 1: MIT 3.022 Microstructural Evolution in Materials 7: Ionic Defects
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2
Defects are not always bad
Gas sensor
Fuel cell
Solid state battery
The Midas touch
© safety.com
© Consumer Reports
By Peter Welleman
© Butterfield Jewlers
Notes: Turning quartz into amethyst using gamma radiation: http://hyperphysics.phy-astr.gsu.edu/hbase/minerals/amethyst.html

## Slide 3: Charge neutrality
Macroscopic electroneutrality
Consider a sphere made of sodium with radius R = 1 cm. What is the energy needed to remove 0.01% of valence electrons from the sphere?
Site ratio conservation
The ratio of the number of regular cation sites to the number of regular anion sites remains constant
MgO crystal
# Mg = # O

## Slide 4: Ionic defect types
A
Schottky defect (vacancy)
B
Frenkel defect (self-interstitial)
C
Substitutional atom
D
Foreign interstitial

## Slide 5: Kroger-Vink notation
General form:
M – atom type; “V ” denotes vacancy
L – site in the original perfect lattice; “i ” denotes interstitial
C – effective charge (or relative charge), equaling to the difference in valence between the species on the site L and the atom that occupies the site in a perfect crystal
  Positive effective charge
  Negative effective charge
  Neutral defect
Quasi-free electron is denoted by ; hole is denoted by
Square brackets denotes defect fraction, e.g.

## Slide 6: Examples of Kroger-Vink notation
Frenkel defect
Schottky defect
Substitutional atom
Foreign interstitial

## Slide 7: Concentration of Frenkel defects
Configurational entropy
Gibbs free energy
Equilibrium fraction of Frenkel defects
Dislodge n atoms from their sites
Place the atoms into n interstitials
Assume that there is one interstitial per lattice site

## Slide 8: Equilibrium constant of defect reactions
Frenkel defect formation
General defect reactions
e.g.
DGf : Gibbs free energy of defect formation minus the configurational entropy term

## Slide 9: Charge compensation in ionic solids
List all possible defect reactions when TiO2 is doped into Al2O3 and determine the defect concentrations
List all charged species
List defect reactions based on charge compensation pairs
Native vacancies:
Foreign substitutional atom:
Interstitials:
Schottky defect
Notes: Anions (except F) usually don’t form interstitials due to their large size

## Slide 10: Charge compensation in ionic solids (cont’d)
List defect reactions based on charge compensation pairs
Foreign substitution
Frenkel defect
Foreign interstitial

## Slide 11: Charge compensation in ionic solids (cont’d)
Combine all equations along with the overall charge neutrality condition to solve defect concentrations
5 equations, 5 unknown variables: a unique solution set
Question: is mass conservation taken into account?
Notes: Mass conservation is taken into account through the equilibrium constants. In this example, K3 and K4 implicitly imply the amount of TiO2 added into the system.

## Slide 12: Charge compensation in non-stoichiometric solids
List all possible defect reactions in non-stoichiometric TiO2 and determine the defect concentrations
Native vacancies:
Electrons and holes:
List all charged species
(1)
(2)
(3)
(4)
Not all reactions are independent: (4) = (1) + 4 × (2) – (3)
List defect reactions based on charge compensation pairs

## Slide 13: Charge compensation in non-stoichiometric solids
Combine all equations along with the overall charge neutrality condition to solve defect concentrations
The defect concentration depends on oxygen partial pressure
Non-degenerate semiconductors

## Slide 14: Defect concentration: examples
For MgO at 1,000K:
DH (eV) | 
MgO | 6.6
CaO | 6.1
LiF | 2.34
LiCl | 2.12
LiBr | 1.8
LiI | 1.3
DH (eV) | 
CaF2 | 2.8
SrF2 | 2.3
BaF2 | 1.9
AgCl | 1.6
AgBr | 1.2
b-AgI | 0.7
Schottky defect
Frenkel defect
Eg (eV) | 
Si | 1.11
Ge | 0.67
MgO | 7.8
CaO | 7.1
ZnO | 3.2
a-TiO2 | 3.0
Electron-hole pair
Notes: Data source: http://www.tf.uni-kiel.de/matwis/amat/def_en/index.html
The dominant interstitial atom type in Frenkel defects is labeled with red color
At room temperature, the entropy of defect formation has much smaller contribution to Gibbs free energy than that of enthalpy

## Slide 15: Defect concentration: examples
For MgO at 1,000K:
DH (eV) | 
MgO | 6.6
CaO | 6.1
LiF | 2.34
LiCl | 2.12
LiBr | 1.8
LiI | 1.3
Schottky defect
Frenkel defect
Eg (eV) | 
Si | 1.11
Ge | 0.67
MgO | 7.8
CaO | 7.1
ZnO | 3.2
a-TiO2 | 3.0
Electron-hole pair
DH (eV) | 
CaF2 | 2.8
SrF2 | 2.3
BaF2 | 1.9
AgCl | 1.6
AgBr | 1.2
b-AgI | 0.7

## Slide 16: The Brouwer approximation
One charged defect of each sign dominates over all others
Example: charge compensation in undoped MgO
  Regime 1:
  Regime 2:
  Regime 3:
  Regime 4:
Electronic compensation
Schottky compensation
Low oxygen partial pressure
High oxygen partial pressure
Solve the charge carrier concentrations in each regime at one specific temperature

## Slide 17: The Brouwer approximation (cont’d)
Equilibrium constants
High oxygen partial pressure regime:

## Slide 18: The Brouwer approximation (cont’d)
Low oxygen partial pressure regime:
Schottky compensation regime (intermediate oxygen partial pressure):
Notes: In the intermediate regime, the charge neutrality condition does not necessarily mean n = p

## Slide 19
log (defect concentration)
Notes: Charge neutrality and the Brouwer approximation do not hold near the boundaries between regimes: the exact solutions do not exhibit the kinks

## Slide 20: Brouwer diagram for doped crystals
Example: Al-doped stoichiometric MgO
  Neglect electronic carriers
  The primary defect in intrinsic MgO is Schottky defect
  Al-substitution of Mg dominates over interstitial formation
Charge compensation regimes (dependent on Al concentration)
  Regime 1 (intrinsic):
  Regime 2 (extrinsic):
(1)
(2)

## Slide 21
log (defect concentration)
Extrinsic
Intrinsic

## Slide 22: You can “see” ionic defects: F-centers
Na
Cl
F-centers in NaCl crystal: electron trapped at an anion (halide) vacancy
NaCl
KCl
KBr
http://education.mrsec.wisc.edu/background/F_center
Notes: Top right: Figure 6.16, page 180, Materials Science Companion for Teaching General Chemistry Publisher: American Chemical Society
Bottom right: http://education.mrsec.wisc.edu/background/F_center/

## Slide 23: Q & A about g-ray irradiated table salt
Is it still edible?
  Yes. First of all, I tried it. Tastes just like regular table salt.
  Secondly, irradiated salt only contains a small fraction of vacancy defects [in the order of 1017 cm-3 according to J. Appl. Phys. 31, 1688 (1960)]. Since the crystal will ionize when dissolved, these point defects don’t make a difference.
  Lastly, g-radiation normally does not trigger nuclear reactions [Nelson et al. “Gamma-Ray Interactions with Matter”], so we don’t need to worry about induced radioactivity.
Okay, it is fun – but why do we need to care?
  Table salt and doped salt are useful materials for radiation dosimetry. See for example: Radiat. Meas. 46, 1856 (2011).

## Slide 24
Understanding defect reactions
Site ratio conservation
Charge neutrality
Equilibrium constant
Kroger-Vink notation
Brouwer approximation
Frenkel & Schottky concentrations
Doping & non-stoichiometric defects
Defect concentration
Brouwer diagram

## Slide 25: List of symbols
Q – electric charge
C – capacitance (note the difference with C, Coulomb, unit of electric charge)
e0 – vacuum permittivity (8.85 × 10-12 F/m)
e – elementary charge (1.602 × 10-19 C)
E – energy
T – temperature
k – Boltzmann constant (1.38 × 10-23 m2 kg s-2 K-1)
n – number of point defects in a solid (slide 7) or free electron concentration (in the discussion of defect equilibrium)

## Slide 26: List of symbols
DSc – configurational entropy change due to formation of a point defect
xf – fractional of lattice sites populated with Frenkel defects
DGf – Gibbs free energy change due to formation of a Frenkel defect minus the configurational entropy contribution
K – equilibrium constant of a defect reaction
p – hole concentration
NC / NV – effective density of states of conduction / valence band

## Slide 27: List of symbols
Eg – band gap energy
N – number of atoms in a solid