## Slide 1: MIT 3.071 Amorphous Materials 13: Optical Properties
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 19
Introduction to Glass Science and Technology
  Ch. 10

## Slide 3
What's so special about ?

## Slide 4: Refraction
Leeuwenhoek Microscope
A flesh-fiber, split and pressed flat

## Slide 5: Transparency
‘People think that data is in the cloud, but it’s not. It’s in the ocean.’

## Slide 6: Color
Palau de la Musica Catalana, Barcelona

## Slide 7: Maxwell Equations (‘macroscopic’ differential form)
Gauss’s Law:
Gauss’s Law for magnetism:
Faraday’s Law:
Ampere’s Law:
James C. Maxwell (1831-1879)
H | Magnetic field | B | Magnetic induction
E | Electric field | D | Electric displacement
Jf | Free current density | rf | Free charge density

## Slide 8: Constitutive relations in amorphous materials
General form for non-bianisotropic media:
Most amorphous materials are isotropic
  E and D (or B and H) always align in the same direction
  In most non-magnetic glasses, mr is close to 1 (m = m0)
Non-magnetic media
Linear media
Non-magnetic media
Notes: See J. A. Kong’s book for a complete discussion about bianisotropic media

## Slide 9: Refractive index of glass: general trends
Addition of heavy elements increases index
  Lead-containing glasses
Addition of alkali oxides increases index
  NBOs have larger polarizability than BOs
Fictive temperature (density) dependence
Rawson, Properties and Applications of Glasses (1980)

## Slide 10: Kramers-Kronig (K-K) relation
w / w0
a (w)
nr (w) -1
Refractive index n and optical absorption a are not independent quantities!

## Slide 11: Refractive index of glasses
Wavelength/frequency dependent (Lorentz oscillators)
l
n
IR
Visible
Static
UV
X-ray
1
Electronic polarizability
Atomic/ionic polarizability
a
Electronic absorption
Atomic/ionic absorption

## Slide 12: Chromatic dispersion of glasses
Abbe number (V-number):
  D, F and C spectral lines: 589.3 nm, 486.1 nm and 656.3 nm
l
n
Visible
Static
UV
X-ray
1
Normal dispersion
IR
Anormalous dispersion
D
F
C
Notes: Visually transparent glasses exhibit normal dispersion in the visible range
Large Abbe number means small dispersion

## Slide 13: Chromatic dispersion of glasses
Abbe number (V-number):
Crown glass (“K”)
Soda-lime silicates
Low index
Low dispersion
Flint glass (“F”)
Lead glasses
High index
High dispersion
Optical polymers
Notes: Note that n_d is different from n_D
‘Super ED’ or ‘FD’ glass made by Ohara in Japan with an Abbe Number of 94.94 − less expensive and easier to work with than CaF2 crystal with a very similar Abbe Number to calcium fluorite.

## Slide 14: Chromatic dispersion of glasses
Prism dispersive spectrometer
Chromatic aberration

## Slide 16: Dispersive concentrators for lateral solar spectrum splitting
Dispersive lens
Concentrating optics
Lateral cell arrays
Combining two materials (glass & polymer) with identical refractive index and different dispersion to split sunlight without bending optical axis
Opt. Lett. 44, 3274 (2019)

## Slide 17: Optical loss in silica glass
The Nobel Prize in Physics 2009
Charles Kuen Kao
Prize motivation:
"for groundbreaking achievements concerning the transmission of light in fibers for optical communication"

## Slide 18: Optical loss / attenuation mechanisms
Semiconductor optoelectronics | Soda-lime glass in the infrared | Transparent ceramics | Fiber-optic glasses
Electronic absorption Absorption induced by electronic transitions | Phonon absorption Absorption resulting from atomic / ionic vibrations | Defect scattering Scattering by crystalline grains, grain boundaries, micro-voids, etc. | Rayleigh scattering Scattering due to density, structure or composition fluctuations

## Slide 19: Optical loss mechanisms in glasses
Extrinsic absorption (impurities or dopants)
  Transition metal or rare earth ions
  Vibrational absorption
Intrinsic attenuation
  Band-to-band transitions
  Urbach tail absorption
  Mid-gap defect state absorption
  Free carrier absorption (FCA)
  Phonon (vibrational) absorption
  Rayleigh scattering
    Density fluctuation
    Structural moieties
Color codes:
Atomic/ionic absorption
Electronic absorption
Scattering

## Slide 20: Electronic absorption in amorphous solids
E
DOS
Conduction band
Valence band
Mobility edge
Mid-gap states
Urbach tail
  1
  2
  3
  4
Band-to-band transition
Urbach bandtail absorption
Defect state absorption
Free carrier absorption

## Slide 21: Electronic absorption in amorphous solids
E
DOS
  1
  2
  3
  4
ET : Tauc gap
ET = 2.1 eV
Band-to-band transition
Band-to-band transition
A. Stern, Photodiodes – World Activities in, 267 (2011).

## Slide 22: Electronic absorption in amorphous solids
E
DOS
  1
  2
  3
  4
A. Stern, Photodiodes – World Activities in, 267 (2011).
Band-to-band transition
Urbach bandtail absorption
Urbach tail absorption

## Slide 23: Electronic absorption in amorphous solids
E
DOS
  1
  2
  3
  4
L. Ley, The Physics of Hydrogenated Amorphous Silicon, 141 (1984).
Band-to-band transition
Urbach bandtail absorption
A: band-to-band
B: Urbach tail
C: Dangling bonds

## Slide 24: Electronic absorption in amorphous solids
E
DOS
  1
  2
  3
  4
Band-to-band transition
Urbach bandtail absorption
Defect state absorption
L. Ley, The Physics of Hydrogenated Amorphous Silicon, 141 (1984).
A: band-to-band
B: Urbach tail
C: Dangling bonds

## Slide 25: Electronic absorption in amorphous solids
E
DOS
  1
  2
  3
  4
Band-to-band transition
Urbach bandtail absorption
Defect state absorption
Free carrier absorption
Drude model:
Theory behind the generalized Drude (Plasma) model

## Slide 26: Electronic absorption in amorphous solids
E
DOS
  1
  2
  3
  4
Band-to-band transition
Urbach bandtail absorption
Defect state absorption
Free carrier absorption
Low mobility small FCA

## Slide 27: Electronic absorption in amorphous solids
E
DOS
  1
  2
  3
  4
Band-to-band transition
Urbach bandtail absorption
Defect state absorption
Free carrier absorption
Absorption coefficient (cm-1)
Band-to-band: > 103
Bandtail and defect states: 1 – 103
FCA: generally weak in amorphous solids

## Slide 28: Vibrational absorption
Atomic spacing
Energy
Harmonic oscillator
Compound or functional group | Primary absorption bands (mm)
O-H | 2.92
S-H | 4.01, 3.65, 3.11, 2.05
P-H | 4.35
Ge-H | 4.95
As-H | 5.02
Si-O | 9.1 – 9.6
Ge-O | 12.8
H2O | 6.3, 2.8
J. Optoelectron. Adv. Mater. 3, 341 (2001)
m
m
k
Atom
Atom
Bond

## Slide 29: Infrared windows of common optical materials
Black diamond (BD-2): Ge28Sb12Se60
Single-crystal germanium lens

## Slide 30: Sources of Rayleigh scattering in glass
Local density fluctuation
  p : photoelastic constant
  b : isothermal compressibility
Concentration scattering
  Local composition fluctuation in multi-component glasses
  Einstein-Smoluchowski scattering: density fluctuation of atmosphere
Ann. Physik 33, 1275 (1910);
Ann. Physik 25, 205 (1908);
J. Appl. Phys. 55, 4052 (1984).

## Slide 31: Intrinsic optical loss spectrum in glass
log(a)
log(l)
Total loss:
Phonon absorption limited
Rayleigh scattering limited
Minimum loss window

## Slide 32: Total optical loss in glasses
SiO2
BaF2-GdF4-ZrF4
CaF2-BaF2-YF3-AlF4
GeS3
Electron. Lett. 17, 775 (1981)
SiO2
Concentration scattering is not taken into account, resulting in unrealistically low loss values

## Slide 33
Photo taken at the
Corning Glass Science and Engineering Laboratory, Rutgers University

## Slide 34: Transparent glass coloring: absorption
Transition metal or rare earth ion additives
Er3+ energy levels
Modern Aspects of Rare Earths and Their Complexes (2003)
Notes: Erbium(III) with f11 configuration has 17 multiplet terms with 41 levels due to spin-orbit coupling.

## Slide 35: Transparent glass coloring: absorption
Transition metal or rare earth ion additives
Absorption spectra of Er3+ in different glasses
J. Lightwave Technol. 9, 234 (1991)

## Slide 36: Transparent glass coloring: absorption
Transition metal or rare earth ion additives
Green tint due to Fe2+ ions
Glass decolorization:

## Slide 37: Examples of color glasses with ion additives
Cobalt blue
Chromium green
Room light
UV illumination
Uranium glass (Vaseline glass)
Manganese amethyst

## Slide 38: Transparent glass coloring: scattering
Precipitation of small crystals or metal nanoparticles
  Rayleigh scattering by nanocrystals
  Plasmon resonance of metal nanoparticles
Opalescent glass: nanocrystals
Lycurgus Cup: Au-Ag nanoparticles
Notes: Cryolite glass image source: https://www.itp.uni-hannover.de/~zawischa/ITP/scattering.html

## Slide 39: Striking colors
Coloring of glass via heat treatment
Example: gold-ruby striking
Annealing at 500 – 700 °C
Melt at 1400 °C and quench
Nature 407, 691 (2000)
Au+
O2-
Au+
Unfired
Fired
Au nanoparticles (dia. 5 – 60 nm)
Notes: Blue/green colors in glasses (ions) are usually more stable than red/gold colors (NPs)

## Slide 40: Photochromic and electrochromic glasses
Optical or electrical control of redox state of ions
© Gentex Corp
Notes: By using viologens and phenlyenediamine as the electrochromic molecules and redox agent, Gentex Corporation has commercialized this type of device for auto-dimming rearview mirrors and smart windows in Boeing 787 aircraft.

## Slide 41: Photochromic and electrochromic glasses
Optical or electrical control of redox state of ions
Carrier injection into transparent conductors to modulate FCA
Bleached transparent
Colored brown-gray
Nature 500, 323 (2013)

## Slide 42: Photochromic and electrochromic glasses
Optical or electrical control of redox state of ions
Carrier injection into transparent conductors to modulate FCA
Nature 500, 323 (2013)

## Slide 43: Summary
Refraction
  Microscopic origin of refraction and chromatic dispersion
  Composition dependence of refractive indices
  Abbe number
Attenuation
  Optical loss mechanisms in general materials
  Optical loss mechanisms in glasses
  Electronic, vibrational, and scattering losses
Coloring
  Ion additives
  Scattering by nanoparticles