## Slide 1: MIT 3.071 Amorphous Materials 14: Optical Fibers and Waveguides
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2
The masters of light
“If we were to unravel all of the glass fibers that wind around the globe, we would get a single thread over one billion kilometers long – which is enough to encircle the globe more than 25,000 times – and is increasing by thousands of kilometers every hour.”
2009 Nobel Prize in Physics
Press Release

## Slide 3: Light confinement via total internal reflection
nhigh
nlow
nlow
Light
q
Condition for TIR:
Core
Cladding
Snell is right
by Ulrich Lohmann
PMMA
Air

## Slide 4: Waveguide cross-section geometries
Slab waveguide
Channel/photonic wire
waveguide
nhigh
nlow
nlow
nhigh
nlow
Rib/ridge waveguide
nhigh
nlow
nlow
1-d optical confinement
2-d optical confinement
cladding
cladding
core
core
cladding
Step-index fiber
Graded-index (GRIN) fiber
core
cladding

## Slide 5: Single-mode vs. multi-mode light guiding

## Slide 6: Optical fiber materials
Glasses: silica and other oxides, chalcogenides, halides, polymers
Metals, crystalline oxides and semiconductors, etc.
Dopants in silica glass
  Increase index: GeO2, P2O5, TiO2
  Decrease index: B2O3
  Luminescent centers: rare earth (e.g. Er)
Refractive index nD of SiO2-GeO2 glass
Appl. Opt. 24, 4486 (2004)

## Slide 7: Standard single-mode silica optical fiber structure
Core/cladding: low loss light propagation
Buffer/jacket: protection against mechanical damage and the environment (UV radiation, humidity, etc.)
Core
Cladding

## Slide 8: Fiber drawing process
Fiber preforms
Drawing tower
Fiber spool
Viscosity window for fiber drawing:
104 to 106 Pa·s
Notes: https://www.technologyreview.com/s/401266/drawing-optical-fibers/

## Slide 9: Glass properties impact fiber processing
Glass forming ability
  Processing window
Liquid fragility
  Fragility parameter
  Temperature sensitivity

## Slide 10: Fiber drawing: diameter control
F
Neck-down region
Preform
Drawing tension:
Fiber diameter is determined by the drawing speed
Fiber diameter is feedback loop controlled in real time during drawing
Candy fiber drawing
A
IEEE Photon. J. 2, 620 (2010)
J. Appl. Phys. 49, 4417 (1978)

## Slide 11: Standard silica fiber preform fabrication
Modified chemical vapor deposition (MCVD)
  SiCl4 + O2 → SiO2 (soot) + Cl2
  GeCl4 + O2 → GeO2 + Cl2
Layer composition and thickness controlled in each torch sweep
Traversing torch
Rotating silica tube
Reactant gases
Soot
High temperature reaction zone
MCVD lathe, University of Southampton
Water-free reaction: minimal -OH contamination
Notes: Silicon tetrachloride has a boiling point (57.7 C) convenient for purification by repeated fractional distillation

## Slide 12: Optical fiber manufacturing and testing

## Slide 13: Multi-material, microstructured optical fibers
Microstructured optical fibers: photonic bandgaps and various sizes of the rings give rise to the different colors
A. Argyros, the University of Sydney
Optical mode shaping
Dispersion engineering
Broadband transmission
Multi-functional sensing
Nat. Mater. 6, 336, (2007)

## Slide 14: Multi-material, microstructured optical fibers
Hollow-core photonic crystal fiber fabrication process flow using the stack-and-draw technique
Optical mode shaping
Dispersion engineering
Broadband transmission
Multi-functional sensing
Nat. Mater. 6, 336, (2007)
Nanophotonics 2, 315-340 (2013)
Notes: (A) Primary preform obtained by assembling a few hundred high purity, low-hydroxyl silica glass capillaries into an array with the required geometry tightly packed inside a glass tube; (B) first stage draw of the primary preform into a ~millimetre sized “cane”; (C) optical image of the cross-section of a HC-PBGF cane showing elimination of interstitial volumes and formation of the central core “defect”; (D) scanning electron microscope image of the microstructured region of the final fibre, showing a much increased diameter to pitch ratio of the cladding holes. The typical hole-to-hole spacing for operation at 1500 nm wavelength is in the range of 4–6 µm (depending on the air filling ratio of the cladding).

## Slide 15: Multi-material, microstructured optical fibers
Rod-in-tube
Extrusion
Stack-and-draw
Adv. Mater. 18, 845 (2006)
Int. J. Appl. Glass Sci. 3, 349 (2012)

## Slide 16: Multi-material, microstructured optical fibers
Adv. Mater. 18, 845 (2006)
Thermal sensing fibers

## Slide 17: Multi-material, microstructured optical fibers
Nat. Biotechnol. 33, 277 (2015)
Multifunctional (optical, electrical and chemical) neural probes

## Slide 18: “Exponential growth is the most powerful force in the universe.”
© TSMC
A 5 MB hard disk (1956)

## Slide 19
Benchtop optical systems based on discrete components

## Slide 20: Photonic integrated circuits (PICs)
Photonic integration enables rugged and low-cost miniature optical systems

## Slide 21: Value proposition for integrated photonics
Cost & scalability
Deployment flexibility
Power savings

## Slide 22
Laser cavity
Optical switch
Photodetector
Waveguide
Waveguide
All optical components integrated on a glass substrate

## Slide 23: State-of-the-art integrated photonics
Optical fiber interface
Photonic chip
IMEC photonic chip & Tyndall fiber array packaging
Substrate
Cladding
Core
Light
Integrated planar waveguide
Substrate platforms: Si, III-V semiconductors, glass, LiNbO3, polymer
Core material: c-Si, III-V, a-Si, SiO2, SiN, ion exchange glass, polymer

## Slide 24: Optical loss in fibers and waveguides
Material attenuation
Surface roughness scattering
  Optical fiber
    Frozen surface capillary waves due to energy equipartition
    Usually small in optical fibers
  Planar waveguide
    Surface roughness resulting from imperfect patterning
    Often the main source of loss
s : RMS roughness
J. Lightwave Technol. 23, 2719 (2005)

## Slide 25: Planar waveguide fabrication: lithography
Substrate
Cladding layer
Core layer
Amorphous waveguide material: ease of deposition, low optical loss
Planar waveguide platform: massively parallel low-cost fabrication, geometry/material diversity, interfacing with other on-chip components

## Slide 26: Planar waveguide fabrication: ion exchange
Scalable, simple lithographic processing
Low optical loss
Potential for adjustments with post-annealing

## Slide 27: Planar waveguide fabrication: nanoimprint
As2S3 waveguide patterned using direct nanoimprint
Opt. Express 18, 19286 (2010)

## Slide 28: Planar waveguide fabrication: laser writing
© Laser Focus World
Laser Direct Writing (LDW)
Glass

## Slide 29: Beyond waveguide fabrication: LDW for data storage

## Slide 30
Applications of integrated optics and photonics
Communications
LIDAR
Augmented reality
Sensing

## Slide 31: Optical communication system
0 = peace
1 = invasion

## Slide 32: Optical communication system
Optical receiver (Rx) / transceiver
Transmitter driver circuit
Optical transmitter (Tx) / transceiver
Electronic digital signal
1
0
1
0
1
1
0
1
0
1
Optical digital signal
Receiver circuit
Electronic digital signal
1
0
1
0
1
Optical fiber / waveguide
Opt. Express 19, B777 (2011)
Fiber ribbon

## Slide 33
 | 2004 |  |  | 2010+ | 
Enterprise Distance: 0.1-10km
Rack-Rack Distance: 1-100m
Board-Board Distance: 50-100cm
Chip-Chip Distance: 1-50cm
OPTICAL
Electrical to optical interconnect
ELECTRICAL
3.125G 10G 40G
3.125G 5-6G 10G 20G
3.125G 5-6G 10G 15-20G
10G >= 40G
Copper Tech
Transition Zone
Integrated
photonics?
Optical Tech

## Slide 34: Wavelength division multiplexing (WDM)
Single optical fiber
Optical channel
World’s first petabit (1015) per second data transmission using a single-core fiber (2020):
382 wavelengths × 15 modes

## Slide 35
See what the “FiOS boy” says about WDM!

## Slide 36: Inside Google’s data center

## Slide 37: Active optical cable (AOC)

## Slide 38: Photonics for AI
AI is communication-intensive
Optics enables high-bandwidth, low-latency, and power-efficiency interconnects
© Effect Photonics

## Slide 39: Co-Packaged Optics (CPO)
Image courtesy of ASE

## Slide 40: Co-Packaged Optics for AI computing

## Slide 41: Augmented reality (AR)

## Slide 42: Augmented reality: how it works
© roadtovr.com

## Slide 43: High refractive index glass for AR

## Slide 44: High refractive index glass for AR
SCHOTT RealView® Datasheet

## Slide 45: High refractive index glass for AR
Flint glass with high-index metal oxides (PbO, ZrO2, TiO2, etc.)

## Slide 46: Summary
Device fabrication
Fiber drawing
  Preform fabrication: MCVD process
  Drawing parameter control: fiber diameter & draw tension
  Multi-material fiber and microstructured fiber processing
Planar waveguide fabrication
Optical loss in fibers and waveguides
Material attenuation
Surface roughness scattering
Applications of integrated photonics
Digital communication systems & augmented reality