## Slide 1: MIT 3.071 Amorphous Materials 2: Classes of Amorphous Materials
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 1 & 5
Introduction to Glass Science and Technology
  Ch. 5

## Slide 3: Network formers, modifiers and intermediates
Glass network formers
  Form the interconnected backbone glass network
Glass network modifiers
  Present as ions to alter the glass network
  Compensated by non-bridging oxygen (NBO) in oxide glasses
  Usually reduce glass network connectivity
Intermediates
  Can function as network formers or modifiers depending on glass composition

## Slide 4: Network formers, modifiers and intermediates
Si
O
O
O
O
Si
O
O
O
Na2O
Si
O
O- Na+
O
O
Si
O
O
O
Na+ O-
Silicon:
glass former
Sodium:
network modifier
Bridging oxygen
Non-bridging oxygen
+
→

## Slide 5
Glass formers
Network modifiers
Intermediates
Glass former: high valence state, covalent bonding with O
Modifier: low valence state, ionic bonding with O

## Slide 6: Silica glass (SiO2)
A 3-D glass network predominantly consisting of corner-sharing SiO4 tetrahedra interconnected by bridging oxygen (BO)
High network connectivity: high softening point, low diffusion coefficient, small coefficient of thermal expansion (CTE)
Cristobalite

## Slide 7: Volume anomaly in silica glass

## Slide 8: Alkali silicate glass
Each alkali ion creates one non-bridging oxygen
Reduced network connectivity: viscosity decreases (compared to silica at the same T), diffusion coefficient and CTE increases
Increased ionic conductivity, reduced chemical resistance
Increasing alkali concentration
Invert glass
Notes: How to Prevent Glass Corrosion: http://www.vitroglazings.com/VitroGlazings/media/sitedocuments/TDs/19_TD105F.pdf
H2O + SiONa -> SiOH + NaOH, and the resulting basic solution further expedites glass corrosion
Fire polish process to enhance surface chemical durability of alkali silicate glass
Reduced softening temperature means that these glasses can be recycled

## Slide 9: Structural determination in alkali silicate glass
Y : the average number of corners shared per SiO4 tetrahedron
In a glass with molar composition: x Na2O · (1-x) SiO2
  Number of NBO per mole: 2x
  Number of BO per mole: 2-3x
  Number of corners shared per mole: (2-3x) × 2 = 4-6x
  Number of tetrahedra per mole: 1-x
  Y = (4-6x) / (1-x)
  Onset of inverted glass structure: Y = 2, x = 0.5
Viscosity isotherms
Y
log10(viscosity)
Y = 2

## Slide 10: Alkali-alkaline earth-silicate glass
Each alkaline earth ion creates two NBOs
Increased network connectivity compared to alkali silicates: stabilized glass network, improved chemical resistance
Approximate composition of commercial soda-lime glass (window glass):
  16Na2O·10CaO·74SiO2
CaO
Si
O
Si
Si
Si
O- Ca2+ O-
+
→

## Slide 11: Borate glass
B2O3: the glass former consisting of corner-sharing BO3 triangles connected by bridge oxygen
B2O3 crystal
B
O
O
B
O
B
Boroxol rings: basic structural unit in boric oxide glass

## Slide 12: Borate glass
B2O3: the glass former consisting of corner-sharing BO3 triangles connected by bridge oxygen
Alkali borate glass:
B
O
O
O
+
→
1/2 Na2O
B
O- Na+
O
O
B
O
O
O
+
→
1/2 Na2O
B-
O
O
O
O
Na+
NBO formation
B3 → B4 conversion

## Slide 13: The Boron anomaly
Fraction of 4-fold coordinated boron
Molar fraction of alkali (%)
NBO formation
B3 → B4 conversion
Initial addition of alkali ions increases network connectivity, reduces CTE and enhances thermal & chemical resistance

## Slide 14: Various properties of lithium borate glass
J. Non-Cryst. Sol. 351, 1103-1112 (2005)
More than two structural transformations contribute to the boron anomaly
Further reading:
Shelby Ch. 5

## Slide 15: (Alkali) borosilicate glass
Borosilicate glass: x M2O · y B2O3 · (1 - x - y) SiO2
  SiO2 and B2O3 : glass formers
  Alkali ions (M+) converts B3 to B4 states (when x / y < 0.5)
  Each additional alkali ion creates one NBO (when x / y > 0.5)
The original Pyrex™ recipe: 4Na2O·13B2O3·2Al2O3·81SiO2
200-inch Hale telescope mirror
Space shuttle tile coating
Notes: Cooling of the Hale telescope mirror took 1 year
The borosilicate glass coating for space shuttle tile contains carbon and that is why it appears black. See for example patent US 4093771.

## Slide 16: (Alkali) aluminosilicate glass
Aluminosilicate glass: x M2O · y Al2O3 · (1 - x - y) SiO2
  SiO2 : glass former
  Al functions as a glass former in the form of AlO4 groups (when x > y)
  Each excess Al atom creates three NBOs (when x < y)
Al3+ in an oxygen octahedron
Activation energy for DC conductivity
y / x
y = x
Notes: The increase in the activation energy at initial additions of alumina is attributed to the tightening of the structure due to the gradual disappearance of NBO. With further additions of alumina, the activation energy starts decreasing because of the looseness of bonding between the alkali ion and the [AlO4] group. When [Al2O3/M2O] > 1, the activation energy starts increasing again because of the blocking effect of the octahedrally coordinated Al+ ion in the interstices.

## Slide 17: Chalcogenide glass (ChG)
ACerS Bull. 94, 24-29 (2015)
Reduced mechanical strength
Low softening temperature
Low phonon energy (infrared transparency)
Enhanced optical (Kerr) nonlinearity

## Slide 18: Amorphous semiconductors
Tetrahedral “glasses”
  a-Si, a-Ge, a-Si:H (hydrogenated amorphous silicon)
Vapor deposition: plasma enhanced chemical vapor deposition (PECVD), sputtering, electron beam evaporation
Dangling bonds

## Slide 19: Metallic glass (amorphous metal, glassy metal)
Inoue’s empirical rules for bulk metallic glass (BMG) formation
  Multicomponent systems consisting of three or more elements
  Significant difference in atomic size ratios (frustration)
  Negative enthalpy of mixing
Polycrystalline metal
Amorphous metal
Grain boundaries

## Slide 20: Other glass groups and glass formers
Phosphate glass: P2O5
Heavy metal oxide (HMO) and transition metal oxide glass
  TeO2, PbO, Bi2O3, V2O5, TiO2, etc.
Halide glass and alloys
  e.g. ZBLAN: ZrF4-BaF2-LaF3-AlF3-NaF
  Chalcohalide, oxyhalide, etc.
Amorphous minerals
  Opal, biominerals
and many others…
Amorphous calcium carbonate in lobster carapace
“The Formula for Lobster Shell,” Max Planck Research

## Slide 21: Representation of glass composition
In oxide glasses, the convention is to list the glass network modifiers in increasing valence order ending with glass network formers
  Example: K2O·CaO·5SiO2
  In mole fraction: 14.3K2O·14.3CaO·71.5SiO2
  By weight: 20.9K2O·12.4CaO·66.7SiO2 (wt%)
In metallic glasses, the listing is usually done in decreasing order of content
  Example: Zr41.2Be22.5Ti13.8Cu12.5Ni10.0 (Vitreloy-1)
Notes: There are always exceptions to the conventions

## Slide 22: Summary
Glass formers, network modifiers, and intermediates
Silicate glass chemistry
  Corner-sharing tetrahedra
  Bridging and non-bridging oxygens
  Different modifiers: alkali, alkali earth
Borates and boron anomaly
Impact of network connectivity on glass properties
Other glass/amorphous systems
  Chalcogenides: weak bonds
  Group IV amorphous semiconductors: passivation of dangling bonds
  Amorphous metals: lacking grain boundaries

## Slide 23: Summary of oxide glass chemistry
 | SiO2 (silicate) | B2O3 (borate)
No modifier | Structural unit: SiO4 No NBOs, low or negative CTE, high softening point, low diffusivity | Structural unit: BO3 No NBOs, corrugated layered structure
Alkali oxide | Each ion creates 1 NBO; large CTE, low softening point, poor chemical durability, ionic conductivity | Each ion creates 1 B4 group or 1 NBO; extremum in glass properties (boron anomaly)
Alkaline earth oxide | Each ion creates 2 NBOs; similar effects as alkali ions although some network connectivity is preserved | Each ion creates 2 B4 groups or 2 NBOs; extremum in glass properties (boron anomaly)
Alumina (Al2O3) | Each ion creates 3 NBOs; in the presence of alkali ions Al3 → Al4 conversion occurs | B2O3 and Al2O3 both serve as glass formers; glass is stable only with high B2O3 content