## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 10: Optoelectronic Properties
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Optoelectronics
Optoelectronics is the study and application of electronic devices and systems that source, detect and control light
Optoelectronics is based on the quantum mechanical effects of light on electronic materials, especially semiconductors
References
Fundamentals of Photonics, Ch. 15
Physics of Semiconductor Devices, Ch. 1
Semiconductor Opto-Electronics, Ch. 3 & 7

## Slide 3: Optical absorption in semiconductors

## Slide 4: Band structure of semiconductors near band edge
k
E
k
E
Direct gap semiconductors:
compound semiconductors
Indirect gap semiconductors:
group IV semiconductors
Eg
Eg

## Slide 5: Band structure of silicon
G :
L :
X :
a = 5.43 Å

## Slide 6: Energy and crystal momentum conservation
Energy conservation
Crystal momentum conservation
Thermalised electron momentum
Photon momentum
k
E

## Slide 7: Energy and crystal momentum conservation
Parabolic band approximation
Energy conservation
Reduced mass:
k
E
EC0
EV0

## Slide 8: Energy and crystal momentum conservation
Energy conservation
For a given photon energy, only a narrow band of states contribute to absorption!
k
E
EC0
EV0

## Slide 9: Electronic density of states in energy bands
In the k-space each electronic state occupies a volume of
where V is the volume of the system
Dispersion relation
Beware of spin degeneracy!

## Slide 10: Absorption in direct gap semiconductors
Photon absorption rate is proportional to the joint density of states: the density of states (pairs) that can participate in the absorption process
Optical transition typically does not flip the electron spin state

## Slide 11: Direct band gap energy determination
V. Mudavakkat et al., Opt. Mater. 34, Issue 5, 893-900 (2012).

## Slide 12: Absorption in indirect gap semiconductors
Conservation laws
k
E
Typical optical phonon energy in Si: 60 meV
AIP Adv. 1, 041403 (2011)

## Slide 13: Absorption in indirect gap semiconductors
Phonon-assisted absorption:

## Slide 14: Indirect band gap energy determination
Appl. Opt. 27, 3777-3779 (1988).
Si
Nanotechnology 23, 075601 (2012).

## Slide 15: Moss-Burstein effect
k
E
k
E
Doping
Increase of apparent bandgap energy in degenerately doped semiconductors
Inhibition of transition due to the Pauli's exclusion principle

## Slide 16: Pauli blocking
Graphene-Enhanced Optical Signal Processing, DOI: 10.5772/67491
Carrier doping via electrostatic gating
Inhibition of transition due to the Pauli's exclusion principle

## Slide 17: A graphene-based waveguide modulator
Nature 474, 64 (2011)

## Slide 18: Quasi-Fermi levels in non-equilibrium semiconductors
Optical or electrical injection increases the density of both types of carriers
In semiconductors displaced from equilibrium, separate quasi-Fermi levels, EFn and EFp must be used for electrons and holes, respectively (EFn = EFp in equilibrium)
Quasi-thermal equilibrium within bands: electron relaxation time within a band is much smaller than across the band gap
Occupation probability in the conduction band:
Occupation probability in the valence band:

## Slide 19: Absorption saturation effect
At high injection levels, the available empty states for electrons in the conduction band are depleted
Equilibrium
High injection level
k
E
k
E
Pumping

## Slide 20: Absorption saturation effect
Absorption coefficient in the presence of saturation:
Equilibrium
High injection level
k
E
k
E
Pumping
Here EC and EV are the energies of the initial and end states

## Slide 21: Amorphous solids
Short range order (SRO)
Lack of long range order (LRO)
Properties pertaining to SRO
  Energy band formation
  Density of states
Properties pertaining to lack of LRO
  Crystal momentum (not a good quantum number anymore!)
  Localized states (Anderson localization)
Unlike gases, amorphous solids are NOT completely random
Amorphous
Random
vs.

## Slide 22: Anderson localization in disordered systems
Localization criterion: sufficiently large variations
P. W. Anderson
Disorder leads to (electron, photon, etc.) wave function localization

## Slide 23: Anderson localization in disordered systems
Extended states (Bloch states)
Localized states

## Slide 24: Density of states (DOS) in crystalline and amorphous solids
E
DOS
Conduction band
Valence band
Band gap
E
DOS
Conduction band
Valence band
Crystalline solids
Mobility edge
Mid-gap states
Urbach tail
Amorphous solids
Defect states

## Slide 25: Tauc gap and Tauc plots
Tauc gap ET definition:
It is merely a fitting parameter and has little physical significance!
ET = 3.3 eV

## Slide 26: Stimulated and spontaneous emission
Stimulated emission
Spontaneous emission

## Slide 27: Stimulated emission
The reverse process of optical absorption
Electron-hole recombination to emit a photon in the presence of an external electromagnetic field excitation
Energy conservation
Optical gain
k
E
where w is the angular frequency of the external field as well as the emitted photon

## Slide 28: Net gain and optical amplification
Net gain = gain – loss
In practical applications, additional loss sources (scattering, FCA, etc.) need to be considered in the loss term as well
Population inversion
L. A. Coldren and S. W. Corzine, Diode Lasers and Photonic Integrated Circuits

## Slide 29: Single-mode rate equation
Consider a semiconductor with uniform carrier density
n : carrier density np : photon number
kabs , kstim , ksp : absorption, stimulated and spontaneous emission coefficients, which are environment-independent
Absorption rate
Stimulated emission rate
Spontaneous emission rate
No carrier injection

## Slide 30: Single-mode blackbody radiator
In thermal equilibrium
Energy conservation:
Hot blackbody ( ):
Cold blackbody ( ):
Fermi-Dirac distribution
Planck distribution

## Slide 31: Single-mode “hot” blackbody radiator
In thermal equilibrium
Thermal equilibrium
Absorption and stimulated emission dominate over spontaneous emission in a “hot” blackbody
At high temperatures, occupation probability of all states are equal

## Slide 32: Single-mode “cool” blackbody radiator
In thermal equilibrium
All the rate constants are the same specified by detailed balance
Note: the rate constant ka-e is NOT a material constant as it depends on the optical mode under investigation
Rereading Einstein on Radiation

## Slide 33: Optical gain in semiconductors
The absorption curve at zero injection level and the gain curve at complete inversion are symmetric with respect to the horizontal axis
Their shape reflects the joint DOS in the material

## Slide 34: Optical amplification
Under steady-state carrier injection:
Optical amplification:
Gain medium
Net radiative recombination
Non-radiative recombination
Current injection
Optical injection

## Slide 35: Carrier density in semiconductor devices
Solving the current continuity and the Poisson equations
Current continuity
Poisson equation
0 V bias
0.5 V forward bias
1-D semiconductor device simulator:
SimWindows download

## Slide 36: Stimulated emission and spontaneous emission in technical applications
Stimulated emission
Spontaneous emission
Optical amplifiers
Lasers
LEDs
Fluorescence imaging
Photoluminescence spectroscopy

## Slide 37: Engineering spontaneous emission rate: Purcell effect
Fermi’s golden rule:
No photon states: suppressed spontaneous emission (SE)
  Photonic band gap
Large photon density of states: enhanced (i.e. faster) SE rate
  Optical resonant cavity
Enhancement factor (Purcell factor) of SE in a cavity:
Initial state yi
electron in CB + 0 photon
Final state yf
electron in VB + 1 photon
n : refractive index Q: cavity Q-factor*
l : wavelength V: cavity mode volume
Notes: In defining Purcell factor, the Q is given as min(Q_cavity, Q_emitter linewidth)

## Slide 38: Engineering spontaneous emission rate: Purcell effect
SE suppression
SE enhancement
"Investigation of spontaneous emission from quantum dots embedded in two-dimensional photonic-crystal slab," Electron. Lett. 41, 1402-1403 (2005).

## Slide 39: List of symbols
E – energy
Eg – band gap energy
k / ke – electron wave vector
a – lattice constant
ћ – reduced Planck constant, 1.055 × 10-34 J·s
w – angular frequency of light
EC / EV – energy of a state in conduction / valence band
EC0 / EV0 – energy of conduction / valence band edge
kC / kV – wave vector of a state in conduction / valence band

## Slide 40: List of symbols
me* – electron effective mass
b – photon wave vector
kB – Boltzmann constant, 1.38 × 10-23 m2·kg·s-2·K-1
T – thermodynamic temperature
c – speed of light in vacuum, 2.99792458 × 108 m/s
mr – reduced mass
r – electronic density of state
V – volume
rC – density of state of conduction band
rj – joint density of state

## Slide 41: List of symbols
a – absorption coefficient
wq / kq – angular frequency / wave vector of phonon
ET – Tauc gap
EF – Fermi energy
EFn / EFp – quasi-Fermi level for conduction / valence band
fC / fV – occupation probability in conduction / valence band
s – gain coefficient
g – net gain coefficient

## Slide 42: List of symbols
n / p – electron / hole density
t – time
Rabs / Rstim / Rsp – absorption / stimulated emission / spontaneous emission rate
kabs / kstim / ksp – absorption / stimulated emission / spontaneous emission coefficient
np – photon density
ka-e – absorption-emission coefficient
G – optical injection rate of electronic carriers
Jn – electronic current density

## Slide 43: List of symbols
G – waveguide modal confinement factor
D – electric displacement
rf – free charge density
E – electric field
e – (absolute) permittivity
F – electric potential
NA / ND – acceptor / donor concentration
e – elementary charge, 1.602 × 10-19 C
Gi-f – transition probability per unit of time
H – Hamiltonian of perturbation

## Slide 44: List of symbols
Ei / Ef – energy of initial / final state
yi / yf – wave function of initial / final state
FP – Purcell enhancement factor
Q – quality factor
l – free-space wavelength