## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 2: Electromagnetic Wave Theory
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: References
Fundamentals of Photonics, Ch. 2 and 5
Photonics: Optical Electronics in Modern Communications, Ch. 1
Principles of Nano-optics, Ch. 2

## Slide 3: Maxwell Equations (‘macroscopic’ differential form)
Gauss’s Law:
Gauss’s Law for magnetism:
Faraday’s Law:
Ampere’s Law:
James C. Maxwell (1831-1879)
H | Magnetic field | B | Magnetic induction
E | Electric field | D | Electric displacement
Jf | Free current density | rf | Free charge density

## Slide 4: Charge conservation
Ampere’s Law:
Gauss’s Law:
Vector identity:
Charge conservation:
Free electric current flowing through any enclosed surface S is equal to the change rate of free charge within the surface

## Slide 5: Constitutive relations
General form for non-bianisotropic media:
Linear (low light intensity), isotropic media
  Non-ferroelectric & non-ferromagnetic crystals with a cubic lattice (rock salt, silicon, gold, etc.)
  Amorphous glasses and polymers
  E and D (or B and H) always align in the same direction
  In most non-magnetic materials, mr is very close to 1 (m = m0)
Non-magnetic media
Notes: See J. A. Kong’s book for a complete discussion about bianisotropic media

## Slide 6: Constitutive relations (cont’d)
Linear, electrically or magnetically anisotropic media:
  Non-cubic crystals
  Poled glasses and polymers
P | Polarization | M | Magnetization
e0 | Vacuum permittivity = 8.85 × 10-12 F/m | m0 | Vacuum permeability = 1.26 × 10-6 N/A2
e | Permittivity | m | Permeability
c | Electric susceptibility | cm | Magnetic susceptibility
Principal system
Notes: See J. A. Kong’s book for a complete discussion about bianisotropic media

## Slide 7: Transparent polycrystalline ceramics
Typical opacity of polycrystalline materials: scattering
Sources of scattering
  Grains with different orientations
  Inter-grain secondary phases
LumiceraTM, Murata Inc.
Solution:
  Cubic lattice material (isotropic)
  Processing optimization to eliminate secondary phases
Advantages
  Superior mechanical strength
  High refractive index and damage threshold
Spinel structure (cubic)

## Slide 8: Wave equation in source-free, isotropic media
Source-free, isotropic media:
Vector identity
Wave equation (vectorial equation: 6 equations total)
Non-magnetic media

## Slide 9: Helmholtz equation for monochromatic waves
Wave equation:
Monochromatic wave: single angular frequency w
Helmholtz equation:
Complex amplitude
Define
wave velocity
wave number (a scalar)

## Slide 10: Monochromatic plane wave solution
Plane wave solution:
Amplitude (real):
Phase:
Wave vector :
  A measure of spatial period
0
2A
l
where

## Slide 11: Monochromatic plane wave solution (cont’d)
The surfaces of constant phase (wave front) are parallel planes perpendicular to the wave propagation direction
Phase:
0
2A
l
Example:
A set of parallel planes moving along the x-axis at the velocity of c
Wave front:
x
y
z

## Slide 12: Monochromatic plane wave solution (cont’d)
Plane wave solution in vacuum:
Plane wave in an isotropic, linear medium
n : refractive index
Non-magnetic media

## Slide 13: Complex refractive indices
Complete description of material optical properties
  nr : polarizability
  K : loss (dimensionless)
Absorption coefficient in cm-1
Attenuation

## Slide 14: Kramers-Kronig (K-K) relation
nr (refractive index) and K (absorption) are interdependent
Allows us to relate the real and imaginary parts of the susceptibility function:
  Formally symmetric with respect to real and imaginary parts
In non-magnetic media:
(dilute gas)

## Slide 15: Kramers-Kronig (K-K) relation (cont’d)
a(w)
1/(w2 - w02)
w0
K-K relation:
Negative contribution
Positive contribution
Normalized angular frequency

## Slide 16: Kramers-Kronig (K-K) relation (cont’d)
w / w0
a (w)
nr (w) -1
Refractive index data:
http://www.ioffe.ru/SVA/NSM/nk/index.html
http://www.luxpop.com/

## Slide 17: Increasing nr via quantum coherence
High refractive index material is attractive for a number of applications, e.g. high NA immersion photolithography
Is refractive index enhancement always accompanied by absorption increase?
Theoretical proposal: M. Scully, “Enhancement of index of refraction via quantum coherence,” Phys. Rev. Lett. 67, 1855 (1991).
Experimental realization: N. Proite et al., “Refractive Index Enhancement with Vanishing Absorption in an Atomic Vapor” Phys. Rev. Lett. 101, 147401 (2008).
(K)
(n)

## Slide 18: Transmission through dielectric interfaces
Boundary conditions of fields
  The conditions have to be satisfied everywhere and at all times on the boundary
Derivation of Snell’s law
  Phase matching: continuity of
  E-field across the boundaries
Snell’s law

## Slide 19: Fresnel equation at normal incidence
Continuity of E-field parallel to interface
E i + E r = E t
Boundary condition of B-field parallel to interface
Field induction
Fresnel equation: reflection coefficients
Half wave loss: n1 < n2
  p phase shift between incident
  and reflected wave
n1 = n2 : index matching, R = 0
Bi
Br
Bt
Ei
Er
Et
n1
n2
Boundary conditions

## Slide 20: Refractive index matching liquids
A Pyrex rod in water
In index matching oil
Quoted from “How to make glass disappear in a liquid”
Applications:
Reduce Fresnel losses in fiber optics
Refractometry: calibrate instruments
Strain analysis of transparent materials

## Slide 21: Index matching solution for live tissue imaging
Water solution index matched to live tissues reduces optical scattering
Enhancing solution index by adding dyes with absorption peaks in the UV
Science 385, 1061 (2024)

## Slide 22: Refractive index of gold
n ~ 0.37 @ 1 eV
Experimental value: R > 90%
Why is that ???
Imaginary part of index n (extinction coefficient) contributes to reflection as well!

## Slide 23: Linearly polarized wave optical reflection
TE (transverse electric, s-polarized) polarization
  Electric field parallel to substrate surface
TM (transverse magnetic, p-polarized) polarization
  Magnetic field parallel to substrate surface
TE or s-polarized
TM or p-polarized
Electric field
Electric field

## Slide 24: Linearly polarized wave optical reflection
TE (transverse electric, s-polarized) polarization
  Electric field parallel to substrate surface
TM (transverse magnetic, p-polarized) polarization
  Magnetic field parallel to substrate surface
low index
high index
high index
low index
TE
TM
TE
TM

## Slide 25: Transfer matrix method (TMM)
n1
n2
d1
d2
n3
d3
…
ni-1
di-1
ni
di
Incident light
Reflected light
Refracted light
?
?
Interface
1
2
4
3
Boundary conditions
E1
B1
E2
B2
E4
B4
B3
E3
TE polarization:
(i)
(t)

## Slide 26: Transfer matrix method (TMM)
n1
n2
d1
d2
n3
d3
…
ni-1
di-1
ni
di
Incident light
Reflected light
Refracted light
?
?
Interface matrix (TE):
Interface matrix (TM):

## Slide 27: Transfer matrix method (TMM)
n1
n2
d1
d2
n3
d3
…
ni-1
di-1
ni
di
Incident light
Reflected light
Refracted light
?
?
Layer
1
2
3
4
Propagation matrix
Phase delay
(i)

## Slide 28: Transfer matrix method (TMM)
n1
n2
d1
d2
n3
d3
…
ni-1
di-1
ni
di
Incident light
Reflected light
Refracted light
?
?
Transfer matrix
Transmittance:
Reflectance:

## Slide 29: Practical considerations in TMM applications
Anisotropic and magneto-optical media
  S. Teitler and B. Henvis, "Refraction in Stratified, Anisotropic Media," J. Opt. Soc. Am. 60, 830-834 (1970).
  H. Kato, T. Matsushita, A. Takayama, M. Egawa, K. Nishimura, and M. Inoue, "Theoretical analysis of optical and magneto-optical properties of one-dimensional magnetophotonic crystals," J. Appl. Phys. 93, 3906-3911 (2003).
Thick samples (compared to coherent length of light)
  C. Katsidis and D. Siapkas, "General Transfer-Matrix Method for Optical Multilayer Systems with Coherent, Partially Coherent, and Incoherent Interference," Appl. Opt. 41, 3978-3987 (2002).

## Slide 30: Anti-reflection coatings (ARCs)
Minimize reflection on surfaces
  Solar cells, detectors, lithography
Resist pattern w/o AR coating
Wavy patterns on pattern edge due to reflection/interference
Smooth pattern edge
when
Single ARC layer on Si designed for l = 550 nm
Quarter-wavelength layer

## Slide 31: Distributed Bragg Reflectors (DBRs)
Quarter-wavelength stack (1-D photonic crystal)
  Index sequence: H – L – H – L …
  High index contrast leads to large stop band (high reflectance band) bandwidth and increased reflectance
H
L
H
L
H
L
High-index substrate
Air
nH = 3.46
nL = 1.33
nH = 2.00
nL = 1.33

## Slide 32: DBRs for gravitational wave detection
LIGO @ MIT Museum
Advanced optical coatings for the discovery of gravitational waves

## Slide 33: Distributed Bragg Reflectors (DBRs)
In the frequency domain, the stop bands periodically appear at odd integral multiples of the 1st stop band center frequency
Why the stop band does not appear at even multiples?
First stop band center frequency: 1000 cm-1

## Slide 34: Poynting vector and energy flux
Energy flux of electromagnetic waves:
Time-averaged energy flux:
E
H
S, k

## Slide 35: List of symbols
D – electric displacement
rf – free charge density
B – magnetic induction
E – electric field
H – magnetic field
Jf – free current density
t – time
Qf – amount of free charge within an enclosed surface S
w – angular frequency
l – wavelength of light

## Slide 36: List of symbols
P – electric polarization (density)
M – magnetization or magnetic polarization (the same letter is also used to denote transfer matrix)
e0 – vacuum permittivity, 8.854 × 10−12 C/Vm
m0 – vacuum permeability, 1.26 × 10−6 H/m
e – (absolute) permittivity
m – permeability
c – electric susceptibility
cm – magnetic susceptibility
A – (real) wave amplitude

## Slide 37: List of symbols
c – wave velocity
k – wave number
– wave vector
– position vector
k0 – wave number in free space
c0 – speed of light in vacuum, 2.99792458 × 108 m/s
er – relative permittivity or dielectric constant
mr – relative permeability, ~ 1 for non-magnetic media
n – refractive index
nr – real part of refractive index

## Slide 38: List of symbols
K – imaginary part of refractive index or extinction coefficient
a – absorption coefficient
E┴ / B┴ – electric / magnetic field component perpendicular to an interface
E// / B// – electric / magnetic field component parallel to an interface
q – angle of incidence, reflection or refraction
kx / ky / kz – wave vector component along x / y / z axis
Ei / Er / Et – electric field of incident / reflected / transmitted wave

## Slide 39: List of symbols
Bi / Br / Bt – magnetic field of incident / reflected / transmitted wave
R – reflectance or intensity reflection coefficient
– Poynting vector