## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 7: Surface Plasmon Polaritons
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: References
Principles of Nano-optics, Ch. 12
Surface Plasmons on Smooth and Rough Surfaces and on Gratings
  H. Raether, Springer-Verlag
  Ch. 2

## Slide 3: Optical properties of metals
Properties of metals are largely determined by free electrons
Electrons populate states whose energy Ee < EF
Dielectrics
Metals

## Slide 4: Drude-Sommerfeld model for free electrons
Dynamic equation describing electron motion:
where
plasma frequency

## Slide 5: Drude-Sommerfeld model for free electrons
Noble metals: gold, silver
  High free electron density (~ 1023/cm3): large wp
  Low damping (large electron mobility): small g
In the visible-IR wavelength regime:
e.g. in gold:

## Slide 6: Complex refractive index of gold
In visible and NIR
Visible spectrum
http://www.ioffe.ru/SVA/NSM/nk/Metals/Gif/au.gif
Refractive index n
Absorption index K

## Slide 7: Complex refractive index of silver
Visible spectrum
http://www.ioffe.ru/SVA/NSM/nk/Metals/Gif/ag.gif
In visible and NIR
Refractive index n
Absorption index K

## Slide 8: Complex refractive index of aluminum
Visible spectrum
http://www.ioffe.ru/SVA/NSM/nk/AluminumCompounds/Gif/al.gif
In visible, Al is more lossy than Ag!
Refractive index n
Absorption index K

## Slide 9: Lorentz-Drude model for bound electrons
Interband transitions: bound electron oscillations
Dynamic equation describing electron motion:
Overall relative dielectric constant of metal:
contributions from both free and bound electrons
Notes: K-K relation holds for the Lorentz-Drude mode: https://web.pa.msu.edu/courses/2019fall/PHY842/LECTURE_NOTES/4-9.oct30.pdf

## Slide 10: Drude models applied to metal gold
Large negative real part
Small positive imaginary part: low optical loss
Free electrons
Bound electrons
Resonance absorption peaks at w = wb
Relatively minor contribution
Multiple interband transitions occur at short wavelengths (l < 500 nm for gold)
Images quoted from Principles of Nano-optics

## Slide 11: Lorentz-Drude model for dielectric materials
Wavelength/frequency dependent dielectric response
 | r (static, w = 0) | n ()
Ge | 16 | 4
Si | 11.7 | 3.5
LiNbO3 | 43 | 2.27
BaTiO3 | 3600 | 2.46
l
n
IR
Visible
Static
UV
X-ray
1
Electronic polarizability
Atomic polarizability

## Slide 12: Surface plasmon polariton (SPP) mode
SPP mode on planar metal-dielectric interfaces
  Field components: Ex, Ez, Hy
  Localized at the interface: field exponentially decays in both the metal and dielectric sides
Waveguide modes in dielectric slabs
  TM field components: Ex, Ez, Hy
  TE field components: Hx, Hz, Ey
  Localized at the high index core: field exponentially decays in the low index cladding
Dielectric waveguide mode
z
y
x
Metal
Dielectric
SPP mode
z
y
x

## Slide 13: Derivation of SPP mode fields
Field components
Boundary conditions
Metal
Dielectric
SPP mode
z
y
x

## Slide 14: Derivation of SPP mode fields (cont’d)
Ampère's circuital law:
is a vector:

## Slide 15: Derivation of SPP mode fields (cont’d)
Dispersion relations of SPP mode
Large negative real part
Small positive imaginary part
In the case of
Metal
Dielectric
z
y
x
The SPP mode propagates along the z-axis (real kz) and is localized at the interface (imaginary kx)

## Slide 16: SPP mode and electron oscillation
In metal, Ex is delayed by p/2 in phase relative to Ez
Negative e m suggests that electron displacement is in the same direction as the external electric field
Metal
Dielectric
++
- -
++
- -
++
Ez
Exm
The primary E-field component is longitudinal
Electron motion
Ez
Exm

## Slide 17: Lossless SPP mode in ideal metal
Ideal metal:
K is the absorption index, right?
Loss of guided modes scales with the imaginary part of wave vector along the propagation direction (kz or b); on the other hand, imaginary wave vector along the transverse direction (kx and ky) creates optical confinement rather than loss!
Plane wave in metal
SPP mode in ideal metal
If
kz is a real number
kz is imaginary

## Slide 18: Length scales of SPP mode
Transverse confinement
  Dielectric side: 1/Im(kxd) ~ 100 to 1000 nm
  Metal side: 1/Im(kxm) ~ 10 to 100 nm
  Gold @ l = 600 nm:
  1/Im(kxd) = 390 nm, 1/Im(kxm) = 24 nm
  Silver @ l = 600 nm:
  1/Im(kxd) = 280 nm, 1/Im(kxm) = 31 nm
Propagation distance
  1/Im(kz) ~ 10 to 1000 mm
  Silver @ l = 514.5 nm: 1/Im(kz) = 22 mm
  Silver @ l = 1060 nm: 1/Im(kz) = 500 mm
Metal
Dielectric
SPP mode
z
y
x

## Slide 19: SPP mode dispersion relation
w
kz
Light line in dielectric
i.e.
Drude-Sommerfeld:
From Plasmonics: Fundamentals and Applications, S. Maier, Springer (2007).

## Slide 20: Coupling to SPP mode
Direct coupling from free space to SPP mode is prohibited
Phase matching methods:
  Prism coupling:
  1) Otto configuration
  2) Kretschmann configuration
  Grating coupling
Vacuum light line
Light line in prism
w
kz

## Slide 21: Coupling to SPP mode
Direct coupling from free space to SPP mode is prohibited
Phase matching methods:
  Prism coupling:
  1) Otto configuration
  2) Kretschmann configuration
  Grating coupling
Vacuum light line
Light line in prism
w
kz

## Slide 22: Coupling to SPP mode
Direct coupling from free space to SPP mode is prohibited
Phase matching methods:
  Prism coupling:
  1) Otto configuration
  2) Kretschmann configuration
  Grating coupling
Vacuum light line
qi
Metal gratings
L
w
kz

## Slide 23: Coupling to SPP mode
NSOM probe excitation
Nanoparticle scattering
Fluorescence emission
Fiber-optic coupling
(a)
(b)
(c)
(d)
A. Sharma et al., IEEE Sens. J. 7, 1118 (2007).

## Slide 24: Coupling to SPP mode
The phase matching condition is satisfied only at specific incident angle & wavelength combinations
Back coupling (leakage) into radiative modes
Prism:
Grating:
Surface plasmon “resonance” indicates phase matching
Only TM light couples to SPP
SPP mode shows lower loss in Ag than in Au at l = 633 nm
The phase matched coupling condition is very sensitive to dielectric constant changes
Image quoted from Principles of Nano-optics

## Slide 25: Surface plasmon resonance (SPR) sensors: a historic perspective
Biosensors & Bioelectronics 10, 1-4 (1995).
http://www.biacore.com/lifesciences/history/index.html

## Slide 26: SPR sensing: mechanism
Interrogation scheme
  Angular interrogation
  Wavelength interrogation
  Intensity/phase
Coupling design
  Prism coupling
  Grating coupling (GC-SPR)
  Waveguide/fiber excitation
J. Homola et al.,“Surface plasmon resonance sensors: review,” Sens. Actuators, B 54, 3-15 (1999).
Biacore Tech Note 23: Label-free interaction analysis in real-time using surface plasmon resonance
Handbook of Surface Plasmon Resonance, R. Schasfoort and A. Tudos Ed., RSC Publishing (2008).

## Slide 27: SPR sensing: instrument design
Disposable cartridge
Hand-held reader
© Sensata
Bulk RI detection limit: 5 × 10-6

## Slide 28: SPR vs. resonant cavity sensors
Performance metrics
  RI sensitivity: resonance peak shift per unit bulk refractive index change
  Resonators (cavity perturbation):
  SPR (phase matching): > 104 nm/RIU
  Spectral width of resonance peak (Q)
  Dielectric resonators: Q ~ 10,000
  SPR: Q ~ 100 due to optical loss
< 103 nm/RIU
w
kz
Phase matching
w/o index change
Dw
with index change
Z. Yu et al., Opt. Express 19, 10029-10040 (2011).
J. Hu et al., J. Opt. Soc. Am. B. 26, 1032-1041 (2009).

## Slide 29: Surface plasmon waveguides
D. Gramotnev et al., Nat. Photonics 4, 83-91 (2010).
M. Stockman, Phys. Rev. Lett. 93, 137404 (2004).
Dielectric guided mode
  As waveguide size shrinks:
  poor transverse confinement and eventually cut-off
Channel plasmon polariton (CPP) mode
  As waveguide size shrinks:
  improved transverse confinement: no cut-off !
z
y
x

## Slide 30: Channel plasmon polariton modes and tapers
Wedge mode
Groove mode
Hybridized mode
Nanofocusing tapers
Sub-diffraction-limit (< l/10) confinement
Typical propagation length ~ 1 mm
D. Pile et al., “Theoretical and experimental investigation of strongly localized plasmons on triangular metal wedges for subwavelength waveguiding,” Appl. Phys. Lett. 87, 061106 (2005).
E. Moreno et al., “Channel plasmon-polaritons: Modal shape, dispersion, and Losses,” Opt. Lett. 31, 3447-3449 (2006).
H. Choi et al., “Compressing surface plasmons for nanoscale optical focusing,” Opt. Express 17, 7519-7524 (2009).

## Slide 31: List of symbols
Ee – energy of electron
p – momentum of electron
m – electron mass
k – wave vector
EF – Fermi energy
kF – wave vector of electrons at Fermi surface
ћ – reduced Planck constant (1.055 × 10-34 J·s)
ne – electron density
– position vector indicating electron position
t – time

## Slide 32: List of symbols
g – damping coefficient
or E – electric field
e – elementary charge (1.602 × 10-19 C)
w – angular frequency of oscillating electric field
– amplitude of electron oscillation
– electric polarization (density)
e0 – vacuum permittivity (8.854 × 10−12 C/Vm)
er,e / er,b – free / bound electron contribution to relative permittivity (dielectric constant)
wp – plasma frequency
n – real part of refractive index

## Slide 33: List of symbols
K – imaginary part of refractive index or extinction coefficient
wb – characteristic oscillation frequency of bound electrons
er – relative permittivity or dielectric constant
H – magnetic field
Ed / Em – electric field in dielectric / metal
Hd / Hm – magnetic field in dielectric / metal
kz – propagation constant of guided mode (i.e. wave vector along propagation direction z)
k0 – free space wave vector

## Slide 34: List of symbols
em / ed – permittivity of metal / dielectric
c – speed of light in dielectric medium
c0 – speed of light in vacuum (2.99792458 × 108 m/s)
qi – incident angle of excitation light
np – refractive index of prism
– reciprocal lattice vector of grating along z direction
L – grating period
dl – resonant wavelength shift
l0 – resonant wavelength
G – modal confinement factor