## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 9: Nonlinear Optics
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: References
Fundamentals of Photonics
  Ch. 18 and 19
Nonlinear Optics
  R. W. Boyd
Photonics: Optical Electronics in Modern Communications
  A. Yariv and P. Yeh
  Ch. 8, Ch. 9 and Ch. 14

## Slide 3
“The study of non-linear physics is like the study of non-elephant biology.”
-- Stanislaw Ulam, a mathematician
Non-elephant biology???

## Slide 4: Atomic origin of optical nonlinearity
Simple harmonic oscillator model (linear)
Electronic charge
Atomic nucleus
Restoring force
Linear polarization: parabolic potential
Lorentz-Drude
2nd order nonlinearity: Pockels media
3rd order nonlinearity: Kerr media
2nd order nonlinearity is absent in crystals with centro-symmetry!
Induced dipole moment
Charge density
Electron charge
Displacement
F = kx
F = kx + k2x2
F = kx + k3x3
Damping
Restoring
Driving

## Slide 5: Nonlinear polarization
Linear medium: low field intensity
Nonlinear medium: high field intensity
Linear polarization
Nonlinear polarization
Linear susceptibility tensor
2nd order nonlinear susceptibility tensor
3rd order nonlinear susceptibility tensor
Summation over repeated indices
i, j, k = x, y, z
Notes: Dijkgraaf

## Slide 6: Symmetry and nonlinearity
Symmetry of susceptibility tensors
In lossless media, the nonlinear coefficients are invariant under reshuffling of their indices
  The 2nd order susceptibility tensor of a lossless medium contains 10 independent nonlinear coefficients
2nd order nonlinearity is absent in crystals with centro-symmetry as well as in glasses/liquids
permutation of the indices jkl
Centro-symmetry

## Slide 7: Symmetry and nonlinearity: Si vs. GaAs
Silicon: diamond structure
GaAs: zinc blende structure
3rd order nonlinearity only
2nd & 3rd order nonlinearity
Inversion center

## Slide 8: Glass/polymer poling produces 2nd order nonlinearity
Glass bulk
DC (kV)
T > Tg
Thermal poling:
Apply a high voltage (EDC ~ 106 V/m) at T < Tg and then quench the sample to RT w/o removing the electric field to “freeze in” the polarization.
Material | d (2) (pm/V) | Component
GaAs | 181 | d14
LiNbO3 | 8.8 / 5.8 | d15 / d22
Ge-Sb-S | 8.0 | d22
where the frozen-in EDC results from movement of alkaline ions
Adv. Funct. Mater. 17, 3284-3294 (2007).
Opt. Express 14, 1524-1532 (2006).

## Slide 9: Nonlinear optical effects
2nd order optical nonlinear effects
  Pockels/electro-optic effect
  Second harmonic generation (SHG)
  Sum/difference frequency generation (SFG/DFG)
  Optical parametric amplification/oscillation (OPA/OPO)
3rd order optical nonlinear effects
  Optical Kerr effect/quadratic Pockels effect
  Third harmonic generation (THG)
  Four wave mixing (FWM)
  Two photon absorption (TPA)
  Stimulated Raman/Brillion scattering (SRS/SBS)

## Slide 10: General methodology for nonlinear optics
Write the expression of electric field in medium
  e.g. in an optical waveguide
Calculate the linear and nonlinear polarization
Substitute in to the electromagnetic wave equation
Focus on the terms
with relevant frequencies
And then go do the math !
Source term

## Slide 11: Pockels effect / Electro-optic (EO) effect
2nd order optical nonlinearity
Externally applied electric field modifies the optical properties of materials
  Refractive index, bifringence, etc.
Total electric field:
(E0 << Eex)
Static polarization
Polarization oscillating at the optical frequency
Dielectric constant change due to 2nd order nonlinearity

## Slide 12: Electro-optic materials
Electro-optic coefficient rij
MIT 6.731 Semiconductor Optoelectronics: Theory and Design

## Slide 13: Electro-optic modulators
Encodes 1/0 signal streams onto an optical beam
Electro-optic materials: LiNbO3, III-V, EO polymers
Mach-Zehnder interferometer E-O modulator

## Slide 14: Second harmonic generation (SHG)
2nd order optical nonlinearity
Use light with wavelength l = l0 to generate light with l = l0 / 2
  Frequency doubling w = 2w0
Total electric field:
Radiating dipole with a frequency w = 2w0
Rigorous solution:
Energy is conserved

## Slide 15: Phase matching condition
Only when 2k1 = k2 will SHG be efficient
  n (l1) = n (l2)
General rule for parametric processes
  SHG, SFG/DFG, THG, FWM
  Momentum conservation
2k1 = k2
2k1 ≠ k2
~ 100% SHG conversion efficiency is possible by optimizing phase matching!

## Slide 16
Green lightsaber ???
Diode pumped solid state (DPSS) laser

## Slide 17: Sum frequency generation (SFG) Difference frequency generation (DFG)
2nd order optical nonlinearity
Start with two beams ω = ω1 and ω = ω2
  SFG: ω3 = ω1 + ω2 , k3 = k1 + k2
  DFG: ω3 = ω1 - ω2 , k3 = k1 - k2
SFG/DFG for photodetection
  Use a 1060 nm laser to convert 10 μm mid-infrared radiation to 960 nm near-infrared radiation that can be handled by low-cost detectors
Sum frequency
Pump laser
Laser emission
SHG
Image courtesy of Institut für Angewandte Physik
"Mid-infrared single-photon counting," Opt. Lett. 31, 1094-1096 (2006).

## Slide 18: Optical Kerr effect Third harmonic generation (THG)
3rd order optical nonlinear effects
3rd order optical nonlinearity is present in all materials
Total electric field:
Consider the ω term
Consider the 3ω term
Optical Kerr effect: light-induced refractive index change
Third harmonic generation (THG): frequency tripling
Change of the maginary part of non-linear index: two photon absorption

## Slide 19: Two photon absorption (TPA)
Bimolecular process
  Absorption depends quadratically on light intensity
  Absorption coefficient
Superior spatial confinement of photo-physical and photo-chemical reactions
  3-d patterning using two photon polymerization (TPP)
  Resolution beyond the diffraction limit

## Slide 20: Two photon absorption (TPA)
Opt. Express 12, 5221 (2004)
Bimolecular process
  Absorption depends quadratically on light intensity
  Absorption coefficient
Superior spatial confinement of photo-physical and photo-chemical reactions
  3-d patterning using two photon polymerization (TPP)
  Resolution beyond the diffraction limit

## Slide 21: Two photon absorption (TPA)
Photonic Professional GT2
Wavelength |  | 780 nm
Minimum XY feature size |  | 160 nm typical; 200 nm specified
Build volume |  | 100 × 100 × 8 mm³
Scan speed |  | ≥ 100 mm/s
Bimolecular process
  Absorption depends quadratically on light intensity
  Absorption coefficient
Superior spatial confinement of photo-physical and photo-chemical reactions
  3-d patterning using two photon polymerization (TPP)
  Resolution beyond the diffraction limit

## Slide 22: Structures produced by TPP
10 mm

## Slide 23: Applications of TPP
Photonic wire bonding
Opt. Express 20, 17667 (2012)
Micro-optics fabrication
Nat. Photonics 10, 554 (2016)

## Slide 24: Optical Kerr nonlinearity Figure-of-Merit (FOM)
Material | Nonlinear index n2 (10-20 m2/W) | TPA a2 (10-12 m/W) | FOM ( n2/a2l )
Silica (SiO2) | 2.2 | ‒ | ‒
c-Si | 440 | 8.4 | 0.4
a-Si | 7400 | 41 | 1.4
a-As2S3 | 290 | < 0.01 | > 10
a-As2Se3 | 1200 | 1.0 | 2
Data quoted for l = 1550 nm: B. Luther-Davies et al., Opt. Express 15, 9205 (2007); K. Wang and A. Foster, Opt. Lett. 37, 1331-1333 (2012).
Time scale of electronic Kerr effect: ~ 50 fs

## Slide 25: (Spontaneous) Raman scattering
Raman scattering: inelastic interaction of photons with phonons
  Photon – phonon = Stokes line
  Photon + phonon = anti-Stokes line
Spontaneous Raman scattering is a linear process
wp
wp
ws

## Slide 26: Stimulated Raman scattering (SRS)
Each spontaneous scattering process has a stimulated analog
3rd order optical nonlinearity:
+
-
Opt. Express 21, 13864 (2013)
Notes: Typical values of the Raman gain factor g: 1 cm/GW

## Slide 27: Si Raman lasers that make the headline
First silicon laser pulses with life
Gain: Raman amplification
Loss: free carrier absorption due to TPA
Solution 1: pulsed operation
  Pulse width << tcarrier << pulse period
O. Boyraz and B. Jalali, “Demonstration of a silicon Raman laser,” Opt. Express 12, 5269 (2004).

## Slide 28: Si Raman lasers that make the headline
A continuous-wave Raman silicon laser
Loss: free carrier absorption due to TPA
Solution 2: reverse biased p-i-n diode
  Sweep out free carriers generated by TPA
H. Rong et al., “A continuous-wave Raman silicon laser,” Nature 433, 725 (2005).

## Slide 29: Si Raman lasers that make the headline
Loss: free carrier absorption due to TPA
What is your solution to the loss issue?
Solution 3: reduce free carrier life-time
  Introduce deep level impurities: e.g. Au/Ag
  Reduce waveguide size: enhanced surface recombination
  Increase recombination center defect density
Other innovative solutions?
?

## Slide 30: List of symbols
P – electric polarization (density)
ne – electron density
r – displacement of electrons
D – electric displacement
e0 – vacuum permittivity, 8.854 × 10−12 C/Vm
E – electric field
m – reduced mass
g – damping coefficient
wb – characteristic oscillation frequency of bound electrons

## Slide 31: List of symbols
U – potential energy or waveguide modal profile depending on context
c – electric (linear) susceptibility
er – relative permittivity or dielectric constant
cij / dijk / cijkl – linear / 2nd order nonlinear / 3rd order nonlinear susceptibility
PL / PNL – linear / nonlinear polarization (density)
P(2) – 2nd order nonlinear polarization (density)
c(2) / c(3) – 2nd order / 3rd order nonlinear susceptibility
t – time

## Slide 32: List of symbols
T – temperature
Tg – glass transition temperature
Elight / Eex – electric field associated with incident light / applied DC voltage bias
w – angular frequency of light
c.c. – complex conjugate
rij – electro-optic coefficient
n – refractive index
estatic – permittivity at low frequencies (microwave frequencies in particular)

## Slide 33: List of symbols
l / l0 – wavelength of light
k – wave vector
I0 – light intensity
n2 – (Kerr) nonlinear index
Dn / Da – change of refractive index / absorption coefficient due to nonlinear effects
a2 – two photon absorption coefficient
Eg – bandgap energy
ћ – reduced Planck constant, 1.055 × 10-34 J·s
wp – angular frequency of pump light

## Slide 34: List of symbols
ws – angular frequency of Stokes scattered light
Is – Stokes light intensity
Ip – pump light intensity
g – Raman gain factor
tcarrier – carrier lifetime