I. Intramolecular and Intermolecular Forces : Attractive

| Type of Interaction | Classification | Characteristics | Schematic |
| --- | --- | --- | --- |
| Covalent : | Primary or Chemical Bonds : ( usually characterized as individually “strong” ( outer orbital e- cooperatively shared between two or more atoms so that discrete nature of atoms is lost ( quantum mechanical in origin | ( e- are localized ( directional (i.e. oriented at well-defined angles to each other) |  |
| Metallic : |  | ( only metals atoms are involved ( e- are completely delocalized and mobile throughout entire material ( non-directional |  |
| Ionic : ( ion-ion | Secondary or Physical Interactions : ( usually characterized as individually “weak” ( no e- sharing, more subtle attraction between (+) and (-) charges, discrete nature of atoms preserved ( typically exhibits : ( lack of specificity ( lack of directionality ( lack of stoichiometry | ( coulombic in origin, occurs between oppositely charged species ( electron transfer from one atom to another |  |
| Polar Interactions : ( charge-dipole ( dipole-dipole ( hydrogen bonding |  | ( force between an ion and a dipole or two dipoles where the (+) charge attracts the (-) charge (purely electrostatic) ( H-bonding : a special type of dipole-dipole interaction that results from the bonding between a H atom which is partially (+) charged and a highly electronegative atom such as O, F, N, Cl, (directional) |  |
| Polarization Interactions : ( charge-nonpolar (induced or instantaneous dipole) ( dipole-nonpolar (induced dipole) |  | ( an ion or dipole in the vicinity of a nonpolar atom or molecule causes instantaneous polarization and electrostatic attraction |  |
| Dispersion or London Interactions : (*also called charge-fluctuation, electrodynamic, induced-dipole-induced dipole forces) ( nonpolar-nonpolar |  | ( the (+) nucleus of a nonpolar atom attracts the (-) charged electrons of another nonpolar atom resulting in instantaneous, induced, dipoles and fluctuating electron clouds ( quantum mechanical in origin |  |
| Hydrophobic : | Special Interactions : ( not really true “bonds” ( non-directional | ( attraction between nonpolar molecules in aqueous solution caused by their inability to form H-bonds with HOH so as to minimize the disruption of H-bonds in HOH ( entropy-driven |  |
| Entropic Elasticity : |  | ( attractive, recoiling force produced via extensional deformation macromolecules |  |

II. Intramolecular and Intermolecular Forces : Repulsive

| Type of Interaction | Characteristics | Schematic |
| --- | --- | --- |
| Exchange, Hard-Core, or Steric Repulsion : | ( repulsion due to overlap of electron clouds according to Pauli Exclusion Principle, as well as repulsion of (+) charged nuclei ( quantum mechanical in origin |  |
| Born Repulsion : | ( electrostatic repulsion between similarly charged ions |  |
| Hydrophilic : | ( repulsion of two hydrophilic molecules in aqueous solution in order to maximize H-bonding to water |  |
| Entropic Elasticity : | ( repulsive force produced via compression of long-chained, flexible macromolecules |  |
| Diffuse Counterion Electrical Double Layer : | ( repulsive osmotic force between two charged surface due to overlap of diffuse counterion electrical double layers |  |
| Steric Repulsion (Polymers) : | ( osmotic pressure originates from solvent translational entropy and intrachain excluded volume due to short-range monomer-solvent affinity and/or monomer-monomer repulsion. |  |

# Text boxes

anion

cation

+

-

+

+

+

-

+

+

-

+

-

e-

e-

+

e-

e-

e-

e-

e-

e-

e-

e-

e-

e-

e-

-

+

-

+

-

+

+

-

+

-

+

+

VDW

e-

e-

+

+

+

+

+

+