Gold Evaporation Procedures – RM 66-425

(Jen McKeehan 10/31/02)

Initiation:

- Make sure vent valve (upside down valve on left) and valve C (silver crank valve on right) are closed.

- Turn on power switch to black gauge box.  Lower box on shelf to right of evaporation chamber

- Open Valve A

- Turn on cooling water (right faucet)

- Turn on vacuum pump (on floor to left of evaporation chamber)

- Wait at least 20 minutes

- Plug in diffusion pump

- Wait additional 40 minutes or until gauge A reads below 50 militorr (5 e –2)

Loading Samples:

- While waiting, load samples

- Raise evaporator chamber by turning crank

- Load Samples onto underneath of three-legged table

- Attach wafers with binder clips, take off handles

- Weave spring through hole in stand to create spring to hold other samples

- Stand three-legged table inside evaporation chamber. No legs touching holders

- Use a piece of wire to center and hold detector, whole face must be aligned

- Install chromium rod and gold trough, use small metal pieces to prop up trough – must be tight

- Chromium rod is on right side, gold tough on left side, divider in between

- Put gold balls in trough

- 1 gold shot ~ 150 A

- To get more gold balls ask Dr. Choi or Manish Bajaj

- Check conductivity through rod and trough.

- Set volt meter to 200 and sound under (

- Should be less than 1

- There should be no conductivity between holders and bottom

- Clean seal by blowing off and wiping with ethanol

Pumping Down:

- Lower jar with crank

- Close valve A

- Open valve B, and make sure bell jar seals

- Gauge A gives pressure in diffusion pump.  Need to keep it below 200 militorr (2 e –1)

- When gauge A approaches 200 militorr (slow) close B, wait 10 sec, and open A

- When diffusion pump pressure is back down to 50 militorr (quick) then close A, wait 10 sec, open B

- Never open A and B at same time

- Go back and forth (steps 12-15) until gauge B which gives bell jar pressure reads 50 militorr

- Then close valve B and keep valve A open

- When pressure in both is about the same, slowly open gate valve C (right side of evaporation chamber)

- When pressure in diffusion pump jumps up, back off a little and wait for it to equilibrate

- Open valve C completely (several more turns, there is no stop at the end) when there are no more sudden jumps in diffusion pump pressure

- Wait until gauge A reads less than 40 militorr (4 e –2)

- Turn on Ionization Gauge by pushing filament button on gauge box

- Now let pump down until ion gauge (top gauge) reads 4 e –6.  (~ 2 hours)

- Add liquid N to open tube on lower center using funnel

- Add until comes out of overflow hole

- Should lower pressure to 1-2 e –6

Coating:

- Turn on Monitor,	Left = Deposition rate	Right = Thickness (from detector)

- Push Program, Push C, Choose 3 for Chromium, Push Enter, Push Program again

- Plug in blue box

- Turn wheel to control deposition rate – set to 20

- Want ~1 A/sec deposition rate.

- When reach desired thickness (20A = .02), turn wheel down, pull plug

- Push Program, Push C, Choose 1 for Gold, Push Enter, Push Program again

- Push button 3 to zero out detector

- Plug in yellow plugs

- Turn wheel to increase deposition rate – start around 35 and creep up

- Want 1-2A/second deposition

- When reach desired thickness (300 = .3), turn down wheel, pull plugs

- Turn off ion gage

- Turn off Monitor

- Close gate valve

- Unplug diffusion pump

- Open vent calve slowly

- Let vent

- Lift bell jar and remove samples

Shut Down:

- Wait ½ hour

- Turn off cooling water

- Close valve A

- Turn off vacuum pump

- Turn of gauge box

- Lower bell jar

# Text boxes

1 hour

1 hour

+ 2 hr wait

20 minutes

30 min wait

+5 minutes

15 minutes

Total Time ~ 5.5 hours