## Slide 1: Multicore fibre and fibre tapers
Dionne Haynes
FOIA-IV August 2014

## Slide 2
Talk overview
Multicore fibre and photonic lanterns
- MCF for mode scrambling (amplitude and phase)
In collaboration with Itan Gris-Sanchez and Tim Birks
@ Bath University
Multimode fibre tapers
In collaboration with Sergio Leon-Saval @ Usyd

## Slide 3
Enable efficient coupling of “seeing limited "and partially AO corrected PSFs into
the single-mode regime
Enable photonic function in a seeing limited regime with high efficiency
i.e. photonic filters (FBGs) for OH suppression
Enable efficient implementation of diffraction limited spectrographs
Break the dependence of instrument size on telescope diameter as the entrance
slit of the spectrograph becomes diffraction limited thus allowing a much more
compact system for a given resolving power
? New technique to improve mode scrambling and reduce modal noise
i.e. amplitude and phase scrambling
Multicore Fibres and Photonic Lanterns

## Slide 4
And now for something completely different

## Slide 5
MCF for phase and amplitude scrambling
MM core
transition
single cores
transition
MM core
~3 meters in length
The lantern transforms each input MMF mode into a distinctive pattern of amplitudes and phases across the MCF cores - i.e. a supermode
In a perfectly straight MCF with identical cores, these amplitude and phase relationships are preserved, so entering the output lantern we still have that same supermode. The reverse of the input lantern, and the original input mode is restored in the output MMF as in the MCF FBG devices
To get mode scrambling, we deliberately do not preserve the phases between the MCF cores. If the cores are uncoupled, we can do this simply by making their optical lengths different. By making the cores dissimilar, and/or bending the fibre. This couples light pseudo-randomly between the supermodes, and hence between the modes of the output MMF. Vibrating the fibre adds some extra randomisation and time-averaging to the process.

## Slide 6
High resolution spectroscopy i.e. RV science
Calibration
- wavelength calibration (frequency combs)
- sky subtraction
Applications

## Slide 7
MCF consists of 511 individual cores
designed to operate over a broadband
visible wavelength range 380-860nm
has dissimilar cores to provide the path
length differences
some of the cores are 2 and 3 moded at
the shorter wavelengths to persevere
mode number (low loss)

## Slide 8
Incoherent light
MCF511
d
Near Field
Octagonal 100 μm
MCF 55 μm

## Slide 9
Coherent light
MCF511
Near Field
d/3

## Slide 10
Coherent light
Far Field

## Slide 11
Far field patters for entrance spot displacements. Input spot coherent light, diameter 25μm.
Far Field
Incoherent light

## Slide 12
The multicore fiber has equivalent scrambling and modal noise performance to the octagonal fiber
Further improvements of the MCF are anticipated once the residual core structure has been reduced
Splice short section of MMF on ends of MCF PL
Create dopant diffusion by heating end of MCF PL
Aim to generate a stable Gaussian near field and far field pattern
i.e Gaussian profile at image plane and pupil plane
the far field that illuminates the spectrograph grating and much of its optics, and therefore a stable Gaussian profile is desired to achieve low scattering and minimal aberration effects
(Simon Ellis et al. SPIE 2014)
Any movement of the fibre, bending, shaking improves both phase and amplitude scrambling without FRD!
Can be retrofitted to existing fibre feeds at the output end

## Slide 13
Any movement of the fibre, bending, shaking improves both phase and amplitude scrambling without FRD!
Can be retrofitted to existing fibre feeds at the output end
Can splice MMF tapers directly to MM port of PL to perform beam conversion

## Slide 14
On sky test of VIS MCF scrambling fibre
IR scrambling fibre
RV science in IR
Phase and amplitude scrambling for OH suppression
MCF FBG instruments
It is possible that in the future we will have IFUs and MOS instruments in the IR with OH suppression, mode scrambling, modal noise suppression and frequency comb calibration!!!!
Future work

## Slide 15
Optical fibre tapers for focal adaptation
Increased demand for efficient telescope to spectrograph coupling
Tapers provide beam speed and image scale manipulation
Tapers offer a compact alternative to bulk optics
FOIA-IV Dionne Haynes

## Slide 16: Conservation of Etendue
Concept of conservation AΩ states that if light losses are negligible, the spatial and angular content of the light anywhere within or at either end of a taper is described by:
Ai ni2 sin2 θi = Ao no2 sin2 θo
F-ratioout = (do/di) x F-ratioin and F-ratioin < F-ratioout . do / di for lossless transition
using small angle approximation:
n sin θ = NA and Ai / Ao =di2 / do2 therefore NAout / NAin = do / di
however if the product of the input NA and the ratio of the diameters exceeds the maximum NA
that the taper can support, light will escape to the cladding and be lost. Therefore for a lossless
transition the maximum input NA is: NAin < NAout . do / din
θi
θo
Ai
Ao
di
do
FOIA-IV Dionne Haynes

## Slide 17: Fibre taper types
Up-tapers
Fused end taper - taper section fused onto a longer fixed diameter fibre. Transition lengths can be 5 –100mm if made with a fibre tapering station or 2 to 50m if tower drawn. Large transition ratios possible.
Laser machined taper formed out of existing glass material at the end of the fibre. Short transition length 5 – 15mm, maximum transition ratio 2.5 to 3
Down-tapers
Made by controlling the drawing process to produce a single continuous fibre. Transition lengths from 2 – 100mm possible when using a fibre tapering station or 2 to 50m if tower drawn. Large and small transition ratios possible.
fused end up-taper
down-taper
laser machined up-taper
MAGNIFICATION
REDUCTION
FOIA-IV Dionne Haynes

## Slide 18: Fibre taper considerations
Beam speed exiting first taper transition
Beam speed degradation (FRD) in fibre length
Beam speed entering second taper transition
Solution: larger taper ratio at output end to account for FRD in length of fibre!
f/8
f/3
Need 2.7 x taper ratio
likely f/2.7
f/?
FRD
2.7 x taper ratio
f/8
f/7.3
f/8
2.7 x taper ratio
f/3
f/2.7
3 x taper ratio
f/8
EXAMPLE
FOIA-IV Dionne Haynes

## Slide 19: Fibre taper considerations
Do not exceed the maximum NA that the taper can support
f/8
2.5 x taper ratio
f/6
EXAMPLE: Taper NA 0.22 ~f/2.3
f/3.2
f/2.4
f/5.75
f/2.3
f/5
f/2
exceeds taper NA, therefore light escapes to the cladding and is lost
FOIA-IV Dionne Haynes

## Slide 20: 2011- Commercial fibre tapers
The results for two tapers of different length with the same transition ratio of 2:1 are presented. Taper 1 (up- taper) supplied by Polymicro has a 10mm transition length and Taper 2 (down-taper), supplied by Ceram Optec has a 50mm transition length. The tapers were tested at a central wavelength of 600 ± 20nm at fast and slow f-ratios to demonstrate focal reduction and magnification.
Reference fibres of the same fibre type are measured under the same conditions as the tapers. The reference fibre data is used to normalize the taper results such that the intrinsic FRD of the fibre length is accounted for, enabling direct measurement of the taper transition.
The preliminary results show that the commercial tapers perform very well as focal reducers and magnifiers. The taper transitions perform as expected for 1:2 and 2:1 demonstrating that AΩ is conserved.
Polymicro fibre taper, laser machined up-taper, 10mm transition length, 1:2 transition ratio
FOIA-IV Dionne Haynes

## Slide 21: 2012 – Prototype fibre up-taper for focal magnification
instrument requires beam conversion from an f/3 input beam to f/13.9 output beam
FRD in base fibre length f/3  ~f/2.7 to f/2.8
required magnification ~5
therefore fibre core diameter ratio needs to be ~5
Base fiber (~2m long)
Splice
Taper
Cleave
Fiber taper
preform
Manufactured at AIP/innoFSPEC using Vytran GPX-3400 glass processing station
Prototype device design
FOIA-IV Dionne Haynes

## Slide 22: Up-taper manufacture
Vytran GPX-3400 glass processing station
Fibre taper preform: FVA 400 440 580
400 um core, core/clad ratio 1:1.1
Base fibre
FBP080096124
80 μm core
96 μm clad
core/ clad 1:1.2

## Slide 23: Fusion splicing of fibre taper to base fibre
Taper 2
cladding diameter mismatch
~88.0 μm (taper) and 96.0 μm (base fiber)
~6 μm core misalignment
Taper 1
cladding diameter mismatch
~86.4μm (taper) and ~96.0 μm (base fiber)
~4-5 μm core misalignment
core diameter mismatch ~2 μm
 | Total estimated splice loss
Taper 1 | 5.5 to 6.5 %
Taper 2 | 5.5 to 6.5 %
A. D. Yablon – Optical Fibre Fusion splicing
Notes: Taper 5 core misalignment ~4-5um and core diameter mismatch of ~2um offset loss=3.5 to 4.5 % core diameter loss = 2% Total = 5.5 to 6.5 % loss
Taper 9 core misalignment ~7-8um offset loss = 5.5 to 6.5% loss

## Slide 24
Note: Reference fibre throughput ~91% at 600nm
 | fin (95% EE) | Taper Ratio TR | Output EE at fin x TR | Relative throughput
Taper 1 | f/2.7 | ~5.1 | ~95% | 93%
Taper 2 | f/2.7 | ~5.0 | ~92% | 94%
FOIA-IV Dionne Haynes

## Slide 25
 | fin (95% EE) | Taper Ratio TR | Output EE at fin x TR | Relative throughput
Taper 1 | f/3.2 | ~5.1 | ~91% | 95%
Taper 2 | f/3.2 | ~5.0 | ~89% | 95%
Note: Reference fibre (no taper) throughput ~91% at 600nm
FOIA-IV Dionne Haynes

## Slide 26
Manufactured and tested x5 taper transitions
Non optimised splices causing losses
Demonstrated that tapers provide good conservation of Etendue
Development ongoing to reduce losses to improve performance
FOIA-IV Dionne Haynes

## Slide 27
FOIA-IV Dionne Haynes
Thank you!