## Slide 1: Photonic lantern or multi-core fibres for astrophotonics
University of Bath, UK
20 Aug 2014
Itandehui Gris Sánchez

## Slide 3
What is an optical fibre?
Optical waveguide made out of a dielectric material most commonly high purity silica glass, usually several km long.
Low loss window from 800 nm to 1600 nm.

## Slide 4: Standard vs Specialty

## Slide 5
How does an optical fibre guide light?
http://drhart.ucoz.com/Research/fiber_modes.png
  Huygens-Fresnel principle
  Geometric optics?

## Slide 6: What is a photonic lantern?
1 MM core with N modes
low-loss interface between multimode and single-mode waveguides:
N SM cores
mode-number matching:
MM modes = SM cores
SG Leon-Saval et al, Opt Lett 30 (2005) 2545
Notes: Post processed mutlicore optical fibre

## Slide 7: Reciprocal device
low-loss interface between single-mode and multimode waveguides:
N SM cores
1 MM core with N modes
SG Leon-Saval et al, Opt Lett 30 (2005) 2545
mode-number matching:
MM modes = SM cores
N=

## Slide 8: Taper transition
TA Birks et al, Opt Express 20 (2012) 13996
mode 42
mode 42
mode of MM core
supermode of coupled SM cores
independent SM cores
 adiabatic 

## Slide 9: Photonic lanterns, Type 1
SMFs tapered in a photonic crystal fibre template
SG Leon-Saval et al, Opt Lett 30 (2005) 2545
19 SMFs
~4 mm
145 µm
MMF
19 SMF
MMF
transition

## Slide 10: Photonic lanterns, Type 2
SMFs tapered in a low-index glass capillary
D Noordegraaf et al, Opt Express 17 (2009) 1988
D Noordegraaf et al, Opt Express 18 (2010) 4673
N = 61 SMFs
0.76 dB loss
NK Fontaine, OFC (2013) OTh1B.3
DB Mortimore et al, Appl Opt 30 (1991) 650

## Slide 11: Photonic lanterns, Type 3
multicore fibre tapered in a low-index glass capillary
oxy-butane flame
F-doped silica capillary
MCF
TA Birks et al, Opt Express 20 (2012) 13996
loss < 0.5 dB

## Slide 12: Photonic lanterns, Type 4
integrated optics, eg ultrafast laser inscription
RR Thomson et al, Opt Express 19 (2011) 5698
I Spaleniak et al, Opt Lett 21 (2013) 27197

## Slide 13
Photonic lanterns for IR spectral filtering

## Slide 14: FBG as spectral filter
index modulation by UV radiation
www.proandsons.com
Periodic grating  L unique  only one l reflected
J Bland-Hawthorn et al, Nature Commun 2 (2011) 581
Notes: Core foto-sensible 

## Slide 15: SM performance in MM devices
interfacing single-mode FBGs to multimode telescope optics:
SG Leon-Saval et al, Opt Lett 30 (2005) 2545
www.things-to-make-and-do.co.uk
Hubble Ultra-Deep Field

## Slide 16: FBGs to block OH emissions from earth’s atmosphere
J Bland-Hawthorn et al, Opt Express 12 (2004) 5902
Aperiodic FBG in a single mode fibre (SMF)
 Fourier components of L  several l are reflected
Mode dependant response of FBG!
qm

## Slide 17: Spectral filter with multimode FBG's
proof of concept
SG Leon-Saval et al, Opt Lett 30 (2005) 2545
19 FBGs
mean SMF
MMF
measurements "on sky"
J Bland-Hawthorn et al, Nature Comms 2 (2011) 581
C Q Trinh et al, Astron J 145:51 (2013)

## Slide 18
Photonic lanterns for mode scrambling

## Slide 19: Propagation between two lanterns
mode of MM core
supermode of coupled SM cores
independent SM cores
phases preserved
same supermode
same mode
identical paths
ideal case:

## Slide 20: Propagation between two lanterns
mode of MM core
supermode of coupled SM cores
independent SM cores
phases scrambled
several supermodes
severalmodes
perturbed paths
mode spectrum: scrambled, uniformly filled, insensitive to input
losses: MM transmission line with SM performance
mode-number matching
realistic case:
TA Birks et al, Opt Express 20 (2012) 13996
N=
Notes:   Fixed FRD

## Slide 21
TA Birks et al, Opt Express 20 (2012) 13996
Multicore fibre terminated with lanterns
more compact MM FBG:
input
mode scrambler:

## Slide 22
TA Birks et al, Opt Express 20 (2012) 13996
Step-index MMF
input
mode scrambler:
step-index MMF

## Slide 23
Lantern-terminated MCF
input
MCF with lanterns
mode scrambler:
step-index MMF
TA Birks et al, Opt Express 20 (2012) 13996

## Slide 24
Lantern-terminated MCF
input
step-index MMF
MCF with lanterns
t = 0.1 s
mode scrambler:
TA Birks et al, Opt Express 20 (2012) 13996

## Slide 25
511 cores from 1.7704 to 3.3388 fibre diameter 567mm
Multicore fibre scrambler
DM Haynes et al, SPIE (2014) 915155

## Slide 26
Diameter monitor
Preform feed
Furnace
Coating cup
UV lamp
Vfeed
Vdraw
Capstan
Take-up
Hot zone
Vacuum and pressure lines

## Slide 27: PCF and multicore fibre fabrication
Stack and draw

## Slide 28: Tapering the jacketed MCF
TA Birks et al, JLT 10 (1992) 432
fibre
oxy-butane burner

## Slide 29: Conclusions
Photonic lantern: conversion between a multimode port and a multiport system
Four existing lantern technologies
Potential in MM and SM interfaces:
  MM spectral filtering
  Mode scrambler

## Slide 30
Thank you

## Slide 31: Spare slides

## Slide 32: Adjusting the geometry
SG Leon-Saval et al, Nanophotonics 2 (2013) 429
are they the right N modes?
MM core
good array geometry
bad array geometry
NK Fontaine et al, Opt Express 20 (2012) 27123