## Slide 1: MIT 3.071 Amorphous Materials 13: Optical Fibers and Waveguides
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2
The masters of light
“If we were to unravel all of the glass fibers that wind around the globe, we would get a single thread over one billion kilometers long – which is enough to encircle the globe more than 25,000 times – and is increasing by thousands of kilometers every hour.”
2009 Nobel Prize in Physics
Press Release

## Slide 3: Light confinement via total internal reflection
nhigh
nlow
nlow
Light
q
Condition for TIR:
Core
Cladding
Snell is right
by Ulrich Lohmann
PMMA
Air

## Slide 4: Waveguide cross-section geometries
Slab waveguide
Channel/photonic wire
waveguide
nhigh
nlow
nlow
nhigh
nlow
Rib/ridge waveguide
nhigh
nlow
nlow
1-d optical confinement
2-d optical confinement
cladding
cladding
core
core
cladding
Step-index fiber
Graded-index (GRIN) fiber
core
cladding

## Slide 5: Optical fiber materials
Glasses: silica and other oxides, chalcogenides, halides, polymers
Metals, crystalline oxides and semiconductors, etc.
Dopants in silica glass
  Increase index: GeO2, P2O5, TiO2
  Decrease index: B2O3
  Luminescent centers: rare earth (e.g. Er)
Refractive index nD of SiO2-GeO2 glass
Appl. Opt. 24, 4486 (2004)

## Slide 6: Standard single-mode silica optical fiber structure
Core/cladding: low loss light propagation
Buffer/jacket: protection against mechanical damage and the environment (UV radiation, humidity, etc.)
Core
Cladding

## Slide 7: Fiber drawing process
Fiber preforms
Drawing tower
Fiber spool
Viscosity window for fiber drawing:
104 to 106 Pa·s
Notes: https://www.technologyreview.com/s/401266/drawing-optical-fibers/

## Slide 8: Fiber drawing: diameter control
F
Neck-down region
Preform
Drawing tension:
Fiber diameter is determined by the drawing speed
Fiber diameter is feedback loop controlled in real time during drawing
Candy fiber drawing
A
IEEE Photon. J. 2, 620 (2010)
J. Appl. Phys. 49, 4417 (1978)

## Slide 9: Standard silica fiber preform fabrication
Modified chemical vapor deposition (MCVD)
  SiCl4 + O2 → SiO2 (soot) + Cl2
  GeCl4 + O2 → GeO2 + Cl2
Layer composition and thickness controlled in each torch sweep
Traversing torch
Rotating silica tube
Reactant gases
Soot
High temperature reaction zone
MCVD lathe, University of Southampton
Water-free reaction: minimal -OH contamination
Notes: Silicon tetrachloride has a boiling point convenient for purification by repeated fractional distillation

## Slide 10: Optical fiber manufacturing and testing
Notes: Optical Time-Domain Reflectometer (OTDR)

## Slide 11: Glass properties impact fiber processing
Glass forming ability
  Processing window
Liquid fragility
  Fragility parameter
  Temperature sensitivity

## Slide 12: Multi-material, microstructured optical fibers
Microstructured optical fibers: photonic bandgaps and various sizes of the rings give rise to the different colors
A. Argyros, the University of Sydney
Optical mode shaping
Dispersion engineering
Broadband transmission
Multi-functional sensing
Nat. Mater. 6, 336, (2007)

## Slide 13: Multi-material, microstructured optical fibers
Rod-in-tube
Extrusion
Stack-and-draw
Adv. Mater. 18, 845 (2006)
Int. J. Appl. Glass Sci. 3, 349 (2012)

## Slide 15: Planar integration: the paradigm shift
The OLD way:
discrete devices
Integration
The NEW way:
integrated circuits
Smaller, faster cheaper & greener

## Slide 16: Photonic integrated circuit (PIC)
Source
Modulator
Detector
Waveguide
Semiconductor lasers
E-to-O signal encoders
Optical “wires”: signal routing
O-to-E conversion
Optical diodes
Isolator
Lasers: hybrid laser, Ge laser
Isolators: magneto-optical isolator
Modulators: III-V/Si ring and MZI
Waveguides: SOI, nitride, glass, polymer
Detectors: III-V and Ge detectors

## Slide 17
Laser cavity
Optical switch
Photodetector
Waveguide
Waveguide
All optical components integrated on a glass substrate

## Slide 18: State-of-the-art integrated photonics
Optical fiber interface
Photonic chip
IMEC photonic chip & Tyndall fiber array packaging
Substrate
Cladding
Core
Light
Integrated planar waveguide
Substrate platforms: Si, III-V semiconductors, glass, LiNbO3, polymer
Core material: c-Si, III-V, a-Si, SiO2, SiN, ion exchange glass, polymer

## Slide 19: Planar waveguide fabrication
Substrate
Cladding layer
Core layer
Amorphous waveguide material: ease of deposition, low optical loss
Planar waveguide platform: massively parallel low-cost fabrication, geometry/material diversity, interfacing with other on-chip components

## Slide 20: Optical loss in fibers and waveguides
Material attenuation
Surface roughness scattering
  Optical fiber
    Frozen surface capillary waves due to energy equipartition
    Usually small in optical fibers
  Planar waveguide
    Surface roughness resulting from imperfect patterning
    A major loss mechanism
s : RMS roughness
J. Lightwave Technol. 23, 2719 (2005)

## Slide 21: Optical communication system
0 = peace
1 = invasion

## Slide 22: Optical communication system
Optical receiver (Rx) / transceiver
Transmitter driver circuit
Optical transmitter (Tx) / transceiver
Electronic digital signal
1
0
1
0
1
1
0
1
0
1
Optical digital signal
Receiver circuit
Electronic digital signal
1
0
1
0
1
Optical fiber / waveguide
Opt. Express 19, B777 (2011)
Fiber ribbon

## Slide 23: Wavelength division multiplexing (WDM)
Single optical fiber
Optical channel
Single-core fiber communication speed record 2011 (NEC):
370 channels × 273 Gbps data rate = 101 Tbps

## Slide 24
See what the “FiOS boy” says about WDM!

## Slide 25: Inside Google’s data center

## Slide 26
Notes: http://natick.research.microsoft.com

## Slide 27
 | 2004 |  |  | 2010+ | 
Enterprise Distance: 0.1-10km
Rack-Rack Distance: 1-100m
Board-Board Distance: 50-100cm
Chip-Chip Distance: 1-50cm
OPTICAL
Electrical to optical interconnect
ELECTRICAL
3.125G 10G 40G
3.125G 5-6G 10G 20G
3.125G 5-6G 10G 15-20G
10G >= 40G
Copper Tech
Transition Zone
Integrated
photonics?
Optical Tech

## Slide 28: Active optical cable (AOC)

## Slide 29: Summary
Device fabrication
Fiber drawing
  Preform fabrication: MCVD process
  Drawing parameter control: fiber diameter & draw tension
  Multi-material fiber and microstructured fiber processing
Planar waveguide fabrication
Optical loss in fibers and waveguides
Material attenuation
Surface roughness scattering
Optical communications
Digital communication systems & WDM