# Drawing Notes which apply to all carbon fiber parts

| 1 | Nominal material for all plies: |  |
| --- | --- | --- |
|  | a | Fiber shall be Granoc CN-80 (or XN-80), tensile modulus 780 GPa. |
|  | b | Each ply shall be bidirectional fabric, 240 gsm, plain weave (PF-XN80-240). |
|  | c | Resin shall be EX-1515 cyanate ester. |
|  | d | Fiber shall be pre-impregnated with resin (prepreg). |
|  | e | Prepreg shall have resin mass fraction 32% ± 2%. |
| 2 | Alternative materials: |  |
|  | a | Vendor may propose equivalent alternate fiber or resin. |
|  | b | Approval of any alternate(s) is entirely at customer's discretion, and shall be made in writing. |
| 3 | Processing: |  |
|  | a | Cured part shall have fiber volume fraction between 50% and 60%. |
|  | b | Cured part shall have void fraction <= 1%. |
|  | c | Cure temperature shall 121°C for 3 hour minimum hold time (EX-1515). |
|  | d | Any alternate resin shall be cured according to resin manufacturer's recommendations. Cure profile shall be approved by customer in writing. |
|  | e | Minimum vacuum pressure 25 inHg shall be applied during cure. |
|  | f | Additional autoclave pressure of 40-100 psig is preferred. |
|  | g | Surface texture for bonded interfaces shall be generated by incorporating peel ply in the vacuum bag stackup during cure. |
| 4 | Fiber directions, unless otherwise specified on drawings: |  |
|  | a | 0° direction is parallel to center axis for cylindrical parts. |
|  | b | 0° direction is parallel to longest orthogonal direction for planar parts. |
| 5 | Material coupons shall be delivered to customer with parts. |  |
|  | a | Coupons shall be laid up and cured alongside / simultaneous to production parts. |
|  | b | Coupons shall be at least 1" wide x 5" long, and of same thickness. |
|  | c | Vendor shall deliver minimum of 2 coupons per unique layup definition. |
| 6 | Vendor shall deliver the following documentation with parts: |  |
|  | a | Material certifications from fiber and resin manufacturer(s). |
|  | b | Measured time, temperature, and vacuum pressure data during cure of all parts. |
|  | c | Clear documentation of no loss of vacuum pressure during cure. |
|  | d | Measured autoclave pressure data (if applicable). |
|  | e | Total storage and out times of prepreg prior to cure. |

# Estimated laminate properties

| Assumed values for manufacturing process |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Mm | 32.0% |  | resin mass fraction in prepreg |
|  | FAW | 240 | gsm | fiber areal weight |
|  | Vv | 0.5% |  |  |
|  | surface texture thickness | 70 | um | both sides, from LBNL measurements 2013-04-24 with peel-ply surface |
| Estimates of cured ply thickness and prepreg areal weight |  |  |  |  |
|  | CPT woven | 209.2 | µm | cure ply thickness |
|  | PAW | 353 | gsm | prepreg areal weight |
| Fiber and Matrix Properties |  |  |  |  |
|  | Fiber | CN-80 |  |  |
|  | E1f | 780 | GPa | CN series data sheet |
|  | E2f | 8.9 | GPa | by analogy to P-55S fibers |
|  | Em | 4.4 | GPa | Kollar&Springer. Approx value for structural epoxies |
|  | ν12f | 0.23 |  | by analogy to P-55S fibers |
|  | νm | 0.35 |  | Kollar&Springer. Approx value for structural epoxies |
|  | ρf | 2.17 | g/cm³ | CN series data sheet |
|  | ρm | 1.17 | g/cm³ | EX-1515 data sheet |
|  | G12f | 317.1 | GPa |  |
|  | Gm | 1.6 | GPa |  |
| Uni Ply Properties |  |  |  |  |
|  | weave stiffness reduction factor | 5% |  | LBNL typical value, based on 2013-04-12 tensile test data |
|  | Vf | 53.1% |  |  |
|  | Vm | 46.4% |  |  |
|  | √Vf | 0.73 |  |  |
|  | E11 | 395.7 | GPa |  |
|  | E22 | 6.4 | GPa |  |
|  | G12 | 5.9 | GPa |  |
|  | nu12 | 0.284 |  |  |

| Assembly | Description | Drawing MVTX-2-S- | Location where layup applies | Comment | no. plies | Thickness (mm) | Layup ID | Layups: Stackup definitions start at inner surface --> outer surface |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CYSS | CYSS - Cone | 00077 | most of part | ply drop defined in separate row | 10 | 2.16 | A.1 | 0/90 | 0/90 | 0/90 | 0/90 | ±45 | ±45 | 0/90 | 0/90 | 0/90 | 0/90 |
|  |  |  | @ 13.4 mm ply drop off | ±45 ply shall be on INNER surface | 5 | 1.12 | A.2 | drop | drop | drop | drop | drop | ±45 | 0/90 | 0/90 | 0/90 | 0/90 |
| CYSS | CYSS - Cylinder | 00079 | complete part | - | 5 | 1.12 | B | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |  |  |  |  |
| LAYER ONE | L1 - C Ring | 00034 | complete part | machine chamfer | 7 | 1.53 | C | 0/90 | ±45 | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |  |  |
| LAYER ONE | L1 - Pass Through Divider | 00036 | complete part | - | 4 | 0.91 | D | 0/90 | ±45 | ±45 | 0/90 |  |  |  |  |  |  |
| LAYER ONE | L1 - PP1 Divider | 00039 | complete part | - | 4 | 0.91 | D | 0/90 | ±45 | ±45 | 0/90 |  |  |  |  |  |  |
| LAYER ONE | L1 - S. EW - Rib | 00035 | complete part | vendor may propose laying up to alternate thickness 2.5 mm (i.e. to save a mold) | 6 | 1.33 | E | 0/90 | ±45 | 0/90 | 0/90 | ±45 | 0/90 |  |  |  |  |
| LAYER ONE | L1 - S. EW - Spring | 00033 | complete part | machine step down to 0.5 mm and chamfer | 9 | 1.95 | F | 0/90 | ±45 | 0/90 | ±45 | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |
| LAYER ONE | L1- S. EW - Cone | 00032 | complete part | - | 5 | 1.12 | B | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |  |  |  |  |
| LAYER TWO | L2 - C Ring | 00049 | complete part | machine chamfer | 7 | 1.53 | C | 0/90 | ±45 | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |  |  |
| LAYER TWO | L2 - Pass Through Divider | 00051 | complete part | - | 4 | 0.91 | D | 0/90 | ±45 | ±45 | 0/90 |  |  |  |  |  |  |
| LAYER TWO | L2 - PP1 Divider | 00054 | complete part | - | 4 | 0.91 | D | 0/90 | ±45 | ±45 | 0/90 |  |  |  |  |  |  |
| LAYER TWO | L2 - S. EW - Rib | 00050 | complete part | vendor may propose laying up to alternate thickness 2.5 mm (i.e. to save a mold) | 6 | 1.33 | E | 0/90 | ±45 | 0/90 | 0/90 | ±45 | 0/90 |  |  |  |  |
| LAYER TWO | L2 - S. EW - Spring | 00048 | complete part | machine step down to 0.5 mm and chamfer | 11 | 2.37 | G | 0/90 | ±45 | 0/90 | ±45 | 0/90 | ±45 | 0/90 | ±45 | 0/90 | 0/90 |
| LAYER TWO | L2- S. EW - Cone | 00047 | complete part | - | 5 | 1.12 | B | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |  |  |  |  |
| LAYER ZERO | L0 - C Ring | 00007 | complete part | - | 5 | 1.12 | B | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |  |  |  |  |
| LAYER ZERO | L0 - Pass Through Divider | 00022 | complete part | - | 4 | 0.91 | D | 0/90 | ±45 | ±45 | 0/90 |  |  |  |  |  |  |
| LAYER ZERO | L0 - PP1 Divider | 00009 | complete part | - | 4 | 0.91 | D | 0/90 | ±45 | ±45 | 0/90 |  |  |  |  |  |  |
| LAYER ZERO | L0 - S. EW - Cone | 00005 | complete part | - | 5 | 1.12 | B | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |  |  |  |  |
| LAYER ZERO | L0 - S. EW - Rib | 00006 | complete part | vendor may propose laying up to alternate thickness 2.5 mm (i.e. to save a mold) | 6 | 1.33 | E | 0/90 | ±45 | 0/90 | 0/90 | ±45 | 0/90 |  |  |  |  |
| LAYER ZERO | L0 - S. EW - Spring | 00008 | complete part | machine step down to 0.5 mm and chamfer | 9 | 1.95 | F | 0/90 | ±45 | 0/90 | ±45 | 0/90 | ±45 | 0/90 | ±45 | 0/90 |  |
| SERVICE BARREL | SB - Cylinder | 00082 | complete part | - | 10 | 2.16 | A.1 | 0/90 | 0/90 | 0/90 | 0/90 | ±45 | ±45 | 0/90 | 0/90 | 0/90 | 0/90 |

* Expected thickness, including surface texture