## Slide 1: MIT 3.071 Amorphous Materials 9: Glass Strengthening
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 13.8, Ch. 18.12
Introduction to Glass Science and Technology
  Ch. 9, Section 4.4

## Slide 3
Defense
Strengthened Glass
Solar panels
Display
Architecture
Automobile & aviation
Consumer product

## Slide 4: Glass strengthening techniques
Reduce defect density or severity (decrease KI)
Introduce surface compressive stress (increase sf)
Engineer chemistry and microstructure (improve KIc)
Fire polishing
Surface etching
Surface coating
Heat treatment / tempering
Ion exchange
Crystallization
Composites
Engineer glass structures
Notes: Strengthening by surface crystallization is actually based upon two principles. Firstly, the relative contraction of the surface from the set point of the glass to room temperature after the onset of surface crystallization is less for the surface layers than for the glass substrate. Secondly, second-phase inclusions act to increase the effective Klc, which leads to strengthening for an assumed initial flaw distribution.

## Slide 5: Mechanical property dependence on mean coordination number in network glasses
In brittle materials, fracture toughness is determined by elastic modulus and bond energy
Mechanical property evolution in As-Se glass
Phys. Rev. B 82, 195206 (2010)

## Slide 6: Mechanical property dependence on mean coordination number in network glasses
In brittle materials, fracture toughness is determined by elastic modulus and bond energy
Mechanical property evolution in Ge-Se and Ge-Sb-Se glasses
J. Am. Cer. Soc. 90, 177 (2007)

## Slide 7: Thermal and chemical glass strengthening
Adv. Mater. 23, 4578 (2011)
Dd: case depth

## Slide 8: Heat-strengthened / tempered glass
Glass heated to 600 – 650 °C and force-cooled to generate surface compression

## Slide 9: Heat-strengthened / tempered glass
http://www.cardinalst.com/
Parabolic temperature & stress distribution
Glass heated to 600 – 650 °C and force-cooled to generate surface compression
Notes: Here c_P denotes volumetric heat capacity

## Slide 10: Heat-strengthened / tempered glass
Glass heated to 600 – 650 °C and force-cooled to generate surface compression
Air quenched
Additional stress contributions
  Fictive temperature gradient
  Viscoelastic relaxation
D : glass thickness

## Slide 11: Heat-strengthened / tempered glass
Glass heated to 600 – 650 °C and force-cooled to generate surface compression
ASTM C1048 standard
  Heat-strengthened glass: surface stress between 24 – 52 MPa, about twice stronger than annealed (untreated) glass
  Tempered glass: surface stress > 69 MPa (10,000 Psi), 4 to 5 times stronger than untreated glass
http://www.legardien.com/architectural-products
Notes: Tempered glass cannot be obtained by air quench (see previous slide)

## Slide 12: Glass goes ballistic: Bullet vs. Prince Rupert's Drop
Notes: Triboluminescence: https://www.youtube.com/watch?v=k5MORochIDw

## Slide 13: Quantifying the strength of Prince Rupert's drops
Appl. Phys. Lett. 109, 231903 (2016)

## Slide 14: Premature fracture of tempered glass
Nickel sulfide inclusion induced subcritical crack growth
Sulfur is introduced in a fining agent (Na2S) in glass making
The origin of nickel is unclear but likely due to contamination
Fracture 3, 985 (1977)
Notes: https://failures.wikispaces.com/Glass+Breakage+-+Nickel+Sulfide+Inclusions

## Slide 15: Chemical strengthening
Ion exchange in salt bath
Interdiffusion process
  Kinetics limited by slow-moving ion species
  Compressive strain impedes diffusion
Typical case depth in soda-lime glass: 25 to 35 mm
Only applies to alkali/alkali earth glasses
Int. J. Appl. Glass Sci. 1, 131 (2010)
Notes: The process temperature has to be lower than the annealing point to prevent stress relaxation
Advantages over tempering: higher surface stress, the possibility of application to shaped articles (curved or hollow) and of limited thickness, minimal optical distortion, absence of premature failure due to NiS inclusions

## Slide 16: Methods to increase case depth
Electric field, sonic or microwave assisted ion exchange
Use alkali aluminosilicate glasses with an alkali/alumina ratio of ~ 1
Use lesser size-disparity alkali pair for exchange: e.g. Li+ / Na+ instead of Na+ / K+
Add minor quantities of MgO or CaO in glass
Use mixed salt bath
Int. J. Appl. Glass Sci. 1, 131 (2010)
Notes: The high parent glass transition temperature and reduced NBOs in alkali aluminosilicate glasses with an alkali/alumina ratio of ~ 1 allow faster and deeper exchanges at higher immersion temperatures
Mixed salt bath: K from the bath replaces Na in the glass over a short distance and the Na from
the bath replaces Li in the glass over a larger penetration distance.

## Slide 17: Example: Corning Gorilla 5 (sodium aluminosilicate glass)
Addition of aluminum increases softening temperature and Tg
brittle
Increased surface hardness and minor impact on fracture toughness
Larger case depth than that of soda lime glass (50% larger than Gorilla 4)
Data from Corning product information
Notes: The fracture toughness number quoted is measured using a Chevron notch test before ion exchange.
In the case of strengthened glass, the “apparent” fracture toughness depends on crack geometry and testing method. See for example: Influence of Surface Stress on indentation Cracking, J. Am. Cerac. Soc. 69, 223 (1986).

## Slide 18: Sapphire vs. strengthened glass
 | Sapphire | Strengthened glass
Density | 3.97 g/cm3 | 2.4 – 2.5 g/cm3
Tensile strength | 0.27 – 0.41 GPa | N/A
Flexural strength | 0.9 GPa | > 0.8 GPa
Vickers Hardness | 21.5 GPa | 5.8 – 7 GPa
Fracture toughness | 2.3 MPa·m0.5 | 0.7 MPa·m0.5
Young’s modulus | 345 GPa | 60 – 75 GPa
Shear modulus | 145 GPa | 26 – 30 GPa
Refractive index (633 nm wavelength) | 1.75 – 1.77 | 1.50 – 1.52
Data compiled based on specifications of the following products (retrieved online 10/17/2017):
GT ASF Sapphire Cover; Schott Sapphire Glass; Corning Gorilla 5 Glass; Schott Xensation Cover Glass; Asahi Dragontrail Glass

## Slide 19: Glass still has more to offer: scratch resistance
Data from Corning product information
A surface coating layer with ~ 2.25 mm thickness and an index 0.03 higher (or lower) than the substrate glass at 600 nm wavelength

## Slide 20: Glass still has more to offer: native damage resistance (NDR)
Many starter flaws in deformed region
High residual stress
Glass better absorbs the force
No starter flaws in the deformed region
Lower residual stress
Alternative cover glass experiences Lateral Cracking
Glass with NDR better absorbs the force with Densification
Competitive Aluminosilicate Glass
After Ion Exchange
7 Newton Scratch
Glass with NDR
7 Newton Scratch
Science and Technology Division
.
© J. Mauro, Corning Incorporated.
.

## Slide 21: Glass still has more to offer: native damage resistance (NDR)
B
O
O
O
+
→
1/2 Na2O
B-
O
O
O
O
Na+
B3 → B4 conversion
Trigonal boron creates a more open glass structure that is able to densify via plastic deformation upon mechanical compression to avoid crack initiation
Chem. Mater. 28, 4267-4277 (2016)

## Slide 22
Notes: MOR: Modulus of Rupture, i.e. flexural strength

## Slide 23: Chemical strengthening of lithium aluminosilicate glass
Weibull plot after strengthening in varying ratios of NaNO3 + KNO3 baths
Am. Cer. Soc. Bull. 88, 27 (2009)

## Slide 24: Configurational design: laminated glass
Two or more layers of glass (annealed, heat-strengthened or tempered) bonded together by polymer interlayer(s)
Skywalk, Grand Canyon
Breaking pattern

## Slide 25: Facture toughness of laminated glass
Laminated glass is tougher than monolithic glass sheets
J. Eng. Mech. 124, 46 (1998).

## Slide 26: Properly design laminated structures are tougher than monolithic glass
 | Classical multilayer bending theory | The new multi-neutral-axis theory
Formulation |  | 
Assumption | No shear strain | The soft layer relieves the strain by shear deformation
Device Placement | Fixed near the substrate center | Readily tuned by adjusting the elastic contrast
Nat. Photonics 8, 643-649 (2014)

## Slide 27: Flexible glass photonic device fabrication
Si
Device layer
Silicone adhesive
Polyimide substrate
}
Tape
Sandwiched “Oreo” structure for stress relaxation
“Integrated flexible chalcogenide glass photonic devices,” Nat. Photonics 8, 643 (2014)

## Slide 28: Bend… but don’t break!
R ~ 0.3 mm
The multi-neutral axis design enables foldable, robust photonic circuits
Nat. Photonics 8, 643-649 (2014)

## Slide 29: Making stretchable photonics out of rigid glass
Grating coupler
Resonator
Devices on locally stiffened islands interconnected by serpentine waveguides
"Monolithically Integrated Stretchable Photonics," Light Sci. Appl. in press.

## Slide 30: Stretching serpentine glass waveguides
Serpentine waveguides are robust against repeated stretching
0% elongation
36% elongation
Before 3000 cycles @ 42%
After 3000 cycles @ 42%
"Monolithically Integrated Stretchable Photonics," Light Sci. Appl. in press.

## Slide 31: Summary
In many cases, glasses with critically connected network possess high modulus and toughness
Strengthening methods capitalizing on surface compressive stress
Configurational design can further enhance mechanical properties
 | Heat strengthened glass | Tempered glass | Chemically strengthened glass
Surface stress | 24 – 52 MPa | > 69 MPa | Up to 1 GPa
Compressive stress depth | ~ 20% pane thickness | ~ 20% pane thickness | ~ 100 mm
Heat treatment temperature T | Tg < T < Tsoft | Tg < T < Tsoft | T < Tg
Risk of premature failure | N | Y | N