## Slide 1: Temperature Cycle

## Slide 2: Pressure Cycle
End of filling

## Slide 3: Flow path ratio
Flow path ratio is the ratio between L (the distance between the gate and the farthest point in the molding dimension) and T (the thickness of the part) .
When molding large or thin parts, the flow path ratio is calculated to determine if molten plastics can fill the mold cavity.
Polyethylene (PE) L/T = 280-100
Polypropylene (PP) L/T = 280-150
Polyvinyl chloride (PVC) L/T = 280-70
Polystyrene (PS) L/T = 300-220 Polycarbonate (PC) L/T = 160-90
Acrylonitrile butadienstylene
(ABS) L/T = 280-120
Polyamide (PA) L/T = 320-200
Rule of thumb

## Slide 4: Delivery
Sprue
A sprue is a channel through which to transfer molten plastics injected from the injector nozzle into the mold.
Runner
A runner is a channel that guides molten plastics into the cavity of a mold.
Gate
A gate is an entrance through which molten plastics enters the cavity.

## Slide 5: Runner balancing
balanced
Not balanced

## Slide 6: Jetting
This is the phenomenon where the part has a wire-shape flow pattern on the surface.
Cause
Due to inappropriate gate position, a flow of molten plastics into the cavity is cooled in a line shape and remains undissolved with other plastics flow coming later.
Solution
Raise the molten plastics and mold temperature, and increase injection speed to make the initial and later flows of molten plastics dissolve completely. Change the gate position to make the molten plastics touch the facing side before making a line shape.
Die swell
> Thickness, t
t

## Slide 7: Flow mark
This is a phenomenon where the initial flow of molten plastics which solidifies mixes with a later flow and remains undissolved. It develops distinctive patterns such as clouds, scales or tree rings.
Cause
Injection speed is too fast.
Mold or molten plastics temperature is too low.
Solution
Enlarge the gate area to decrease the speed of the molten plastics flowing through the gate.
Increase the pressure retention time for better pressure quality.

## Slide 8: Design for Manufacturing
Moldable: flow path ratio, machine size
Draft angle
Shrinkage
Reinforcements (ribs and bosses)
Cycle time
Appearance, defects
Balance, balance, balance!!

## Slide 9: Draft angle
for removing parts from the mold
1-2o, material, dimension, texture dependent
Cavity side smaller, core side larger.
Crystalline material has more shrinkage.
Amorphous material has smaller shrinkage.

## Slide 10: Shrinkage
L =  L
T =  T
: shrinkage rate
Resin Name Molding Shrinkage (%)
Polyethylene (PE) 1.5-6.0
Polypropylene (PP) 1.0-3.0
Polyvinyl chloride (PVC) 0.1-0.5 Polystyrene (PS) 0.2-0.6
Polycarbonate (PC) 0.5-0.8
Acrylonitrile butadienstylene 0.3-0.8
Polyamide (PA) 0.6-2.0

## Slide 11
Injection Molding

## Slide 13: Recycling of Plastics
State and Federal Regulation
Codes for plastics
  1 PET
  2 HDPE
  3 Vinyl/PVC
  4 LDPE
  5 PP
  6 PS
  7 Other
1