## Slide 1: Analysis of Casting Processes
Fluid mechanics for mold filling
Heat transfer for solidification
Thermodynamics, mass transfer and heat transfer for nucleation and growth
Materials behavior for structure-property relationships

## Slide 2: Mold Filling
Bernoulli’s equation
Reynold’s number
Turbulence
Injection Molding : Re ~ 10-4
h

## Slide 3: Sand v.s. Al mold demonstration
<number>
seconds
oC
Ostalloy 158, Tm: 70oC
Bismuth 50% Lead 26.7% Tin 13.3% Cadmium 10%

## Slide 4: Solidification Time : Sand Casting
<number>
Transient 1-D heat transfer
Solution
Solidification time
Chvorinov’s rule

## Slide 5: Solidification Time : Die Casting
<number>
Transient 1-D heat transfer
Solution
Solidification time

## Slide 6: Comparison: Sand Mold vs Metal Mold
<number>
Sand Mold
Sand casting
ts ~ (V/A)2
Metal Mold
Die casting
ts ~ (V/A)1

## Slide 7: Alloy Solidification
<number>
Schematic illustration of alloy solidification and temperature distribution in the solidifying metal. Note the formation of dendrites in the mushy zone.
Dendrites formation
Constitutional supercooling

## Slide 8: Constitutional Supercooling
<number>
Any bump, or protuberance, extending into the liquid “samples” the stability of the liquid phase. If the liquid is constitutionally supercooled, the bump grows, whereas if the liquid is above its liquidus, the bump melts back.
Bump, or
perturbation
v
Constitutionally supercooled
stable
Cl(x)
Tl(x)
T (x)
v
v

## Slide 9: Constitutional Supercooling
<number>
unstable
stable

## Slide 10: Solidification Patterns
<number>
Figure 10.4 (a) Solidification patterns for gray cast iron in a 180-mm (7-in.) square casting. Note that after 11 min. of cooling, dendrites reach each other, but the casting is still mushy throughout. It takes about two hours for this casting to solidify completely. (b) Solidification of carbon steels in sand and chill (metal) molds. Note the difference in solidification patterns as the carbon content increases. Source: H. F. Bishop and W. S. Pellini.

## Slide 11: Sand Mold Features
<number>
Dimensional, Thermal and Chemical stability at high T
Size and shape
Permeability, Wettability by molten metal
Collapsibility
Cheap: Availability and consistency
Green sand: sand+clay+water
Notes: <number>

## Slide 12: Sequence of Operations for Sand Casting
<number>

## Slide 13: Patterns for Sand Casting
<number>
Figure 11.6 A typical metal match-plate pattern used in sand casting.
Figure 11.7 Taper on patterns for ease of removal from the sand mold.

## Slide 14: Normal Shrinkage Allowance for Some Metals Cast in Sand Molds
<number>
Notes: <number>

## Slide 15: Pattern Design Considerations (for Aluminum)
<number>
Shrinkage allowance: 1.3%
Machining allowance: 1/16”
Minimum thickness: 3/16”
Parting line
Draft angle: 3 to 5 % (more on the core)

## Slide 16: Squeeze Heads
<number>
Figure 11.9 Various designs of squeeze heads for mold making: (a) conventional flat head; (b) profile head; (c) equalizing squeeze pistons; and (d) flexible diaphragm. Source: © Institute of British Foundrymen. Used with permission.
Uniform compaction

## Slide 17: Gating System: Sprue, Runner, and Gate
<number>
Rapid mold filling
Minimizing turbulence
Avoiding erosion
Removing inclusions
Controlled flow and thermal conditions
Minimizing scrap and secondary operations

## Slide 18: Riser: Location and Size
<number>
Casting shrinkage
Directional solidification
Scrap and secondary operation
Temperature gradient rising toward riser
Riser
Slow rate
Fast rate
Intermediate rate
Progressive solidification :
Directional solidification

## Slide 19: Casting Design Modifications
<number>
Suggested design modifications to avoid defects in castings. Note that sharp corners are avoided to reduce stress concentrations.
Large flat areas warp  ribs and serration
Notes: <number>

## Slide 20: Hot Tears
<number>
Figure 10.11 Examples of hot tears in castings. These defects occur because the casting cannot shrink freely during cooling, owing to constraints in various portions of the molds and cores. Exothermic (heat-producing) compounds may be used (as exothermic padding) to control cooling at critical sections to avoid hot tearing.

## Slide 21: Casting Cross-Sections hot spots
<number>
Figure 12.2 Examples of designs showing the importance of maintaining uniform cross- sections in castings to avoid hot spots and shrinkage cavities.
Notes: <number>

## Slide 22: Avoiding Shrinkage Cavities
<number>
Examples of design modifications to avoid shrinkage cavities in castings. Source: Steel Castings Handbook, 5th ed. Steel Founders' Society of America, 1980. Used with permission.
Notes: <number>

## Slide 23: Internal and External Chills
<number>
Various types of (a) internal and (b) external chills (dark areas at corners), used in castings to eliminate porosity caused by shrinkage. Chills are placed in regions where there is a larger volume of metals, as shown in (c).

## Slide 24: Parting Line
<number>
Figure 12.5 Redesign of a casting by making the parting line straight to avoid defects. Source: Steel Casting Handbook, 5th ed. Steel Founders' Society of America, 1980. Used with permission.
Notes: <number>

## Slide 25: Casting Design Modifications
<number>
Figure 12.6 Examples of casting design modifications. Source: Steel Casting Handbook, 5th ed. Steel Founders' Society of America, 1980. Used with permission.
Notes: <number>

## Slide 26: Desirable and Undesirable Die-Casting Practices
<number>
Figure 12.7 Examples of undesirable and desirable design practices for die-cast parts. Note that section-thickness uniformity is maintained throughout the part. Source: American Die Casting Institute.

## Slide 27: Expendable Pattern Casting (Lost-foam)
<number>
Figure 11.15 Schematic illustration of the expendable pattern casting process, also known as lost foam or evaporative casting.

## Slide 28: Lost Foam Casting
<number>

## Slide 29: Advantages of Lost Foam Casting
<number>
Simpler, cheap PS
No parting line
No cores
One-piece flask
Freedom of design, complex shapes, fine detail
Minimum handling of sand
Ease of cleaning and secondary operation
Automation for volume production
Al engine blocks, cylinder head, crank shaft, manifolds, etc.

## Slide 30: Investment Casting
video clip, J. Colton, Georgia Tech.
<number>
Figure 11.18 Schematic illustration of investment casting, (lost-wax process). Castings by this method can be made with very fine detail and from a variety of metals. Source: Steel Founders' Society of America.

## Slide 31: Advantages of Investment Casting
<number>
Intricate geometry
Close dimensional tolerance
Superior surface finish
High-melting point alloys

## Slide 32: Investment Casting of a Rotor
<number>
Figure 11.19 Investment casting of an integrally cast rotor for a gas turbine. (a) Wax pattern assembly. (b) Ceramic shell around wax pattern. (c) Wax is melted out and the mold is filled, under a vacuum, with molten superalloy. (d) The cast rotor, produced to net or near-net shape. Source: Howmet Corporation.

## Slide 33: Hot-Chamber Die-Casting Machine
<number>
Figure 11.24 (b) 800-ton hot-chamber die-casting machine, DAM 8005 (made in Germany in 1998). This is the largest hot-chamber machine in the world and costs about $1.25 million.
(b)
http://www.me.gatech.edu/jonathan.colton/me4210/hotchamber.swf
http://www.me.gatech.edu/jonathan.colton/me4210/coldchamber.swf

## Slide 34: Advantages of Die Casting
High production rates
Closer dimensional tolerances
Superior surface finish
Improved mechanical properties
Al, Mg, , Zn, Cu
0.5 million shots, die life

## Slide 35: Centrifugal Casting Process
<number>
Figure 11.27 Schematic illustration of the centrifugal casting process. Pipes, cylinder liners, and similarly shaped parts can be cast with this process.

## Slide 36: Squeeze-Casting (liquid metal forging)
<number>
Figure 11.29 Sequence of operations in the squeeze-casting process. This process combines the advantages of casting and forging.

## Slide 37: Cost - Casting
Sand casting
    Tooling and equipment costs are low
    Direct labor costs are high
    Material utilization is low
    Finishing costs can be high
Investment casting
    Tooling costs are moderate depending on the complexity
    Equipment costs are low
    Direct labor costs are high
    Material costs are low
Die casting
    Tooling and equipment costs are high
    Direct labor costs are low to moderate
    Material utilization is high

## Slide 38: Quality - Casting
Sand casting
    Tolerance (0.7~2 mm) and defects are affected by shrinkage
    Material property is inherently poor
    Generally have a rough grainy surface
Investment casting
    Tolerance (0.08~0.2 mm)
    Mechanical property and microstructure depends on the method
    Good to excellent surface detail possible due to fine slurry
Die casting
    Tolerance (0.02~0.6 mm)
    Good mechanical property and microstructure due to high pressure
    Excellent surface detail

## Slide 39: Rate - Casting
Sand casting
    Development time is 2~10 weeks
    Production rate is depending on the cooling time : t~(V/A)2
Investment casting
    Development time is 5~16 weeks depending on the complexity
    Production rate is depending on the cooling time : t~(V/A)2
Die casting
    Development time is 12~20 weeks
    Production rate is depending on the cooling time : t~(V/A)1

## Slide 40: Flexibility - Casting
Sand casting
    High degree of shape complexity (limited by pattern)
Investment casting
    Ceramic and wax cores allow complex internal configuration but costs increase significantly
Die casting
    Low due to high die modification costs