## Slide 1: MIT 3.071 Amorphous Materials 10: Electrical and Transport Properties
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 14, Ch. 16
Introduction to Glass Science and Technology
  Ch. 8
3.022 ionic conductivity
3.024 band gap, band diagram, engineering conductivity

## Slide 3: Basics of electrical conduction
Electrical conductivity
Einstein relation
s : electrical conductivity
n : charge carrier density
Z : charge number
e : elementary charge
m : carrier mobility
D : diffusion coefficient
v : carrier drift velocity
E : applied electric field
Both ions and electrons contribute to electrical conductivity in glasses

## Slide 4: Ionic conduction in crystalline materials
Vacancy mechanism
Interstitial mechanism

## Slide 5: Ionic conduction pathway in amorphous solids
There are low energy “sites” where ions preferentially locate
Ionic conduction results from ion transfer between these sites
Ionic conduction is thermally activated
2-D slices of regions with Li site energies below a threshold value in Li2O-SiO2 glasses
Phys. Chem. Chem. Phys. 11, 3210 (2009)

## Slide 6: A tale of two valleys
Assuming completely random hops, the average total distance an ion moves after M hops in 1-D is:
Average diffusion distance:
Average spacing between adjacent sites: d
Electric field E = 0
(1-D)
(3-D)
(1-D)
(3-D)
Ion hopping frequency: n
For correlated hops:
+

## Slide 7: A tale of two valleys
Attempt (vibration) frequency: n0
Frequency of successful hops (ion hopping frequency):
Barrier height DEa
Electric field E = 0
+
Equal probability of hopping along all directions: zero net current

## Slide 8: A tale of two valleys
Energy difference between adjacent sites: ZeEd
Hopping frequency → :
Hopping frequency ← :
Net ion drift velocity:
DEa
Electric field E > 0
+
ZeEd
Notes: Note that the symbol v for velocity is bold and is different from the hopping frequency Nu
The ½ factor signifies bidirectional hopping

## Slide 9: A tale of two valleys
Ion mobility
Electrical conductivity (1-D, random hop)
Einstein relation (3-D, correlated hops)
DEa
Electric field E > 0
+
ZeEd

## Slide 10: Temperature dependence of ionic conductivity
1/T (× 1,000) (K-1)
Dispersion of activation energy in amorphous solids leads to slight non-Arrhenius behavior
Phys. Rev. Lett. 109, 075901 (2012)

## Slide 11: Ionic conductivity in soda-lime glass

## Slide 12: Theoretical ionic conductivity limit in glass
When T → ∞, s → s0 /T
Extrapolation of the Arrhenius plot agrees with infrared spectroscopic measurements in ionic liquids (molten salts)
Note that s0 has a unit of W·cm·K
Solid State Ionics 18&19, 72 (1986)
Annu. Rev. Phys. Chem. 43, 693 (1992)

## Slide 13: Fast ion conductors / superionic conductors
Acta Mater. 61, 759 (2013)
Notes: Some glasses are more conductive than their crystalline counterparts and some are not

## Slide 14: Band structures in defect-free crystalline solids
All electronic states are labeled with real Bloch wave vectors k signaling translational symmetry
All electronic states are extended states
No extended states exist in the band gap

## Slide 15: Band structures in defect-free crystalline solids
In the band gap, wave equation solutions have complex wave vectors k
Kittel, Introduction to Solid State Physics, Ch. 7

## Slide 16: Anderson localization in disordered systems
Localization criterion: V0 / J > 3
P. W. Anderson
Disorder leads to (electron, photon, etc.) wave function localization

## Slide 17: Anderson localization in disordered systems
Extended states (Bloch states)
Localized states

## Slide 18: Density of states (DOS) in crystalline and amorphous solids
E
DOS
Conduction band
Valence band
Band gap
E
DOS
Conduction band
Valence band
Crystalline solids
Mobility edge
Mid-gap states
Urbach tail
Amorphous solids
Defect states

## Slide 19: Tauc gap and Tauc plots
Tauc gap ET definition:
It is merely a fitting parameter and has little physical significance!
ET = 3.3 eV
a – absorption coefficient
ħw – photon energy

## Slide 20: Extended state conduction
Extended state conductivity:
Drift mobility mex increases with temperature (T → ∞, ftrap → 0)
Extended state conductivity follows Arrhenius dependence
m0 : free mobility
ftrap : fraction of time in trap states
Electron drift mobility in a-Si:H
R. Street, Hydrogenated Amorphous Silicon, Ch. 7
Electron mobility in c-Si: 1400 cm2 V-1 s-1

## Slide 21: Hopping conduction via localized states
Fixed range hopping: hopping between nearest neighbors
  Hopping between dopant atoms at low temperature
Variable range hopping (VRH)
  Hopping between localized states near EF
E
DOS
Mobility edge
  EF
R
g
x
y
z

## Slide 22: Variable range hopping
Hopping probability
Within distance R, the average minimal energy difference DE is:
Optimal hopping distance:
x
y
z
R

## Slide 23: DC conductivity in amorphous semiconductors
lns
1/T
Extended state conduction
Variable range hopping
Measured DC conductivity
VRH is most pronounced at low temperature

## Slide 24: VRH in As-Se-Te-Cu glass
Near room temperature, mixed ionic and extended state conduction
At low temperature, variable range hopping dominates
J. Appl. Phys. 101, 063520 (2007)

## Slide 25: Summary
Basics of electrical transport
  Conductivity: scalar sum of ionic and electronic contributions
  Einstein relation
Ionic conductivity
  Occurs through ion hopping between different preferred “sites”
  Thermally activated process and non-Arrhenius behavior

## Slide 26: Summary
Electronic structure of amorphous semiconductors
  Anderson localization: extended vs. localized states
  Density of states
  Mobility edge
  Band tail and mid-gap states
Extended state conduction
  Free vs. drift mobility
  Thermally activated process
Localized state conduction
  Fixed vs. variable range hopping
  Mott’s T -1/4 law of VRH
E
DOS
Conduction band
Valence band
Mobility edge
Mid-gap states
Urbach tail