## Slide 1: MIT 3.071 Amorphous Materials 5: Viscosity of Glass
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 9
Introduction to Glass Science and Technology
  Ch. 6

## Slide 3: The pitch drop experiment
The pitch drop experiment is a long-term experiment which measures the flow of a piece of pitch (asphalt)
The most famous version of the experiment was started in 1927 by Professor Thomas Parnell of the University of Queensland in Brisbane, Australia. The ninth drop fell on 24 April 2014, allowing the experimenters to calculate that pitch has a viscosity approximately 230 billion times that of water.
Ig Nobel Prize in Physics, 2005

## Slide 4: Is glass a solid or a viscous liquid?
“It is well known that panes of stained glass in old European churches are thicker at the bottom because glass is a slow-moving liquid that flows downward over centuries.”
“Successful read/write of digital data in fused silica glass with a recording density equivalent to Blu-ray Disc™, enabling both greater capacity using 100 recording layers and long storage life of 300 million years.”
Hitachi Ltd. Press Release 2014
Notes: The question is asking about the rheological properties of glass – glasses are thermodynamically different from glass forming liquids as can be seen from the H-T diagram and the potential energy landscape.

## Slide 5: Is glass a solid or a viscous liquid?
V
T
Tm
Supercooled liquid
Glass
Solid
Elasticity
instantaneous, transient
Liquid
Viscosity
time-dependent, permanent
E : Young’s modulus
G : shear modulus
h : viscosity (unit: Pa·s or Poise)
Notes: Mathematically similar forms of shear deformation in elastic solid and viscous liquid lead to “viscosity-elasticity analogy”, a useful method for solving viscous flow or shear deformation problems.

## Slide 6: Microscopic origin of elasticity and viscosity
Elasticity: attractive and repulsive forces between atoms
Viscosity: motion of atoms/molecules relative to their neighbors (relaxation)
  Conformation change of (macro)molecules
  Vacancy diffusion
  Dislocation motion
Different relaxation mechanisms have distinctive relaxation time scales
Strong inter-atomic/molecular bonds give rise to high viscosity
Notes: 1 Pa·s = 10 P (Poise) = 1,000 cP

## Slide 7: Temperature dependence of elasticity
Relatively weak temperature dependence
M. R. Vukcevich, J. Non-cryst. Sol., 11, 25-63 (1972).

## Slide 8: Temperature dependence of viscosity
Viscous flow is a thermally activated process
In general, the activation energy DEa is temperature dependent

## Slide 9: The Angell plot and fragility
Science 267, 1924-1935 (1995)
0
1
Glass transition temperature Tg
Fragility parameter
Fragility has nothing to do with mechanical properties of glass!
Notes: Why does the Angell plot converge at high temperatures (at least for metals): https://www.osti.gov/scitech/servlets/purl/1185365; also see: Phys. Rev. B 83, 212202 (2011).

## Slide 10: Strong vs. fragile glass forming liquids
Strong liquids
Arrhenius equation
Covalent glass forming liquids
Fragility often exhibits a minimum at the rigidity percolation threshold ( )
Fragile liquids
Vogel-Fulcher-Tammann (VFT) equation (Williams-Landel-Ferry equation)
Ionic and molecular liquids
Decrease of molecular cluster size as temperature rises
Notes: The VFT/WLF equation is a consequence of time-temperature superposition

## Slide 11: The MYEGA equation of viscosity
The VFT equation diverges at low temperature
The Mauro-Yue-Ellison-Gupta-Allan (MYEGA) equation:
Proc. Nat. Acad. Sci. U.S.A. 106, 19780-19784 (2009)

## Slide 12: Viscosity reference points
h (Pa·s)
101
103
106.6
1012
1013.5
Melting point
Working point
Softening point
Annealing point (Tg)
Straining point
Glass blowing
Fiber drawing
Float glass
Lehr annealing
Working range
Pitch: 2.3 × 108

## Slide 13: Composition dependence of viscosity
High network connectivity and strong bonds lead to high viscosity

## Slide 14: Mixed alkali effect (MAE)
Simultaneous presence of two alkali modifiers in glass leads to non-additive behavior (in particular transport properties)
Na2O
K2O
Na2O
K2O
J. Non-Cryst. Solids 1, 235 (1969);
J. Non-Cryst. Solids 21, 343 (1976);
Phys. Rev. Lett. 90, 155507 (2003).
Possible mechanism: mutual blocking of transport pathways by the two ions
Notes: Note that viscosity decreases with mix ions although ionic conductivity increases with mixed ions

## Slide 15: The thermometer effect
“In the last century and before, most thermometers were made of ‘Thüringer Glas’ which contains silica, lime and, more importantly, equal portions of (mobile) sodium and potassium ions. The problem with these thermometers was that they were rather inaccurate. If a calibrated thermometer was put into boiling water and later into ice of 0 °C, the thermometer did not show 0.0 °C, but about −0.5 °C. This so-called zero point depression took several months to vanish, if the thermometer was stored at room temperature. If it was heated up and cooled down, the effect occurred again. Weber found out in 1883 that this unwished relaxation effect could be diminished by a factor of 10 if only one type of alkali ion (sodium or potassium) was present in the glass, and little later Schott developed the first accurate Li-based thermometer.”
From Solid State Ion. 105, 1-13 (1998)

## Slide 16: Non-Newtonian behavior
Shear stress s
Shear rate
Bingham plastic
Shear thinning
Shear thickening
Newtonian fluid
Rate dependent viscosity

## Slide 17: Non-Newtonian behavior
Rate dependent viscosity
Viscosity h
Shear rate
Bingham plastic
Shear thinning
Shear thickening
Newtonian fluid
Hydroclustering (Image from Wiki)

## Slide 18: Non-Newtonian behavior
Rate dependent viscosity
Viscosity h
Shear rate
Bingham plastic
Shear thinning
Shear thickening
Newtonian fluid
Nanoscale 6, 10470 (2014).

## Slide 19: Non-Newtonian behavior of soda-lime glass
Shear thinning
J. Non-Cryst. Solids 105, 313-322 (1988)
Notes: The limiting stress corresponds to the cohesive strength of glass

## Slide 20: Viscosity measurement: viscometry
h (Pa·s)
103
106.6
1012
1013.5
Melting point
Working point
Softening point
Annealing point (Tg)
Straining point
106
Rotating cylinder
Parallel plate
105
109
107
1013
Beam bending
101

## Slide 21: Precision viscometry based on optical interferometry
Corning Inc.
“… the data reported are related to a single fused silica plate whose absolute shape was monitored over a period of 6 years during which the plate maintained the same posture; … The deformations that have to be detected are at the scale of the nanometre, over a lateral size of 100-150 mm…”
M. Vannoni et al., Eur. Phys. J. E 34, 92 (2011).

## Slide 22: Is glass a solid or a viscous liquid?
“Chocolate Melts,
Flowers Wilt,
Diamonds are Forever”
Glasses
“Depending on the thermal history of the glass, the room temperature viscosity is on the order of 1024 to 1025 Pa·s... Using analytical expressions to describe the glass flow over a wall, we calculate a maximum flow of ~1 nm over a billion years.”
DOI: 10.1111/jace.15092

## Slide 23: Summary
Constitutive relations for linear elasticity and Newtonian viscosity
  Elastic deformation: instantaneous, transient
  Viscous flow: time-dependent, permanent
Temperature dependence of elasticity and viscosity
  Elasticity: results from interatomic forces with minimal temperature dependence
  Viscosity: motion of atoms/molecules with respect to neighbors, thermally activated process

## Slide 24: Summary (cont’d)
Fragility of glass forming liquids: temperature dependence of activation energy in viscous flow
  Strong liquid: Arrhenius equation
  Fragile liquid: VFT equation, size of collective motion units (molecular clusters) increases as temperature decreases
Composition dependence of viscosity
  Mixed alkali effect
Non-Newtonian viscous flow
Viscometry techniques