## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 12: Photodetectors
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: References
Fundamentals of Photonics
  Ch. 17
Photonics: Optical Electronics in Modern Communications
  Ch. 10 & 11
Handbook of Silicon Photonics
  Ch. 10, J. Michel et al.
Handbook of Optics, Volume II
  Ch. 26, J. Bowers and Y. Wey
Infrared Detectors and Systems
  E. L. Dereniak and G. D. Boreman

## Slide 3: Photodetectors: devices used for detection of light
Digital photography
Vision
Communications
Medical imaging

## Slide 4: Classification of photodetectors
Thermal detectors
Thermopile
Bolometer
Pyroelectric detector
…
Photon detectors
Photoconductor
Photovoltaic detector
MSM detector
Photomultiplier
Quantum well infrared photodetector (QWIP)
Schottky barrier diode
…
Reference:
https://www.rp-photonics.com/thermal_detectors.html

## Slide 5: Absorption in semiconductors
Sze, Physics of Semiconductor Devices
Wavelength-energy conversion: l (mm) = 1.24 / Eg (eV)
Heavier atoms generally result in smaller bandgap

## Slide 6: Photoconductive detector
I
V
Dark
Light
Ch. 13, Principles of Biophotonics
S = wd
Quantum efficiency:
Carrier photo-generation rate:
Ohmic contacts

## Slide 7: Photoconductive detector
I
V
Dark
Light
Ch. 13, Principles of Biophotonics
S = wd
Photo-generated carrier density:
Photoconductivity:
Ohmic contacts

## Slide 8: Photoconductive detector
I
V
Dark
Light
Ch. 13, Principles of Biophotonics
S = wd
Photocurrent:
Responsivity
Constant voltage
Ohmic contacts

## Slide 9: Responsivity, speed, and linear dynamic range
Voltage
Geometric dimensions
Optical absorption
Semiconductor properties
Responsivity of photo-conductive detectors is dependent on measurement mode and detector geometry
After Fundamentals of Photonics
Unit: A/W

## Slide 10: Responsivity, speed, and linear dynamic range
Response time of photoconductors is primarily dictated by lifetime of photo-generated carriers
Inherent trade-off between responsivity and speed
Linear dynamic range is bound by the detector saturation limit and noise floor
Voltage
Geometric dimensions
Optical absorption
Semiconductor properties
Unit: A/W

## Slide 11: Responsivity, speed, and linear dynamic range
High-speed photo-conductors based on semiconductors with short lifetime
Optica 5, 44-51 (2018)
70.7% current amplitude, i.e. 50% electrical power
Relationship Between Rise Time and Bandwidth for a Low-Pass System

## Slide 12: Photoconductive gain
Detector gain
Wavelength in mm
Responsivity in A/W
+
-
+
+
+
-
Transit time
External circuit injects carriers into the semiconductor to ensure charge neutrality

## Slide 13: Photoconductor: constant current measurement
I
V
Dark
Light
Ch. 13, Principles of Biophotonics
S = wd
Photovoltage:
Constant current
Responsivity
(V/W)
Notes: The equations assume that the photoconductivity is considerably smaller than the dark conductivity

## Slide 14: Extrinsic photoconductive detectors
Extrinsic Semiconductor Detectors; Optica 1, 264 (2014)

## Slide 15: HgCdTe (MCT) photoconductive detectors
Advances in Infrared Detector Array Technology
Tunable band gap
High electron mobility (~ 105 cm2/Vs)
Hybrid integration with ROIC
© NASA
James Webb Space Telescope
© NASA

## Slide 16: Photovoltaic detector (photodiode)
Quantum efficiency:
I
V
Dark
Light
Responsivity
in the absence of gain
Reverse biased or zero bias
Photo-current
Ohmic contact
Notes: The carrier collection efficiency can be estimated by considering the carrier transit time and the carrier lifetime. It should be close to unity in a well-designed photodiode.

## Slide 17: Spectral response
Surface recombination
Weak band edge absorption
After Fundamentals of Photonics

## Slide 18: Speed of photovoltaic detectors: carrier transit
Drift region
Diffusion region
Iph
t
IPD
t
Drift current
Diffusion current
Carriers generated outside the depletion zone are not efficiently collected (h ↓)
Slow diffusion current component

## Slide 19: Speed of photovoltaic detectors: carrier transit
Image from electronics-notes.com
After Fundamentals of Photonics
Fully depleted p-i-n diode enhances carrier collection and speed
l
l

## Slide 20: Speed of photovoltaic detectors: carrier transit
After Fundamentals of Photonics
l
l
l
l
Shockley-Ramo
Each electron-hole pair contributes e collected charge
l
Notes: The Shockley-Ramo theorem refers to current signals induced on grounded conductors due to moving charges in the space between the conductors. The negative sign is there because it is referring to current generated in the external circuit.

## Slide 21: Speed of photovoltaic detectors: carrier transit
After Fundamentals of Photonics
l
l
Transit time spread
Electron and hole velocity difference
Carrier generation at different locations
Transit-time-limited 3-dB bandwidth
For top-bottom contacted photodiodes

## Slide 22: Speed of photovoltaic detectors: carrier transit
Phys. Rev. B 24, 1014 (1981)
Saturated velocity
Transit-time-limited 3-dB bandwidth
For top-bottom contacted photodiodes
Notes: As the applied electric field increases beyond a certain value, the carrier velocity no longer increases because the carriers lose energy through increased levels of interaction with the lattice, by emitting phonons and even photons as soon as the carrier energy is large enough to do so.

## Slide 23: Speed of photovoltaic detectors: RC delay
Equivalent circuit of a photodiode
R
C
Junction capacitance of p-n photodiodes
Junction capacitance of p-i-n photodiodes

## Slide 24: Optimizing speed of free-space photodiodes
J. Liu, Handbook of Silicon Photonics, Ch. 10.3
p
i
n
d
For a given device area, there is an optimal thickness for vertical p-i-n detectors

## Slide 25: Overcoming the bandwidth-responsivity trade-off
IEEE Photon. Technol. Lett. 17, 175 (2005)
Opt. Express 15, 3916 (2007)
Resonant cavity enhancement
Absorption enhancement
Spectral bandwidth penalty
Waveguide integration
Orthogonal light propagation and carrier collection path
Noise suppression

## Slide 26: Waveguide-integrated photodetectors
Nat. Photonics 4, 527 (2010)
Handbook of Silicon Photonics, Ch. 10.3
10x improvement in bandwidth-efficiency product

## Slide 27: CMOS/CCD image sensors
Reset gate
Source follower
Row selector
Photoelectrons collected in a n-type storage well (SW)
Upon reach out, the transfer gate (TG) is turned on such that photoelectrons are transferred to a capacitor known as “float diffusion” (FD)
This induced a voltage change of ΔV=Q/C, which drives the source follower (SF) transistor for transductance gain
Electric potential
IEEE J. Electron Devices Soc. 2, 33 (2014)

## Slide 28: Avalanche photodiode (APD)
Sze, Physics of Semiconductor Devices
Nat. Photonics 4, 527 (2010)
Avalanche breakdown: carrier multiplication via impact ionization
Separate-absorption-charge-multiplication (SACM) structure
Ionization ratio should be minimized to reduce avalanche gain noise and increase bandwidth
Notes: Ionization ratio: ratio of multiplication rates of two types of carriers

## Slide 29: Metal-semiconductor-metal (MSM) detectors
After Fundamentals of Photonics
Two back-to-back metal-semiconductor Schottky junctions
J. Brouckaert, Ph.D. Thesis
Schottky contacts

## Slide 30: Metal-semiconductor-metal (MSM) detectors
I
V
Carriers trapped in potential well: low current
Dark
Light
J. Brouckaert, Ph.D. Thesis

## Slide 31: Metal-semiconductor-metal (MSM) detectors
I
V
Current increases due to barrier height decrease
Light
Dark
J. Brouckaert, Ph.D. Thesis

## Slide 32: Metal-semiconductor-metal (MSM) detectors
I
V
VFB
Barrier vanishes; current saturates
Dark
Light
J. Brouckaert, Ph.D. Thesis

## Slide 33: Metal-semiconductor-metal (MSM) detectors
After Fundamentals of Photonics
MSM vs. p-i-n detectors
Simpler structure
Smaller capacitance per unit area: transit-time-limited high speed
Lower responsivity: electrode shadowing (back illumination, waveguide integration, transparent contact)
Dark current leakage: contact quality (Schottky barrier enhancement layer)

## Slide 34: Detector noise
I
t
Measured signal i(t)
Noise-free signal
Time domain
Standard deviation of noise
Signal-to-noise ratio (SNR)
with frequency-domain filter

## Slide 35: Detector noise
Photonics: Optical Electronics in Modern Communications, Ch. 10
www.ophiropt.com/laser--measurement/knowledge-center/article/10378
SNR can be improved by selecting a proper measurement frequency (if the noise is non-white) and decreasing noise bandwidth
I
t
Noise-free signal
PSD
frequency
Time domain
Frequency domain
B
Measured signal i(t)
fc
Notes: B = 1/2t applies to rectangular pulse: see Dereniak and Boreman Ch. 5.5

## Slide 36: Detector noise mechanisms
Photon shot noise
Dark current shot noise
  Shot noise is absent in photoconductors (with the exception of quantum shot noise)
Thermal noise (Johnson-Nyquist noise)
Generation-recombination noise (G-R noise)
1/f noise (flicker noise)
Circuit noise
Johnson–Nyquist Noise in Photodiode Circuits
Notes: https://www.hamamatsu.com/resources/pdf/ssd/e02_handbook_si_photodiode.pdf

## Slide 37: Detector SNR performance metrics
Noise equivalent power (NEP)
  Optical power producing unity SNR at 1 Hz noise bandwidth
  NEP measurement protocols
(Specific) detectivity D*
  Figure-of-merit (FOM) for evaluating a free-space detector’s SNR performance
  Assumption:
not applicable to photoconductors

## Slide 38: D* of different detectors
Characteristics and use of infrared detectors
D* is lower in narrow-gap semiconductors
Cooling improves D*
Photon detectors have higher D* compared to thermal detectors

## Slide 39: Bit error rate (BER)
On-off keying (OOK)
Received photon number m follows Poisson distribution
0
20
40
After Fundamentals of Photonics
Notes: Assumptions: 1) the 0 bit is defined as no photon received and 1 bit is defined as non-zero photon received; 2) no other noise than photon shot noise is considered, i.e. there is no noise associated with the 0 bit; and 3) the 0 and 1 bits have equal probability to appear

## Slide 40: Detector design optimization: photoconductors*
Absorber thickness d ↑
  Quantum efficiency ↑
  Responsivity ↑
  Johnson noise ↑ (SNR ?)
  3-dB bandwidth →
Spacing between electrodes l ↑
  Quantum efficiency →
  Responsivity ↓
  Johnson noise ↓ (SNR ↓)
  3-dB bandwidth →
*Constant current mode & in-plane electrode configuration

## Slide 41: Detector design optimization: photodiodes*
Absorber thickness d ↑
  Quantum efficiency ↑
  Responsivity ↑
  Current shot noise → (SNR ↑)
  3-dB bandwidth ↓
Detector active area A ↑
  Quantum efficiency →
  Responsivity →
  Current shot noise ↑ (SNR ↑, NEP ↑, D* →)
  3-dB bandwidth ↓
*Top-bottom contacted vertical p-i-n junction

## Slide 42: List of symbols
l – free-space wavelength
Eg – band gap energy
I – electric current
V – voltage
E – electric field
d – thickness of absorber (photoconductor), or thickness of depletion layer (photodiode)
t – photo-generated carrier lifetime (which is also the time constant of photoconductive detectors)
Dn / Dp – photo-generated carrier density

## Slide 43: List of symbols
h – quantum efficiency
a – absorption coefficient
Rl – optical reflectance on detector surface
l / w – length / width of absorber
Iph – irradiance of incident light (optical power per area)
A – active area of free-space detector
Vd – active volume of detector
ћ – reduced Planck constant, 1.055 × 10-34 J·s
w – angular frequency of light
Ds – photoconductivity

## Slide 44: List of symbols
– responsivity
g – detector gain
q – charge collected by circuit per photo-electron generated
v – drift velocity of carriers
f3dB – 3-dB bandwidth
tr – 10%-to-90% rise time
n / p – electron / hole density
z – carrier collection efficiency
i – instantaneous electric current signal

## Slide 45: List of symbols
IPD – photocurrent generated by a photodiode
Q – charge carried by the particle
ftr – transit-time-limited 3-dB bandwidth
ID – dark current
tRC – RC time constant
R – load resistance
C – detector junction capacitance
fRC – RC-limited 3-dB bandwidth
e – permittivity of detector active material at radio frequency

## Slide 46: List of symbols
dopt – optimal depletion layer thickness in a free-space detector that yields maximum bandwidth
VRT – reach-through voltage, beyond which MSM structure becomes fully depleted
VFB – flat-band voltage
si – noise current
– mean of current signal
f – frequency
PSD – noise power spectral density
B – noise bandwidth

## Slide 47: List of symbols
tint – measurement integration time
si,tot – total noise current including all noise contributions
e – elementary charge, 1.602 × 10-19 C
kB – Boltzmann constant, 1.38 × 10-23 m2·kg·s-2·K-1
T – thermodynamic temperature
NEP – noise equivalent power
D* – (specific) detectivity
BER – bit error rate
m – photon number received by the detector in a bit
P0 / P1 – probability of mistaking a 0-bit for 1 / a 1-bit for 0

## Slide 48: List of symbols
– average photon number received by the detector in a 1-bit
P(m) – probability of receiving m photons in a 1-bit