## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 5: Optical Resonant Cavities
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Optical resonance and resonant cavities
Optical resonant mode
  A time-invariant, stable electromagnetic field pattern (complex amplitude): an eigen-solution to the Maxwell equations
  Discretized resonant frequencies (eigen-values), i.e. these modes appear only at particular frequencies/wavelengths
  The modal fields are usually spatially confined in a finite domain
Optical resonant cavities (resonators)
  Devices that support optical resonant modes
Guided mode resonance, surface plasmon (polariton) resonance, and spoof surface plasmon resonance all refer to coupling to propagating modes, even though the same term “resonance” is referenced!

## Slide 3: Resonance: a mechanical analog
The resonance frequency of a string determines the pitch of sound it produces

## Slide 4: An infinite corridor in two mirrors
Electromagnetic waves between two perfect conductors (perfect mirrors)
Photon
Interference between back-and-forth reflected light
Standing wave formation

## Slide 5: A ray tracing model
Field amplitude: 1
…
t1, r1
t2, r2
a1
a2
…
an
α = 2pK/λ, L
Transmission coefficient
Ray tracing: summation of field amplitude, taking into account interference effect (the phase term)
when |r| < 1

## Slide 6: A close inspection of phasor summation
Transmission coefficient
A vector on the complex plane with a modulus/length ≤1
Firstly let’s look at a lossless cavity, i.e. α = 0, r1 = r2 = 1, and thus |r| = 1.
when |r| < 1
When kL ≠ Np, the vectors have different directions…
When kL = Np, the vectors are aligned (resonant condition).
Finite, non-vanishing transmitted intensity ONLY at resonance
Transmission spectra
ω
Peak FWHM = 0
Eq. (1)
Ttot
Phasor
FSR = pc/L
Free Spectral Range

## Slide 7: A close inspection of phasor summation
Transmission coefficient
When there is loss in the cavity, |r| < 1, and Eq. (1) holds
when |r| < 1
The transmission spectra have non-vanishing values even when the resonant condition is not met!
Transmission spectra
FSR = pc/L
Ttot
ω
Peak FWHM ≠ 0!
Eq. (1)
FSR: Free Spectral Range, peak separation
ω0 : resonant (angular) frequency
Δω : peak FWHM (Full Width at Half Maximum)
Quality factor Q:
Cavity finesse:
Extinction ratio: 10·log10(Tmax/Tmin)
A vector on the complex plane with a modulus/length ≤1
Phasor
Free Spectral Range

## Slide 8: Standing wave modes in F-P cavities
…
t1, r1
t2, r2
α = 2pK/λ, L
z
y
x
Cavity field:

## Slide 9: Standing wave modes in F-P cavities (cont’d)
…
N = 4
N = 5
N = 3
N = 2
N = 1

## Slide 10: Important concepts
Quality factor (Q-factor)
Finesse
Free spectral range (FSR, frequency domain)
W : Energy stored in the cavity in J
Ploss : Power loss in J/s or W
Include the factor 2 for travelling wave cavities
Include the factor 2 for travelling wave cavities

## Slide 11: Important concepts
Free spectral range (FSR)
Quality factor (Q-factor)
Finesse
FSR
W : Energy stored in the cavity in J
Ploss : Power loss in J/s or W
Full width at half maximum (FWHM) Dl should be calculated in linear scale, not in dB scale!
Reference: Juejun Hu, Ph.D. thesis, Appendix I
Traveling wave cavity
wavelength domain

## Slide 12: Optical loss in cavities
Round trip loss in an F-P cavity
Coupling loss (mirror loss):
  Non-unity mirror reflectance
  Independent of cavity length
Internal loss (distributed loss):
  Absorption/scattering of light in the cavity
  Loss proportional to cavity length L
Both Q and finesse scales inversely with cavity loss
  If distributed loss dominates, Q is independent of cavity length
  If coupling loss dominates, F is independent of cavity length

## Slide 13: Cavity perturbation theory
Resonant frequency shift due to perturbation
Material perturbation
Shape perturbation
The frequency shift scales with field intensity
e
e + De
e
e
S. Johnson et al., ”Perturbation theory for Maxwell’s equations with shifting material boundaries,” Phys. Rev. E 65, 066611 (2002).

## Slide 14: Standing wave vs. travelling wave cavities
Standing wave resonators
Photonic crystal (PhC) cavity / Fabry-Perot (F-P) cavity
Light forms a standing wave inside the cavity
Traveling wave resonators
Micro-ring/disk/racetrack resonators, microspheres
Light circulates inside the resonant cavity
2-d PhC cavity (top-view)
F-P cavity
Micro-disk
Micro-ring
Microsphere attached to a fiber end

## Slide 15: Whispering gallery mode
CW mode
Sound wave
Acoustics
Optics

## Slide 16: Standing wave vs. travelling wave cavities
Standing wave resonators
Light forms a standing wave inside the cavity
Traveling wave resonators
Light circulates inside the resonant cavity
z
z
z
z
Azimuthally symmetric travelling wave cavities support CW & CCW travelling wave modes as well as standing wave modes; and they are all degenerate (i.e. same resonant frequency)
z
z
z
+
=

## Slide 17: Degeneracy lifting in travelling wave cavities
Antisymmetric mode
Symmetric mode
Breaking the cavity azimuthal symmetry leads to resonance frequency splitting of standing wave modes
Nat. Photonics 4, 46 (2010).
APL 97, 051102 (2010).
IEEE JSTQE 12, 52 (2006).
PNAS 107, 22407 (2010).

## Slide 18: Optical coupling to cavity modes
Coupling approaches
  Free space coupling: F-P cavity
  Waveguide/fiber coupling: traveling wave cavities, PhC cavities
    Phase matching condition: efficient coupling
External Q-factor
  Energy loss due
  to coupling: Qex
  Extinction ratio
  depends on coupling
    Critical coupling
Opt. Lett. 33, 2500 (2008)

## Slide 19: Optical coupling to cavity modes
Coupling approaches
  Free space coupling: F-P cavity
  Waveguide/fiber coupling: traveling wave cavities, PhC cavities
    Phase matching condition: efficient coupling
External Q-factor
  Energy loss due
  to coupling: Qex
  Extinction ratio
  depends on coupling
    Critical coupling
Transmission (dB)
Wavelength (μm)
Increase coupling strength

## Slide 20: Critical coupling
Critical coupling
Complete power transfer: transmittance T = 0
Maximum field enhancement inside the resonator
Occurs when Qex = Qin
Under coupling
Qex > Qin
Over coupling
Qex < Qin
input
through = 0

## Slide 21: Critical coupling as a consequence of interference

## Slide 22: Matrix representation of directional couplers
a1
a2
b1
b2
a2
a1
b2
b1
Lossless coupler
Ch. 4, Photonics: Optical Electronics in Modern Communications, A. Yariv and P. Yeh
Linear, lossless, uni-directional, reciprocal, single-mode couplers
where
a1
a2
b1
b2
Coupler1
Coupler2
…
Coupler n
Cascadability:
Matrix K1
Matrix K2
Matrix Kn

## Slide 23: Coupling matrix approach for travelling wave cavities
a2
a1
b2
b1
Lossless
coupler
α : waveguide loss; β : propagation constant; L : round-trip length
5 mm
where
A. Yariv, Electron. Lett. 36, 321-322 (2000).

## Slide 24: Coupling matrix approach for travelling wave cavities
Coupler
1
a3
a1
a4
a2
Coupler
2
Coupler
3
a7
a5
a8
a6
a11
a9
a12
a10
Coupler
4
a15
a13
a16
a14
L6, a6
L5, a5
L4, a4
L3, a3
L2, a2
L1, a1
3rd order add-drop filters
Coupled resonator steady state solution:
2 equations for each coupler: 8 total
1 equation for each ring section: 6 total
2 known inputs: a1, a16
Compile the equation coefficients into a 14-by-14 matrix
Solve the set of linear equations
The algorithm can be automated to solve coupled cavities of arbitrary topology

## Slide 25: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
Loaded Q-factor at critical coupling:
Under coupling
Over coupling
Determining the coupling regime
Group index:
Variations of resonator Q among different azimuthal orders:
Opt. Lett. 37, 1586-1588 (2012)
* More generally, loss can be inferred from Q and extinction ratio even for non-critically-coupled rings: Matlab code for loss extraction

## Slide 26: Waveguide loss measurement
Cut-back
Camera imaging
Ring resonator
Fabry-Perot
IEEE PTL 6, 1244-1247 (1994)
Appl. Opt. 47, 6625-6630 (2008)
Opt. Express 27, 17876-17886 (2019)
Accurate determination of facet reflectance is the key

## Slide 27: Optical resonator: a ubiquitous platform
Selective spectral transmission/reflection
  Optical filters for WDM
Coherent optical feedback
  Lasers
Increased optical path (interaction) length
  Spectroscopy and sensing
  Modulators and switches
  Slow light: coupled resonator optical waveguide (CROW)
  Cavity-enhanced photodetector
Enhanced field amplitude (photon LDOS)
  Nonlinear optics
  Cavity quantum-electrodynamics (QED)
  Cavity optomechanics

## Slide 28: Wavelength Division Multiplexing (WDM)
Better use of existing fiber bandwidth
Little cross-talk between channels
Transparent to data format and rate
Mature technology

## Slide 29
See what the “FiOS boy” says about WDM!

## Slide 30: Wavelength Division Multiplexing (WDM)
Better use of existing fiber bandwidth
Little cross-talk between channels
Transparent to data format and rate
Mature technology
Multiplexing
De-multiplexing
λ1 λ2 λ3 …

## Slide 31: Ring resonator add-drop filter
λ1
λ2
•
•
• λn
λ1
λ2
…
λn
Add-drop filter design rules:
Low insertion loss: critical coupling, low WG loss
Low cross-talk:
large extinction ratio, FSR >> channel spacing
Flat response in the pass band
B. Little et al., J. Lightwave Technol. 15, 998 (1997).
B. Little et al., IEEE PTL 16, 2263 (2004).
T. Barwicz et al., JLT 24, 2207 (2006).
F. Xia et al., Opt. Express 15, 11934 (2007).
P. Dong et al., Opt. Express 18, 23784 (2010).

## Slide 32: Semiconductor lasers
AlGaAs-GaAs-AlGaAs double heterojunction lasers
n-type AlGaAs
GaAs
p-type AlGaAs
+
-
mirror
mirror
Laser output
Edge-emitting laser

## Slide 33: Vertical Cavity Surface Emitting Lasers (VCSELs)
On-wafer testing
Single longitudinal mode operation
Low threshold current
Long lifetime
http://www.rp-photonics.com/vertical_cavity_surface_emitting_lasers.html

## Slide 34: Vertical Cavity Surface Emitting Lasers (VCSELs)
← VCSEL
← VCSEL
← VCSEL

## Slide 35: Resonator optical sensors: refractometry
Y Y Y Y Y Y Y Y Y Y
Surface functionalization coating selectively binding to the target species
Species
The effective index change due to specific surface binding is used to detect target species
Refractometry relies on surface coatings to provide specificity

## Slide 36: Resonator optical sensors: refractometry
Light into waveguide
Resonant condition:
Resonator

## Slide 37: Resonator optical sensors: refractometry
Light into waveguide
Resonant condition:
Resonance shift:
Using resonance shift to detect molecular binding
Resonator

## Slide 38: Resonator optical sensors: absorption spectrocopy
Light into waveguide
Resonator
Resonant condition:

## Slide 39: Resonator optical sensors: absorption spectrocopy
Light into waveguide
Resonator
Effective optical path length:
Using extinction ratio change to detect optical absorption caused by target molecules

## Slide 40: Resonator optical sensors: refractometry
IEEE J. Sel. Top. Quantum Electron. 16, 654 (2010)
Low-cost, single-use passive photonic sensor chips with limit of detection down to < 10-6 RIU
Highly multiplexed analysis
On-chip reference resonators to calibrate temperature fluctuations
Maverick Detection System © Genalyte

## Slide 41: Silicon micro-ring switch/modulator
Refractive index change in silicon via free carrier dispersion effect: optical/electrical carrier injection
Low power consumption due to small footprint
V. Almeida et al., “All-optical control of light on a silicon chip,” Nature 431, 1081 (2004).
Q. Xu et al., “Micrometer-scale silicon electro-optic modulator,” Nature, 435, 325 (2005).

## Slide 42: The challenge: narrow band operation & fabrication/thermal sensitivity
Si waveguide cross-section 450 nm × 200 nm
2000 GHz
Q = 1,000

## Slide 43: Active thermo-optic compensation
Nanophotonics 3, 269 (2014)
Use transmittance variation from the resonator to perform feedback control on integrated heaters

## Slide 44: Towards electronic-photonic convergence
Nature 528, 534-538 (2015)

## Slide 45: Resources: VM-Lab Simulations
Ring resonators: add-drop configuration
  Wavelength
  Resonator size
  Coupling gap
Ring resonators: all-pass configuration

## Slide 46: List of symbols
a / b – field amplitude
t1 / r1 – amplitude transmission / reflection coefficient of mirror or coupler 1
k – wave vector of light in the cavity
r – round-trip amplitude transmission coefficient
T – transmittance (measured with intensity)
Q – quality factor, Q-factor
F – finesse
FSR – free spectral range
Dw – full width at half maximum of resonant peak measured with angular frequency

## Slide 47: List of symbols
w0 – angular frequency of light at resonance
l0 – resonant wavelength
L – cavity length
c – speed of light
W – energy stored in resonator
Ploss – energy loss rate (in J/s or W) of resonator
Dl – full width at half maximum of resonant peak measured in the wavelength domain
ng – group index
c0 – speed of light in vacuum (2.99792458 × 108 m/s)

## Slide 48: List of symbols
e – permittivity
E – electric field
– position vector
Qex – extrinsic quality factor, quality factor calculated from energy loss rate due to coupling to resonator
Qin – intrinsic quality factor, quality factor calculated from energy loss rate due to optical loss inside resonator
Qtot – loaded quality factor, which accounts for both coupling and intrinsic losses
k – (amplitude) cross coupling coefficient of resonator coupler

## Slide 49: List of symbols
a – waveguide loss
b – propagation constant
Qcr – loaded quality factor at critical coupling
neff – effective index
N – longitudinal modal index (a positive integer)
dl – resonant wavelength shift due to effective index change