## Slide 1: MSEG 803 Equilibria in Material Systems 12: Solution Theory
Prof. Juejun (JJ) Hu
hujuejun@udel.edu

## Slide 2: Gibbs theorem
Solid 1 consisting of N1 atoms on N1 lattice sites
Solid 2 consisting of N2 atoms on N2 lattice sites
Solid solution with the same lattice structure and completely random distribution of atoms
  Inter-atomic force are the same for all three types of atomic pairs: 1-1, 2-2, and 1-2
1
2
1+2

## Slide 3: Gibbs theorem
Ideal (random) solid solution
Entropy of mixing
1
2
1+2
Notes: The entropy of mixing is also consistent with the informational theory definition of entropy

## Slide 4: Gibbs theorem for ideal gas
Entropy of mixing ideal gases (at the same T and P):
Derivation: # of spatial “sites” m >> # of molecules n for ideal gas (classical limit of quantum statistics)
T, P, n1
T, P, n2
Same T and P :

## Slide 5: Ideal solid solutions
Inter-atomic force is the same for all types of bonds
Random mixing is always preferred!

## Slide 6: Regular binary solution theory
Assumptions:
  Random distribution of atoms
  Bond energy between 1-2 is different from those of 1-1 and 2-2
negative enthalpy of mixing: 1-2 type of hetero-polar bond energetically favorable
positive enthalpy of mixing: 1-1 and 2-2 types of homopolar bonds preferred
Site i
Site j
1
2

## Slide 7: Negative enthalpy of mixing

## Slide 8: Positive enthalpy of mixing (high T)

## Slide 9: Positive enthalpy of mixing (intermediate T)

## Slide 10: Positive enthalpy of mixing (low T)

## Slide 11: The intercept rule
The chemical potentials of components 1 and 2 are given by the intercept of the tangent line of the Gibbs free energy curve
x1
G
x1, x2
m1
m2
Pure 1
Pure 2
G(x1, x2)

## Slide 12: Phase composition determination
The composition of phases are determined by the common tangent lines on the Gibbs free energy curve
  Minimization of G
The curve is generally asymmetric for non-ideal solution solutions
x1,a
x1,b
DGmix at T = T0
m1
m2
a
b

## Slide 13
Gibbs free energy
Phase diagram
Miscibility gap
Miscible region
Convex G curve: miscible solution
Concave G curve: phase separation
Notes: Miscibility gap: the bond energy gain of homopolar bond formation dominates over the entropy of mixing

## Slide 14: Miscibility gap in Au-Ni alloy phase diagram

## Slide 15: Short range order (SRO)
Regular solution theory: random distribution of atoms
  Probability of forming 1-2 is the same as that of forming 1-1 and 2-2 bonds
Large negative enthalpy of mixing
  Bond energy of 1-2 bonds is much larger than average bond energy of 1-1 and 2-2 bonds
  Heteropolar bonds strongly preferred over homopolar bonds
  SRO maximizes the number of 1-2 hetero-polar bonds
  Binary phase with SRO at low T (DHmix dominates the contribution to DGmix)
Site i
Site j
1
2

## Slide 16: Short range order (SRO)
B2 ordering in BCC structures (atom 1 and 2 molar ratio 1:1)
Ordering in molar ratio 1:1 FCC structures is impeded by tetrahedral units

## Slide 17: Short range order (SRO)
Experimental validation of SRO phase formation vs. miscibility gap due to positive DHmix
  Structural characterization
  Calorimetry measurement
x1
T
SRO phase
x1
Miscibility gap due to positive DHmix
T

## Slide 18: Completely miscible solid/liquid solution
Liquid and solid phases each has its own G curve
Liquid phase has molar lower Gibbs free energy at high T
x1
T
Pure 1
Pure 2
l
s
x1
G (at T = T1)
Pure 1
Pure 2
l
s
T1

## Slide 19: Completely miscible solid/liquid solution
Liquid and solid phases each has its own G curve
Equilibrium phase composition is determined by the common tangent line
x1
T
x1,l
Pure 1
Pure 2
l
s
x1,s
x1
G (at T = T2)
x1,l
m1
m2
Pure 1
Pure 2
l
s
x1,s
T2

## Slide 20: Completely miscible solid/liquid solution
The term is larger (less negative) for
solids; thus at low T solid becomes the stable phase
x1
T
Pure 1
Pure 2
l
s
x1
G (at T = T3)
Pure 1
Pure 2
l
s
T3

## Slide 21: Eutectic phase diagram
x1
T
T1
b
l
x1
G (at T = T1)
Pure 1
Pure 2
l
b
a
a
Convex liquid phase Gibbs free energy curve lies everywhere below the G curves of a and b phases: homogeneous liquid phase l

## Slide 22: Eutectic phase diagram
x1
T
a
T2
b
l
x1
G (at T = T2)
Pure 1
Pure 2
l
a
b
Compositions of l, a and b phases are determined by the common tangents

## Slide 23: Eutectic phase diagram
x1
T
a
T3
b
l
x1
G (at T = T3)
Pure 1
Pure 2
l
a
b
Compositions of l, a and b phases are determined by the common tangent
Three phases share a common tangent at eutectic T

## Slide 24: Eutectic phase diagram
x1
T
a
T4
b
l
x1
G (at T = T4)
Pure 1
Pure 2
l
a
b
Compositions of a and b phases are determined by the common tangent