## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 13: Modulators and Switches
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: References
Fundamentals of Photonics
  Ch. 18 & 21
Photonics: Optical Electronics in Modern Communications
  Ch. 9
Handbook of Silicon Photonics
  Ch. 9, Marris-Morini et al.

## Slide 3: Optical modulators vs. optical switches
Optical modulator
  A device that can be used to manipulate a property of light
  Intensity modulator, phase modulator, polarization modulator, spatial light modulator (SLM), etc.
  Electro-optic modulator, electroabsorption modulator, acoustic-optic modulator, optomechanical modulator, etc.
Optical switch
  A device that establishes and releases connections among transmission paths
  Electro-optic switch, acoustic-optic switch, optomechanical switch, magneto-optic switch, etc.

## Slide 4: (Intensity) modulator characteristics
Contrast/extinction ratio:
Insertion loss (IL):
Power/energy consumption
Speed
  3-dB bandwidth
  Eye diagram
AC photocurrent
Modulation frequency (Hz)
1.5 dB
3-dB bandwidth
Light intensity (dB)
Time t

## Slide 5: Eye diagram
Opt. Express 21, 9722 (2013)
www.edn.com/eye-diagram-basics-reading-and-applying-eye-diagrams/;
DOI:10.1002/9781119264422

## Slide 6: Optical switch metrics
Insertion loss (IL):
Crosstalk
  Ratio of transmitted power from the target output port over the maximum leaked power from a “non-target” port
Power/energy consumption
Speed
m × n switch
m input ports
n output ports
2 × 2 switch
Bar state
Cross state

## Slide 7: Waveguide phase shifter/modulator
Refractive index n
Input mode
Output
Unmodulated phase delay:
Phase modulation:
Refractive index n + Dn
The phase modulation scales with waveguide length L and refractive index modulation Dn of the active material
The phase modulation () can be enhanced via slow light effect
Opt. Express 16, 16659 (2008)

## Slide 8: Thermo-optic waveguide phase shifter
Cladding
Core
Resistive heater
Cladding
Core
Metal vias
Metal heater
Doped waveguide heater
Simple structure
Applicable to all waveguide platforms
Increased thermal mass: large Pp·t
Complex fabrication
Only available in semiconductors
Superior heating efficiency

## Slide 9: Thermo-optic waveguide phase shifter
Metal heater
Doped waveguide heater
Simple structure
Applicable to all waveguide platforms
Increased thermal mass: large Pp·t
Complex fabrication
Only available in semiconductors
Superior heating efficiency
Opt. Express 27, 10456 (2019)

## Slide 10: Thermo-optic waveguide phase shifter
Opt. Express 22, 10487 (2014)
L = 61.6 mm, Pp = 25 mW, t = 1.2 ms, f3dB = 130 kHz, IL = 0.23 dB

## Slide 11: Thermo-optic waveguide phase shifter
Temperature profile
Voltage map
Opt. Express 22, 10487 (2014)
L = 61.6 mm, Pp = 25 mW, t = 1.2 ms, f3dB = 130 kHz, IL = 0.23 dB

## Slide 12: Electro-optic phase shifter: Pockels effect
LiNbO3-on-Si electro-optic phase shifter
Opt. Express 26, 23728 (2018)
High-speed operation (> 100 GHz), potential for low optical loss
Vp·L = 6.7 V·cm

## Slide 13: Free carrier plasma dispersion effect: Drude model
Free carrier plasma dispersion effect
Free carrier absorption
Figure of merit

## Slide 14: Free carrier plasma dispersion effect in Si
IEEE Photonics J. 3, 1171 (2011)

## Slide 15: Si phase shifters based on free carrier effect
 | Forward bias | Reverse bias
Index change Dn | ~ 10-3 | ~ 10-4
Insertion loss (Dj = p) | ~ 2 dB @ 1550 nm | ~ 5 dB @ 1550 nm
Bandwidth | ~ 1 GHz* | > 30 GHz
*Opt. Express 21, 11869 (2013)
Reverse biased Si p-i-n modulators are used for high-speed operation despite their high losses
Notes: It is possible use forward-bias modulators for high data rate transmission (e.g. 50 Gb/s), although the performance (in terms of Vpi*L) is severely compromised limited by the intrinsic device bandwidth.

## Slide 16
High-speed Si modulators
OFC 2019, Tu2H.2
Multiple doping levels to minimize electrical resistance while avoiding high optical losses

## Slide 17: Device platforms: interferometer modulator
Mach-Zehnder interferometer (MZI)
Phase shifter
Broadband operation; large footprint and power consumption
Traveling wave design: group velocity matching of microwave and optical signals
In Si p-i-n modulators, the applied phase shift is often < p

## Slide 18: Device platforms: 2 × 2 interferometer switch
Phase shifter
2 × 2 coupler
2 × 2 directional coupler
2 × 2 multimode interferometer (MMI)

## Slide 19: Device platforms: 2 × 2 interferometer switch
Phase shifter
j = 0
j = p/2
j = p/2
j = 0
Dj = 0
Phase shifter
j = 0
j = p/2
j = p/2
j = p
Dj = p
Cross state
Bar state

## Slide 20: Device platforms: micro-ring modulator
Light into waveguide
All-pass resonator
Resonant condition:

## Slide 21: Device platforms: micro-ring modulator
Light into waveguide
Resonance shift:
Small footprint, low power consumption
Narrowband operation: demands temperature stabilization
All-pass resonator

## Slide 22: Device platforms: 2 × 2 micro-ring switch
On resonance
Add port
Drop port
Through port
Off resonance
Small footprint, low power consumption
Narrowband operation: demands temperature stabilization

## Slide 23: Building an N × N switch network
DOI: 10.1109/SMC.2015.152
Cross-bar network
Benes network
 | Cross-bar | Benes
Element count | N 2 | N log2N − N/2
Contact count | 2N | 2N log2N − N
Non-blocking? | No | Yes

## Slide 24: Building an N × N switch network
MEMS micro-mirror
© Lucent Technologies
© Fujitsu
Scalable, mature technology
Low crosstalk
Relatively slow (~ ms)
Opt. Express 26, 16022 (2018)

## Slide 25: Electroabsorption modulator (EAM): Franz-Keldysh effect (FKE)
Energy
Position
FKE in Ge
Thin Solid Films 525, 110 (2012)
FKE takes place in uniform bulk semiconductors
Sub-gap absorption tail and above-gap absorption oscillation
Field-induced effect: ultrafast (sub-fs time scale)
EC0
EV0
Notes: Oscillations in above-bandgap absorption caused by overlap variations between electron standing waves

## Slide 26: Electroabsorption modulator (EAM): quantum-confined Stark effect (QCSE)
QCSE takes place in quantum wells (QWs)
Decreased transition energy and recombination efficiency
Field-induced effect: ultrafast (sub-fs time scale)

## Slide 27
High-speed Ge EAM based on FKE
Small footprint, low energy consumption
IL limited by indirect gap absorption
Nat. Photonics 2, 433 (2008)

## Slide 28
Applications: high-speed communications
Optical receiver (Rx) / transceiver
Transmitter driver circuit
Optical transmitter (Tx) / transceiver
Electronic digital signal
1
0
1
0
1
1
0
1
0
1
Optical digital signal
Receiver circuit
Electronic digital signal
1
0
1
0
1
Optical fiber / waveguide
Opt. Express 19, B777 (2011)
Fiber ribbon

## Slide 29
Applications: high-speed communications

## Slide 30
Applications: high-speed communications

## Slide 31
Applications: optical spectroscopy
input
detection
dL
-2 dL
22 dL
-23 dL
-25 dL
24 dL
DOWN
UP
DOWN
DOWN
UP
UP
DOWN
UP
Unique exponential scaling enables high performance within a chip-scale platform
IEEE J. Sel. Top. Quantum Electron. 23, 5900110 (2017)

## Slide 32
Applications: optical spectroscopy
Device fabricated using standard silicon photonics foundry service
Nat. Commun. 9, 4405 (2018)

## Slide 33
Applications: optical spectroscopy
Nat. Commun. 9, 4405 (2018)
Packaged with temperature control and standard optical fiber interface

## Slide 34: List of symbols
Ron/off – contrast/extinction ratio of intensity modulator
Pout (Von) / Pout (Voff) – instantaneous optical output power from an intensity modulator at its on / off state
Pin – input optical power into the intensity modulator
IL – insertion loss
l0 – free-space wavelength
b – propagation constant
L – phase shifter length
k0 – wave number in free space
neff – waveguide effective index

## Slide 35: List of symbols
ng – waveguide group index
n – refractive index of the active material
Dn – refractive index change of the active material
j – optical phase
Dj – phase modulation
G – confinement factor in the active material
g – fraction of electric field energy confined in the active material
f3dB – 3-dB bandwidth
t – time constant of modulation or switching

## Slide 36: List of symbols
Pp – power required to achieve p phase shift
Vp – voltage required to achieve p phase shift
Dk – change of imaginary part of refractive index in the active material
Da – absorption coefficient change of the active material
Eg – band gap energy
EC0 / EV0 – energy of conduction / valence band edge
N – optical channel count
j – number of optical switches